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Supporting Information SI 3.   Thermal degradation temperatures (Td), corresponding weight loss (WL), and residual mass of BC, Ag–PROB, Ag–PROB@BC, and Ag–PROB@BC–ZIF-8 obtained from TGA analysis.


	Sample
	Td1 (°C)
	Wd1 (%)
	Td2 (°C)
	Wd2 (%)
	Residue (%)

	BC
	352.83
	84
	468.61
	10
	0.57

	Ag-PROB@BC
	288.97
	23
	350.80
	46
	13.84

	Ag-PROB@BC/ZIF-8
	351.13
	41
	404.02
	20
	24.20

	Ag-PROB
	310.01
	61
	-
	-
	37.77




