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a) ATR-FTIR spectre of Polypropylene. HQI : 0.88772

[image: ]
b) ATR-FTIR spectre of Polyethylene. HQI:  0.80886  
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c) ATR-FTIR spectre of Styrene butadiene. HQI: 0.85149
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d) ATR-FTIR spectre of Ethylene propylene diene. HQI: 0.93234
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e) ATR-FTIR spectre of Polyacrylate polyester. HQI: 0.85177
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f) ATR-FTIR spectre of Polyvinyl formal.  HQI: 0.75197
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g) ATR-FTIR spectre of G19 EPDM-peroxide. HQI:  0.90299
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h) ATR-FTIR spectre of Ethylene propylene EPR 618337. HQI: 0.77643
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i) ATR-FTIR spectre of Bisphenol A epoxy. HQI: 0.77975 
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j) ATR-FTIR spectre of Polysulfide Caulking. HQI : 0.72931
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k) ATR-FTIR spectre of Polystyrene. HQI: 0.92845

Fig. 8S Selected ATR-FTIR transmittance spectra of main polymers detected in the spectral range of 650 to 4000 cm
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——— Current Sample
polyvinyl formal, Formal 82%, acetate 12%, hydroxyl 6% Granular CAS 63450-15-
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——— Current Sample

G19 EPDM-Peroxide cured Warco Run#1
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——— Current Sample

Ethylene Propylene EPR 618337 Run#3
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——— Current Sample
Bisphenol A epoxy cured with polypropylene glycol, 2 part epoxy
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——— Current Sample

Polysulfide Caulking, high CaCOg3 filler
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——— Current Sample

Polystyrene, clear solid part

T T T T T T T T
2000

500
Wavenumber (cm-1)





image1.png
——— Current Sample

Polypropylene, isotactic Pellets CAS 9003-07-0
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——— Current Sample
Polyethylene, chlorinated, Chlorine content 36 wt%, Kaolin clay impurity, CAS 647
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——— Current Sample

Styrene butadiene rubber, SBR, Rubber Toy Ball
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——— Current Sample
ETHYLENE PROPYLENE DIENE TERPOLYMER Ethylene 70% diene 4% Pellets
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——— Current Sample
Polyacrylate polyester window caulking, CaCO3 filler
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