Table S1: Particle size parameters and proximate analysis a

| Nº | Sample | d10 | d50 | d90 | PSD curve | d4,3 | d3,2 | SSA | Shape | PD | Method | M | V | A | FC | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | Almond shell |  | 44.3 |  | No | 75.3 | 26.5 | 0.227 | No |  | Laser diffraction |  |  |  |  | [28] |
| 2 | Almond shell | 13.2 | 44.2 | 133.2 | No |  |  |  | No | 2.71 | Laser diffraction | 8.3 | 64.97 | 21.72 | 5.01 | [142] |
| 3 | Bark (of pine) |  | 80 |  | Yes |  |  |  | Yes - SEM |  | Laser diffraction | 5.75 | 68.55 | 1.7 |  | [17] |
| 4 | Barley straw |  | 120 |  | Yes |  |  |  | Yes - SEM |  | Laser diffraction | 15.35 | 63.3 | 4.2 |  | [17] |
| 5 | Cacao |  | 92 |  | Yes |  |  |  | No |  | Laser diffraction | 7.8 |  |  |  | [143] |
| 6 | Cinnamonum campora, fraction 0-63 μm | 10.29 | 29.76 | 66.78 | Yes - fraction 0-500 μm |  |  | 0.35 | Yes - Polarized light microscopy |  | Laser diffraction | ≤ 5% |  |  |  | [112] |
| 7 | Cinnamonum campora, fraction 125-250 μm | 52.25 | 161.86 | 313.18 | Yes - fraction 0-500 μm |  |  | 0.07 | Yes - Polarized light microscopy |  | Laser diffraction | ≤ 5% |  |  |  | [112] |
| 8 | Cinnamonum campora, fraction 250-500 μm | 138.3 | 303.23 | 568.19 | Yes - fraction 0-500 μm |  |  | 0.04 | Yes - Polarized light microscopy |  | Laser diffraction | ≤ 5% |  |  |  | [112] |
| 9 | Cinnamonum campora, fraction 63-125 μm | 17.76 | 66.5 | 157.51 | Yes - fraction 0-500 μm |  |  | 0.19 | Yes - Polarized light microscopy |  | Laser diffraction | ≤ 5% |  |  |  | [112] |
| 10 | Coconut | 22.8 | 83.3 | 274.7 | No |  |  |  | No | 3.02 | Laser diffraction | 8.7 | 78.94 | 0.92 | 11.44 | [142] |
| 11 | Cooperage residues | 137.2 | 396.2 | 804 | No |  |  |  | No | 1.68 | Laser diffraction | 11.6 | 82.75 | 1.23 | 4.42 | [142] |
| 12 | Cork (bark of Quercus suber L.) |  | 47.4 |  | Yes |  |  |  | Yes - SEM |  | Coulter counter | 5.4 | 92.6 |  | 2 | [144] |
| 13 | Corn cob, fraction < 500 μm | 45 | 372.6 | 777.8 | No |  | 98.1 |  | Yes - SEM |  | Laser diffraction | 7.1 | 82.4 d | 8.8 | 17.6 d | [107] |
| 14 | cupressus funebris | 3.64 b | 32.47 | 76.31 b | No |  |  |  | No |  | Laser diffraction |  |  |  |  | [145] |
| 15 | Dalbergia cochinchinensis | 5.78 b | 38.36 | 91.76 b | No |  |  |  | No |  | Laser diffraction |  |  |  |  | [145] |
| 16 | Forest residue |  | 230 |  | Yes |  |  |  | Yes - SEM |  | Laser diffraction | 5.3 | 73.25 | 2.55 |  | [17] |
| 17 | Forest residue - wood + bark |  | 275 |  | No |  |  |  | No |  | Sieves | 6 | 2.9 | 78 |  | [146] |
| 18 | Hardwood pellets - bark dust (Nova Scotia, Canada) |  |  |  | Yes |  |  |  | No |  | Sieves |  |  |  |  | [147] |
| 19 | Lycopodium |  | 35.9 |  | Yes |  |  |  | No |  | Laser diffraction | 5.8 |  |  |  | [143] |
| 20 | Miscanthus |  | 130 |  | Yes |  |  |  | Yes - SEM |  | Laser diffraction | 7 | 73.2 | 1 |  | [17] |
| 21 | Norway spruce (Picea abies) | 28.4 | 148.5 | 602.7 | Yes | 239 | 71 | 0.7 | Yes - SEM |  | Laser diffraction | 5.8 | 79 | 4.1 | 11.1 | [148] |
| 22 | Oakwood |  | 62.9 |  | Yes |  |  |  | No |  | Laser diffraction | 7.7 |  |  |  | [143] |
| 23 | Olive pit |  | 68.2 |  | No | 90.7 | 36.7 | 0.155 | No |  | Laser diffraction |  |  |  |  | [28] |
| 24 | Olive pit |  | 1300 |  | No |  |  |  | No |  | Sieves |  |  |  |  | [28] |
| 25 | Olive pomace pellets, fraction < 45 μm | 9 | 31 | 54 | No |  |  |  | Yes - SEM |  | Laser diffraction | 1.10 | 74.5 | 8.3 | 17.1 | [120] |
| 26 | Olive pomace pellets, fraction 212-75 μm | 38 | 162 | 254 | No |  |  |  | Yes - SEM |  | Laser diffraction | 1.00 | 79.3 | 14 | 6.7 | [120] |
| 27 | Olive pomace pellets, fraction 425-212 μm | 162 | 388 | 615 | No |  |  |  | Yes - SEM |  | Laser diffraction | 0.60 | 66 | 8.5 | 25.5 | [120] |
| 28 | Olive pomace pellets, fraction 75-45 μm | 19 | 62 | 117 | No |  |  |  | Yes - SEM |  | Laser diffraction | 1.00 | 76 | 10.7 | 13.3 | [120] |
| 29 | Orange peel | 62.4 | 226.6 | 549.7 | No |  |  |  | No | 2.15 | Laser diffraction | 7 | 73.1 | 9.8 | 10.1 | [142] |
| 30 | Peanut shell, fraction < 500 μm | 24.3 | 176.1 | 698.5 | No |  | 63.5 |  | Yes - SEM |  | Laser diffraction | 7 | 78.1 d | 8 | 21.9 d | [107] |
| 31 | Pine |  |  |  | No |  |  |  | No |  | Sieves |  |  |  |  | [106] |
| 32 | Pine cone | 27 | 105 | 211 | No |  |  |  | No | 1.75 | Laser diffraction | 6.7 | 75.54 | 7.83 | 9.93 | [142] |
| 33 | Pine nut shells | 9.51 | 46.88 | 439.19 | No | 134.64 | 17.47 |  | Yes - SEM |  | Laser diffraction | 5.4 | 73.2 | 9.8 | 11.7 | [109] |
| 34 | pine sawdust | 3.99 b | 36.57 | 100.62 b | No |  |  |  | No |  | Laser diffraction |  |  |  |  | [145] |
| 35 | Pinus massoniana, fraction 0-63 μm | 12.77 | 34.16 | 77.9 | Yes - fraction 0-500 μm |  |  | 0.28 | Yes - Polarized light microscopy |  | Laser diffraction | ≤ 5% |  |  |  | [112] |
| 36 | Pinus massoniana, fraction 125-250 μm | 29.78 | 120.09 | 279.06 | Yes - fraction 0-500 μm |  |  | 0.1 | Yes - Polarized light microscopy |  | Laser diffraction | ≤ 5% |  |  |  | [112] |
| 37 | Pinus massoniana, fraction 250-500 μm | 66.67 | 219.04 | 459.9 | Yes - fraction 0-500 μm |  |  | 0.05 | Yes - Polarized light microscopy |  | Laser diffraction | ≤ 5% |  |  |  | [112] |
| 38 | Pinus massoniana, fraction 63-125 μm | 18.12 | 57.21 | 154.14 | Yes - fraction 0-500 μm |  |  | 0.18 | Yes - Polarized light microscopy |  | Laser diffraction | ≤ 5% |  |  |  | [112] |
| 39 | Pistachio nut shells | 8.42 | 55.37 | 240.49 | No | 93.98 | 16.95 |  | No |  | Laser diffraction | 2.7 | 78.4 | 8.3 | 10.7 | [109] |
| 40 | Poplar |  |  |  | No |  |  |  | No |  | Sieves |  |  |  |  | [106] |
| 41 | Populus alba, fraction 0-63 μm | 12.91 | 38.06 | 94.91 | Yes - fraction 0-500 μm |  |  | 0.27 | Yes - Polarized light microscopy |  | Laser diffraction | ≤ 5% |  |  |  | [112] |
| 42 | Populus alba, fraction 125-250 μm | 56.84 | 180.78 | 418.62 | Yes - fraction 0-500 μm |  |  | 0.06 | Yes - Polarized light microscopy |  | Laser diffraction | ≤ 5% |  |  |  | [112] |
| 43 | Populus alba, fraction 250-500 μm | 164.62 | 565.78 | 1402.98 | Yes - fraction 0-500 μm |  |  | 0.02 | Yes - Polarized light microscopy |  | Laser diffraction | ≤ 5% |  |  |  | [112] |
| 44 | Populus alba, fraction 63-125 μm | 30.25 | 89.44 | 204.33 | Yes - fraction 0-500 μm |  |  | 0.11 | Yes - Polarized light microscopy |  | Laser diffraction | ≤ 5% |  |  |  | [112] |
| 45 | Radiata Pine | 37.25 | 92.08 | 210.1 | Yes |  |  |  | Yes - video microscope system | 2.69 | Light scattering | 1.18 |  |  |  | [149] |
| 46 | Rape seed straw |  | 220 |  | Yes |  |  |  | Yes - SEM |  | Laser diffraction | 11.5 | 50.95 | 5.4 |  | [17] |
| 47 | Sewage sludge (Catalonia) |  | 92 |  | No | 103.2 | 50.3 | 0.119 | No |  | Laser diffraction |  |  |  |  | [28] |
| 48 | Sewage sludge (Catalonia) |  | 638.2 |  | No | 699.6 | 490.3 | 0.012 | No |  | Laser diffraction |  |  |  |  | [28] |
| 49 | Sewage sludge (Madrid) |  | 94.7 |  | No | 104.2 | 33.5 | 0.179 | No |  | Laser diffraction |  |  |  |  | [28] |
| 50 | Sewage sludge (Madrid) |  | 98.1 |  | No | 107.5 | 47.8 | 0.125 | No |  | Laser diffraction |  |  |  |  | [28] |
| 51 | Sewage sludge (Madrid) |  | 1500 |  | No |  |  |  | No |  | Sieves |  |  |  |  | [28] |
| 52 | Softwood pellets - white dust (British Columbia, Canada) |  |  |  | Yes |  |  |  | No |  | Sieves |  |  |  |  | [147] |
| 53 | Sorghum |  | 120 |  | Yes |  |  |  | Yes - SEM |  | Laser diffraction | 6.55 | 70.4 | 5.25 |  | [17] |
| 54 | Southern pine | 25.4 | 189.8 | 739.4 | Yes | 294 | 72 | 1.7 | No |  | Laser diffraction | 5 | 78.5 | 2.5 | 14 | [108] |
| 55 | Southern pine (Pinus palustris) |  | 53.2 |  | Yes |  |  | 1.71 | Yes - SEM |  | - | 5 | 78.5 | 2.5 | 14 | [128] |
| 56 | Southern yellow pine wood pellets (USA) |  |  |  | Yes |  |  |  | No |  | Sieves |  |  |  |  | [147] |
| 57 | Spanish pine |  | 320 |  | Yes |  |  |  | Yes - SEM |  | Laser diffraction | 7.4 | 78.15 | 0.25 |  | [17] |
| 58 | Spruce |  |  |  | No |  |  |  | No |  | Sieves |  |  |  |  | [106] |
| 59 | Straw | 18.8 | 105.4 | 279.4 | No |  |  |  | No | 2.47 | Laser diffraction | 8.8 | 76.14 | 8.42 | 6.64 | [142] |
| 60 | Torrefied Pine |  |  |  | No |  |  |  | No |  | Sieves |  |  |  |  | [106] |
| 61 | Torrefied Poplar |  |  |  | No |  |  |  | No |  | Sieves |  |  |  |  | [106] |
| 62 | Torrefied Spruce |  |  |  | No |  |  |  | No |  | Sieves |  |  |  |  | [106] |
| 63 | Torrefied wood pellets |  | 104 |  | No | 154.8 | 46 | 0.13 | No |  | Laser diffraction |  |  |  |  | [28] |
| 64 | Torrefied wood pellets |  | 3500 |  | No |  |  |  | No |  | Sieves |  |  |  |  | [28] |
| 65 | Torrified Norway spruce | 15 | 67 | 281 | Yes |  |  |  | Yes - SEM |  | Laser diffraction | 2.8 | 77 | 4.1 | 15.9 | [148] |
| 66 | Torrified Norway spruce (Picea abies) |  | 38.5 |  | Yes |  |  | 2.1 | No |  | - | 2.7 | 69.4 | 5.8 | 22.1 | [128] |
| 67 | Torrified southern pine |  | 36.6 |  | Yes |  |  | 1.47 | Yes - SEM |  | - | 3.3 | 70.3 | 4.3 | 22.1 | [128] |
| 68 | Vine shoot | 9.9 | 37.5 | 199.7 | No |  |  |  | No | 5.06 | Laser diffraction | 6.2 | 54.72 | 36.77 | 2.31 | [142] |
| 69 | Walnut shells | 9.05 | 51.86 | 310.76 | No | 114.79 | 15.91 |  | No |  | Laser diffraction | 4.9 | 74.4 | 6.2 | 14.5 | [109] |
| 70 | Wheat straw |  | 171.2 |  | No | 230.3 | 78.5 | 0.076 | No |  | Laser diffraction |  |  |  |  | [28] |
| 71 | White wood |  |  |  | No |  |  |  | No |  | Sieves |  |  |  |  | [106] |
| 72 | Wood (90% birch, 10% spruce) |  | 80 |  | Yes |  |  |  | Yes - SEM |  | Laser diffraction | 1.65 | 81.87 | 0.39 |  | [17] |
| 73 | Wood (fibrous sample), as received: 41% < 500 μm and 0.3% < 75 μm |  |  |  | No |  |  |  | Yes - digital camara photo |  | - | 60 |  |  |  | [150] |
| 74 | Wood (fibrous sample), fraction < 75 μm |  |  |  | No |  |  |  | Yes - digital camara photo |  | Sieves | 60 |  |  |  | [150] |
| 75 | Wood (fibrous sample), fraction < 75 μm |  |  |  | No |  |  |  | No |  | Sieves | 60 |  |  |  | [150] |
| 76 | wood (mixture of beech and oak), fraction 25-45 μm |  |  |  | No | 23.5 |  |  | No |  | Coulter counter | 40 |  |  |  | [151] |
| 77 | wood (mixture of beech and oak), fraction 45-71 μm |  |  |  | No | 42.7 |  |  | No |  | Coulter counter | 40 |  |  |  | [151] |
| 78 | wood (mixture of beech and oak), fraction 90-125 μm |  |  |  | No | 82.5 |  |  | No |  | Coulter counter | 40 |  |  |  | [151] |
| 79 | Wood chips |  | 146.6 |  | No | 207.1 | 92.9 | 0.065 | No |  | Laser diffraction |  |  |  |  | [28] |
| 80 | Wood chips |  | 1100 |  | No |  |  |  | No |  | Sieves |  |  |  |  | [28] |
| 81 | Wood dust from the production of particleboard (hammer mill dust) | 4.43 | 15.96 | 37.74 | Yes |  |  |  | Yes - video microscope system | 2.64 | Light scattering | 3.88 |  |  |  | [149] |
| 82 | Wood dust from the production of particleboard (silo dust) | 18.96 | 56.02 | 113.07 | Yes |  |  |  | Yes - video microscope system | 2.36 | Light scattering | 1.74 |  |  |  | [149] |
| 83 | Wood pellets |  | 404.1 |  | No | 210.5 | 87.5 | 0.069 | No |  | Laser diffraction |  |  |  |  | [28] |
| 84 | Wood pellets |  | 3000 |  | No |  |  |  | No |  | Sieves |  |  |  |  | [28] |
| 85 | Wood pellets | 28.03 | 184.16 | 576.28 | No |  |  |  | Yes - SEM |  | Laser diffraction | 6 | 85.6 | 2.4 | 14.4 | [6] |
| 86 | Wood pellets | 33.02 | 180.38 | 569.24 | No |  |  |  | Yes - SEM |  | laser diffraction | 6.7 | 84.5 | 4.3 | 15.4 | [6] |
| 87 | Wood pellets | 37.09 | 194.62 | 608.8 | No |  |  |  | Yes - SEM |  | laser diffraction | 4.9 | 89.9 | 13 | 10.1 | [6] |
| 88 | Wood pellets | 34.46 | 223.06 | 636.12 | No |  |  |  | Yes - SEM |  | laser diffraction | 6.7 | 94.1 | 2.4 | 5.9 | [6] |
| 89 | Woodchips | 47.3 | 152.7 | 378.5 | No |  |  |  | No | 2.17 | Laser diffraction | 6.6 | 86.9 | 0.22 | 6.28 | [142] |
| 90 | Coal | 126.65 | 190.46 | 225.92 | No | 195.85 | 92.96 | 0.04 | Yes - SEM |  | Laser diffraction |  |  |  |  | [45] |
| 91 | Coal | 98.78 | 145.78 | 209.51 | No | 149.06 | 72.87 | 0.05 | Yes - SEM |  | Laser diffraction |  |  |  |  | [45] |
| 92 | Coal | 47.81 | 95.56 | 160.92 | No | 99.44 | 56.65 | 0.11 | Yes - SEM |  | Laser diffraction |  |  |  |  | [45] |
| 93 | Coal | 10.33 | 33.89 | 47.08 | No | 35.88 | 11.98 | 0.54 | Yes - SEM |  | Laser diffraction |  |  |  |  | [45] |
| 94 | Coal | 5.12 | 11.53 | 20.48 | No | 11.92 | 4.06 | 1.48 | Yes - SEM |  | Laser diffraction |  |  |  |  | [45] |
| 95 | Coal | 1.8 | 5.42 | 10.21 | No | 5.41 | 2.17 | 2.76 | Yes - SEM |  | Laser diffraction |  |  |  |  | [45] |
| 96 | Coal (Colombia) | 6.8 | 28.1 | 85.2 | Yes | 40 | 15 | 15.8 | Yes - SEM |  | Laser diffraction | 3.2 | 33.7 | 15.3 | 47.8 | [108] |
| 97 | Coal (Huaibei, China) | 7.92 | 45.2 | 91.66 | Yes |  |  |  | No | 1.85 | Laser diffraction | 2.16 | 35.77 | 20.55 | 51.03 | [46] |
| 98 | Coal (Kellingley, UK) | 5 | 25.5 | 65.3 | Yes | 31 | 12 | 3.7 | Yes - SEM |  | Laser diffraction | 1.7 | 29.2 | 19.1 | 50 | [108] |
| 99 | Coal (Lvliang, China) | 16.67 | 52.36 | 205.4 | Yes |  |  |  | No | 3.6 | Laser diffraction | 1.03 | 23.38 | 6.92 | 71.32 | [46] |
| 100 | Coal (Lvliang, China) | 17.11 | 51.13 | 111.2 | Yes |  |  |  | No | 1.84 | Laser diffraction | 1.03 | 23.38 | 6.92 | 71.32 | [46] |
| 101 | Coal (Neimeng, China) | 9.54 | 45.37 | 101.4 | Yes |  |  |  | No | 2.02 | Laser diffraction | 1.48 | 14.03 | 14.25 | 73.72 | [46] |
| 102 | Coal (Ningxia, China) | 7.14 | 43.69 | 91.62 | Yes |  |  |  | No | 1.93 | Laser diffraction | 1.58 | 33.51 | 28.54 | 47.51 | [46] |
| 103 | Coal (Spain) |  | 26.8 |  | No | 32.1 | 9.7 | 0.62 | No |  | Laser diffraction |  |  |  |  | [28] |
| 104 | Coal (Tiefa, China) | 12.37 | 55.94 | 103.4 | Yes |  |  |  | No | 1.63 | Laser diffraction | 9.76 | 40.97 | 28.12 | 42.44 | [46] |
| 105 | Coal (Tiefa, China) | 9.63 | 37.33 | 71.95 | Yes |  |  |  | No | 1.67 | Laser diffraction | 9.76 | 40.97 | 28.12 | 42.44 | [46] |
| 106 | Coal (UK) |  | 45.9 |  | No | 55.3 | 19.5 | 0.307 | No |  | Laser diffraction |  |  |  |  | [28] |
| 107 | Coke (Spain) |  | 77.4 |  | No | 90.6 | 23.2 | 0.258 | No |  | Laser diffraction |  |  |  |  | [28] |
| 108 | Coke (Spain) |  | 1200 |  | No |  |  |  | No |  | Sieves |  |  |  |  | [28] |
| 109 | Lignite |  | 73 |  | No |  |  | 2.35/0.11 c | No | 1.3 | BET & Dynamic image analysis | 8-10% |  |  |  | [152] |
| 110 | Lignite |  | 15 |  | No |  |  | 3.41/0.38 c | No | 1.6 | BET & Dynamic image analysis | 8-10% |  |  |  | [152] |
| 111 | Lignite |  | 21 |  | No |  |  | 3.04/0.30 c | No | 1.8 | BET & Dynamic image analysis | 8-10% |  |  |  | [152] |
| 112 | Lignite (Germany) |  | 30 |  | Yes |  |  |  | Yes - SEM |  | Laser diffraction | 9.85 | 46.1 | 3.85 |  | [17] |
| 113 | Lignite (Spain) |  | 50 |  | Yes |  |  |  | Yes - SEM |  | Laser diffraction | 16.65 | 36.6 | 17.1 |  | [17] |

a The following units and abbreviations had been used: d10 (μm), d50 (μm), d90 (μm), d4,3 (μm), d3,2 (μm), PD – polydispersity (-), M – moisture content (%), V – volatile content (%), A – ash content (%), FC – fixed carbon (%)

b The paper reports d5 (written as d10) and d95 (written as d90)

c SSA determined using the BET method (highest value, includes roughness and porous surfaces) and the image analysis method (lowest value, projection of particle outer surface)

d Values reported as dry ash free (daf)

[142]	J. García Torrent, Á. Ramírez-Gómez, N. Fernandez-Anez, L. Medic Pejic, A. Tascón, Influence of the composition of solid biomass in the flammability and susceptibility to spontaneous combustion, Fuel. 184 (2016) 503–511. https://doi.org/10.1016/j.fuel.2016.07.045.

[143]	S. Hosseinzadeh, J. Berghmans, J. Degreve, F. Verplaetsen, A model for the minimum ignition energy of dust clouds, Process Saf. Environ. Prot. 121 (2019) 43–49. https://doi.org/10.1016/j.psep.2018.10.004.

[144]	R. Pilão, E. Ramalho, C. Pinho, Overall characterization of cork dust explosion, J. Hazard. Mater. 133 (2006) 183–195.

[145]	A. Liu, J. Chen, X. Huang, J. Lin, X. Zhang, W. Xu, Explosion parameters and combustion kinetics of biomass dust, Bioresour. Technol. 294 (2019) 122168. https://doi.org/10.1016/j.biortech.2019.122168.

[146]	J. García-Torrent, E. Conde-Lázaro, C. Wilén, A. Rautalin, Biomass dust explosibility at elevated initial pressures, Fuel. 77 (1998) 1093–1097. https://doi.org/10.1016/S0016-2361(97)00285-8.

[147]	S. Melin, Testing of Explosibility and Flammability of Airborne Dust from Wood Pellets, Wood Pellet Assoc. Canada. (2008) 1–19.

[148]	C. Huéscar Medina, H. Sattar, H.N. Phylaktou, G.E. Andrews, B.M. Gibbs, Explosion reactivity characterisation of pulverised torrefied spruce wood, J. Loss Prev. Process Ind. 36 (2015) 287–295. https://doi.org/10.1016/j.jlp.2014.12.009.

[149]	M.C. Lee, Y.S. Kim, D.H. Rie, Analysis of explosion characteristics of combustible wood dust in confined system using the thermal decomposition rate and mass loss rate, Appl. Therm. Eng. 109 (2016) 432–439. https://doi.org/10.1016/j.applthermaleng.2016.08.010.

[150]	P.R. Amyotte, C.T. Cloney, F.I. Khan, R.C. Ripley, Dust explosion risk moderation for flocculent dusts, J. Loss Prev. Process Ind. 25 (2012) 862–869. https://doi.org/10.1016/j.jlp.2012.05.007.

[151]	S. Callé, L. Klaba, D. Thomas, L. Perrin, O. Dufaud, Influence of the size distribution and concentration on wood dust explosion: Experiments and reaction modelling, Powder Technol. 157 (2005) 144–148. https://doi.org/10.1016/j.powtec.2005.05.021.

[152]	K.-W. Stahmer, M. Gerhold, Study of the explosion reactions of sucrose, activated charcoal, polyethylene and lignite Part 1: Effect of variation in particle surface area upon explosion reaction, J. Loss Prev. Process Ind. 46 (2017) 177–184. https://doi.org/10.1016/j.jlp.2017.02.010.