Table S2: Flammability and explosion severity parameters a

| Nº | Sample | Pmax | KSt | dP/dtmax | MIE | MITl | MITc | MEC | LOC | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | Almond shell |  |  |  |  | 290 |  |  |  | [28] |
| 2 | Almond shell | 7.1 | 157.0 | 580.0 | 610 | 290 | 440 | 60 |  | [142] |
| 3 | Bark (of pine) | 8.7 b | 98.0 | 361.0 | 50 | 310 | 460 | 30 | 10.0 | [17] |
| 4 | Barley straw | 8.3 b | 58.0 | 213.7 | 620 | 310 | 440 | 90 | 13.0 | [17] |
| 5 | Cacao |  |  |  | 350 |  | 760-840 c |  |  | [143] |
| 6 | Cinnamonum campora, fraction 0-63 μm | 8.3 | 182.0 | 670.5 |  |  |  |  |  | [112] |
| 7 | Cinnamonum campora, fraction 125-250 μm | 7.9 | 92.0 | 338.9 |  |  |  |  |  | [112] |
| 8 | Cinnamonum campora, fraction 250-500 μm | 7.8 | 66.0 | 243.1 |  |  |  |  |  | [112] |
| 9 | Cinnamonum campora, fraction 63-125 μm | 8 | 150.0 | 552.6 |  |  |  |  |  | [112] |
| 10 | Coconut | 7.3 | 150.0 | 552.0 | 220 | 280 | 400 | 60 |  | [142] |
| 11 | Cooperage residues | 7.3 | 131.0 | 484.0 | 1000 | 350 | 420 | 150 |  | [142] |
| 12 | Cork (bark of Quercus suber L.) | 6.2 | 179.0 | 659.4 |  |  |  | 40 |  | [144] |
| 13 | Corn cob, fraction < 500 μm | 8 d | 60.0 | 221.0 |  |  |  | 0.62 |  | [107] |
| 14 | cupressus funebris | 7.3 | 206.3 | 760.0 |  | 390-400 | 290-300 | 80 |  | [145] |
| 15 | Dalbergia cochinchinensis | 7.4 | 217.5 | 801.4 |  | 370-380 | 280-290 | 70 |  | [145] |
| 16 | Forest residue | 8.1 b | 84.0 | 309.5 | 50 | 300 | 440 | 60 | 10.0 | [17] |
| 17 | Forest residue - wood + bark | 9.1 | 92.3 | 340.0 | 40 | 320 | 400 | 20 |  | [146] |
| 18 | Hardwood pellets - bark dust (Nova Scotia, Canada) | 8.4 | 162.0 | 595.0 | 17 | 310 | 450 | 70 | 10.5 | [147] |
| 19 | Lycopodium |  |  |  | 4 |  | 680 c |  |  | [143] |
| 20 | Miscanthus | 7.1 b | 31.0 | 114.2 | 260 | 290 | 460 | 120 | 20.0 | [17] |
| 21 | Norway spruce (Picea abies) | 8.2 d | 95.0 | 350.0 |  |  |  |  |  | [148] |
| 22 | Oakwood |  |  |  | 42 |  | 482 c |  |  | [143] |
| 23 | Olive pit |  |  |  |  | 300 |  |  |  | [28] |
| 24 | Olive pit |  |  |  |  | >400 |  |  |  | [28] |
| 25 | Olive pomace pellets, fraction < 45 μm | 7.6 | 69.0 | 255.0 | >1000 | 550 |  | 90 |  | [120] |
| 26 | Olive pomace pellets, fraction 212-75 μm | 8.4 | 45.0 | 166.0 | >1000 | 480 |  | 110 |  | [120] |
| 27 | Olive pomace pellets, fraction 425-212 μm | 7.3 | 23.0 | 84.0 | >1000 | 500 |  | 140 |  | [120] |
| 28 | Olive pomace pellets, fraction 75-45 μm | 7.8 | 70.0 | 258.0 | >1000 | 540 |  | 100 |  | [120] |
| 29 | Orange peel | 7.3 | 127.0 | 469.0 | 1000 | 300 | 440 | 125 |  | [142] |
| 30 | Peanut shell, fraction < 500 μm | 7.1 | 25.0 | 92.1 |  |  |  | 0.85 e |  | [107] |
| 31 | Pine |  |  |  | 37 |  |  | 0.4 f |  | [106] |
| 32 | Pine cone | 7.1 | 143.0 | 527.0 | 260 | 320 | 380 | 60 |  | [142] |
| 33 | Pine nut shells | 8.9 d | 61.0 | 224.7 |  |  |  |  |  | [109] |
| 34 | pine sawdust | 7 | 194.4 | 716.3 |  | 420-430 | 300-310 | 110 |  | [145] |
| 35 | Pinus massoniana, fraction 0-63 μm | 7.5 | 129.0 | 475.2 |  |  |  |  |  | [112] |
| 36 | Pinus massoniana, fraction 125-250 μm | 7.2 | 89.0 | 327.9 |  |  |  |  |  | [112] |
| 37 | Pinus massoniana, fraction 250-500 μm | 6.8 | 58.0 | 213.7 |  |  |  |  |  | [112] |
| 38 | Pinus massoniana, fraction 63-125 μm | 7.6 | 118.0 | 434.7 |  |  |  |  |  | [112] |
| 39 | Pistachio nut shells | 9.3 d | 82.0 | 302.1 |  |  |  |  |  | [109] |
| 40 | Poplar |  |  |  | 26 |  |  | 0.46 f |  | [106] |
| 41 | Populus alba, fraction 0-63 μm | 8.9 | 247.0 | 910.0 |  |  |  |  |  | [112] |
| 42 | Populus alba, fraction 125-250 μm | 8.8 | 184.0 | 677.9 |  |  |  |  |  | [112] |
| 43 | Populus alba, fraction 250-500 μm | 7.8 | 86.0 | 316.8 |  |  |  |  |  | [112] |
| 44 | Populus alba, fraction 63-125 μm | 8.9 | 158.0 | 582.1 |  |  |  |  |  | [112] |
| 45 | Radiata Pine | 8.4 f | 103.1 | 380.0 |  |  |  |  |  | [149] |
| 46 | Rape seed straw | 7.3 b | 32.0 | 117.9 | >1000 | 330 | 420 | 210 | 20.0 | [17] |
| 47 | Sewage sludge (Catalonia) |  |  |  |  | 310 |  |  |  | [28] |
| 48 | Sewage sludge (Catalonia) |  |  |  |  | >400 |  |  |  | [28] |
| 49 | Sewage sludge (Madrid) |  |  |  |  | 280 |  |  |  | [28] |
| 50 | Sewage sludge (Madrid) |  |  |  |  | 260 |  |  |  | [28] |
| 51 | Sewage sludge (Madrid) |  |  |  |  | >400 |  |  |  | [28] |
| 52 | Softwood pellets - white dust (British Columbia, Canada) | 8.1 | 146.0 | 537.0 | 17 | 300 | 450 | 70 | 10.5 | [147] |
| 53 | Sorghum | 7.2 b | 28.0 | 103.2 | 1400 | 300 | 440 | 120 | 20.0 | [17] |
| 54 | Southern pine | 8 d | 105.0 | 386.8 |  |  |  |  |  | [108] |
| 55 | Southern pine (Pinus palustris) | 9 d | 105.0 | 386.8 |  |  |  |  |  | [128] |
| 56 | Southern yellow pine wood pellets (USA) | 7.7 | 98.0 | 360.0 | 20 | 320 | 455 | 25 | 13.5 | [147] |
| 57 | Spanish pine | 7.2 b | 23.0 | 84.7 | 450 | 350 | 460 | 90 | 17.0 | [17] |
| 58 | Spruce |  |  |  | 6 |  |  | 0.52 |  | [106] |
| 59 | Straw | 7.2 | 157.0 | 579.0 | 440 | 320 | 420 | 60 |  | [142] |
| 60 | Torrefied Pine |  |  |  | 42 |  |  | 0.37 f |  | [106] |
| 61 | Torrefied Poplar |  |  |  | 22 |  |  | 0.61 f |  | [106] |
| 62 | Torrefied Spruce |  |  |  | 5 |  |  | 0.57 f |  | [106] |
| 63 | Torrefied wood pellets |  |  |  |  | 320 |  |  |  | [28] |
| 64 | Torrefied wood pellets |  |  |  |  | 320 |  |  |  | [28] |
| 65 | Torrified Norway spruce | 9.1 d | 122.0 | 449.5 |  |  |  | 63 |  | [148] |
| 66 | Torrified Norway spruce (Picea abies) | 9.1 d | 110.0 | 405.2 |  |  |  | 54 |  | [128] |
| 67 | Torrified southern pine | 8.8 d | 115.0 | 423.7 |  |  |  | 55 |  | [128] |
| 68 | Vine shoot | 7.2 | 136.0 | 501.0 | 260 | 300 | 420 | 300 |  | [142] |
| 69 | Walnut shells | 9.4 d | 98.0 | 361.0 |  |  |  |  |  | [109] |
| 70 | Wheat straw |  |  |  |  | 320 |  |  |  | [28] |
| 71 | White wood |  |  |  | 21 |  |  |  |  | [106] |
| 72 | Wood (90% birch, 10% spruce) | 7.8 b | 87.0 | 320.5 | 60 | 340 | 420 | 30 | 10.0 | [17] |
| 73 | Wood (fibrous sample), as received: 41% < 500 μm and 0.3% < 75 μm | 7.2 | 41.0 | 151.0 | 300 - 1000 g |  | >580 | 100 |  | [150] |
| 74 | Wood (fibrous sample), fraction < 75 μm | 7.8 | 80.0 | 294.7 | 300 - 1000 g |  | 420 | 30 |  | [150] |
| 75 | Wood (fibrous sample), fraction < 75 μm | 8.2 | 149.0 | 548.9 | 10 - 30 g |  | 410 | 20 |  | [150] |
| 76 | wood (mixture of beech and oak), fraction 25-45 μm | 7.7 | 135.7 | 500.0 |  |  |  |  |  | [151] |
| 77 | wood (mixture of beech and oak), fraction 45-71 μm | 7.5 |  |  |  |  |  |  |  | [151] |
| 78 | wood (mixture of beech and oak), fraction 90-125 μm | 7.1 |  |  |  |  |  |  |  | [151] |
| 79 | Wood chips |  |  |  |  | 360 |  |  |  | [28] |
| 80 | Wood chips |  |  |  |  | 390 |  |  |  | [28] |
| 81 | Wood dust from the production of particleboard (hammer mill dust) | 8.3 f | 111.8 | 412.0 |  |  |  |  |  | [149] |
| 82 | Wood dust from the production of particleboard (silo dust) | 8.1 f | 92.3 | 340.0 |  |  |  |  |  | [149] |
| 83 | Wood pellets |  |  |  |  | 300 |  |  |  | [28] |
| 84 | Wood pellets |  |  |  |  | >400 |  |  |  | [28] |
| 85 | Wood pellets |  |  | 16.0 h |  |  |  | 0.36 h |  | [6] |
| 86 | Wood pellets |  |  | 17.0 h |  |  |  | 0.46 h |  | [6] |
| 87 | Wood pellets |  |  | 14.0 h |  |  |  | 0.67 h |  | [6] |
| 88 | Wood pellets |  |  | 23.0 h |  |  |  | 0.38 h |  | [6] |
| 89 | Woodchips | 7.4 | 150.0 | 553.0 | 160 | 350 | 460 | 60 |  | [142] |
| 90 | Coal | 4.2 | 25.4 | 93.6 |  |  |  |  |  | [45] |
| 91 | Coal | 4.7 | 31.8 | 117.2 |  |  |  |  |  | [45] |
| 92 | Coal | 4.9 | 34.6 | 127.5 |  |  |  |  |  | [45] |
| 93 | Coal | 5.4 | 47.6 | 175.4 |  |  |  |  |  | [45] |
| 94 | Coal | 6 | 74.9 | 275.9 |  |  |  |  |  | [45] |
| 95 | Coal | 6.3 | 88.5 | 326.0 |  |  |  |  |  | [45] |
| 96 | Coal (Colombia) | 8.5 d | 129.0 | 475.2 |  |  |  | 75 |  | [108] |
| 97 | Coal (Huaibei, China) | 8.2 d | 153.1 | 564.0 |  |  |  |  |  | [46] |
| 98 | Coal (Kellingley, UK) | 8.2 | 80.0 | 294.7 |  |  |  | 120 |  | [108] |
| 99 | Coal (Lvliang, China) | 7.6 | 97.7 | 360.0 |  |  |  |  |  | [46] |
| 100 | Coal (Lvliang, China) | 7.9 | 128.9 | 475.0 |  |  |  |  |  | [46] |
| 101 | Coal (Neimeng, China) | 6.1 | 73.6 | 271.0 |  |  |  |  |  | [46] |
| 102 | Coal (Ningxia, China) | 6.8 | 120.2 | 443.0 |  |  |  |  |  | [46] |
| 103 | Coal (Spain) |  |  |  |  | 270 |  |  |  | [28] |
| 104 | Coal (Tiefa, China) | 7 | 184.6 | 680.0 |  |  |  |  |  | [46] |
| 105 | Coal (Tiefa, China) | 7.7 | 176.4 | 650.0 |  |  |  |  |  | [46] |
| 106 | Coal (UK) |  |  |  |  | >400 |  |  |  | [28] |
| 107 | Coke (Spain) |  |  |  |  | 360 |  |  |  | [28] |
| 108 | Coke (Spain) |  |  |  |  | >400 |  |  |  | [28] |
| 109 | Lignite | 7.8 b | 146.0 | 537.9 |  |  |  |  |  | [152] |
| 110 | Lignite | 7.9 b | 165.0 | 607.9 |  |  |  |  |  | [152] |
| 111 | Lignite | 8.2 | 142.0 | 523.1 |  |  |  |  |  | [152] |
| 112 | Lignite (Germany) | 7.7 | 105.0 | 386.8 | 30 | 230 | 420 | 60 | 9.0 | [17] |
| 113 | Lignite (Spain) | 7.8 | 107.0 | 394.2 | 420 | 240 | 400 | 90 | 8.0 | [17] |

a The following units are used: Pmax (bar(g)), KSt (bar·m/s), dP/dtmax (bar/s), MIE (mJ), MITl (ºC), MITc (ºC), MEC (g/m3), LOC (%)

b The paper reports bar(a), this table repots bar(g)

c The paper reports MITc values obtained from previously published literature

d The paper reports Pmax as a ratio

e The paper reports MEC expressed as burnt equivalence ratio

f The paper reports MEC values represented as an equivalence ratio, i.e. the ratio between the real fuel concentration in air and the stoichiometric fuel to air concentration

g The paper reports MIE (inductancce) as a range

h The paper reports dP/dtmax as rate of pressure rise vs. equivalence ratio and MEC values as a ratio