Reaction to fire of birch plywood bonded with three different adhesive systems at multiple scales

Supplementary Information

S 1 Results of the Shapiro–Wilk normality tests and Levene homogeneity tests for the density of the Mini-SBI boards. Shapiro–Wilk tests were performed for the residuals of the respective datasets. Assumption assessment refers to the applicability of ANOVA-based analysis.

| Cone Calorimeter | Shapiro-Wilk p | Levene p | Assumption assessment |
| --- | --- | --- | --- |
| Density (kg/m³) | 0.615 | 0.008 | heterogeneity of variance |

S 2 Results of the Shapiro–Wilk normality tests and Levene homogeneity tests for the cone calorimeter variables. Shapiro–Wilk tests were performed for the residuals of the respective datasets. Assumption assessment refers to the applicability of ANOVA-based analysis.

| Cone Calorimeter | Shapiro-Wilk p | Levene p | Assumption assessment |
| --- | --- | --- | --- |
| Time to ignition (s) | 0.141 | 0.289 | assumptions fulfilled |
| Time to flame off (s) | 0.188 | 0.091 | assumptions fulfilled |
| Total heat release (MJ/m²) | 0.888 | 0.308 | assumptions fulfilled |
| Total heat release rate 600s (MJ/m²) | 0.695 | 0.479 | assumptions fulfilled |
| Peak heat release 1 (kW/m²) | 0.585 | <0.001 | heterogeneity of variance |
| Peak heat release 2 (kW/m²) | 0.505 | 0.156 | assumptions fulfilled |
| Maximum average rate of heat emission (kW/m²) | 0.065 | 0.119 | assumptions fulfilled |
| Total smoke production (m²/m²) | 0.997 | 0.084 | assumptions fulfilled |
| Total smoke prod. nonfl. phase (m²/m²) | 0.043 | 0.06 | deviation from normality |
| Total smoke prod. flaming phase (m²/m²) | 0.972 | 0.225 | assumptions fulfilled |
| Mass at sustained flaming (g) | 0.447 | 0.072 | assumptions fulfilled |
| Mass loss (%) | 0.129 | 0.439 | assumptions fulfilled |
| MLR ignition and end of the test (g/s) | 0.549 | 0.39 | assumptions fulfilled |
| MLR 10 % and 90 % of mass loss (g/s) | 0.06 | 0.022 | heterogeneity of variance |

S 3 Results of the Shapiro–Wilk normality tests and Levene homogeneity tests for the simulation of SBI based on cone calorimeter variables. Shapiro–Wilk tests were performed for the residuals of the respective datasets. Assumption assessment refers to the applicability of ANOVA-based analysis.

| Simulation of SBI based on Cone Calorimeter | Shapiro-Wilk p | Levene p | Assumption assessment |
| --- | --- | --- | --- |
| THR600s | 0.866 | 0.788 | assumptions fulfilled |
| FIGRA0.4MJ | 0.151 | 0.917 | assumptions fulfilled |
| THR600s + 10% time to ignition | 0.671 | 0.677 | assumptions fulfilled |
| FIGRA0.4MJ + 10% time to ignition | 0.204 | 0.873 | assumptions fulfilled |
| THR600s - 10% time to ignition | 0.934 | 0.858 | assumptions fulfilled |
| FIGRA0.4MJ - 10% time to ignition | 0.167 | 0.786 | assumptions fulfilled |

S 4 Results of the Shapiro–Wilk normality tests and Levene homogeneity tests for the Mini-SBI variables used in the two-way ANOVA. Shapiro–Wilk tests were performed for the residuals of the respective models. Assumption assessment refers to the applicability of ANOVA-based analysis.

| Mini-SBI | Shapiro-Wilk p | Levene p | Assumption assessment |
| --- | --- | --- | --- |
| THR | <0.001 | 0.003 | deviation from normality and heterogeneity of variance |
| THR600s | 0.771 | 0.156 | assumptions fulfilled |
| FIGRA600s | 0.379 | 0.487 | assumptions fulfilled |
| FIGRA0.02 | 0.451 | 0.005 | heterogeneity of variance |