Appendix

Table A1: Density r of liquid Al versus temperature T. The relative standard uncertainty is 2%.

| T [K] | r [g/cm3] | T [K] | r [g/cm3] | T [K] | r [g/cm3] | T [K] | r [g/cm3] |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 909.8 | 2.379 | 1120.6 | 2.317 | 1332.6 | 2.251 | 1612.1 | 2.167 |
| 931.3 | 2.303 | 1122.6 | 2.237 | 1339.4 | 2.222 | 1637.4 | 2.143 |
| 939.7 | 2.353 | 1130.2 | 2.290 | 1341.8 | 2.212 | 1638.3 | 2.142 |
| 944.0 | 2.360 | 1130.9 | 2.245 | 1343.8 | 2.184 | 1644.5 | 2.151 |
| 945.2 | 2.292 | 1130.9 | 2.237 | 1344.4 | 2.203 | 1660.1 | 2.129 |
| 949.4 | 2.289 | 1131.3 | 2.314 | 1352.6 | 2.199 | 1674.4 | 2.124 |
| 956.7 | 2.289 | 1142.5 | 2.312 | 1363.4 | 2.196 | 1688.7 | 2.139 |
| 957.7 | 2.278 | 1155.0 | 2.309 | 1364.3 | 2.197 | 1692.2 | 2.133 |
| 962.1 | 2.349 | 1157.2 | 2.234 | 1365.8 | 2.217 |  |  |
| 962.4 | 2.286 | 1157.3 | 2.230 | 1368.0 | 2.173 |  |  |
| 974.7 | 2.283 | 1163.7 | 2.234 | 1379.2 | 2.232 |  |  |
| 980.4 | 2.345 | 1167.9 | 2.279 | 1383.2 | 2.201 |  |  |
| 985.5 | 2.344 | 1172.1 | 2.237 | 1392.9 | 2.214 |  |  |
| 986.7 | 2.275 | 1177.3 | 2.305 | 1402.1 | 2.198 |  |  |
| 987.9 | 2.277 | 1183.0 | 2.237 | 1403.6 | 2.197 |  |  |
| 1002.7 | 2.275 | 1186.9 | 2.233 | 1420.8 | 2.201 |  |  |
| 1003.9 | 2.276 | 1188.5 | 2.236 | 1432.6 | 2.209 |  |  |
| 1007.6 | 2.268 | 1192.3 | 2.302 | 1441.9 | 2.185 |  |  |
| 1010.9 | 2.338 | 1193.6 | 2.302 | 1448.0 | 2.190 |  |  |
| 1017.3 | 2.331 | 1195.7 | 2.270 | 1459.8 | 2.185 |  |  |
| 1021.6 | 2.274 | 1201.0 | 2.302 | 1467.5 | 2.201 |  |  |
| 1025.8 | 2.275 | 1206.2 | 2.228 | 1480.6 | 2.184 |  |  |
| 1046.1 | 2.332 | 1208.3 | 2.217 | 1483.0 | 2.180 |  |  |
| 1053.2 | 2.266 | 1211.7 | 2.217 | 1507.5 | 2.196 |  |  |
| 1054.5 | 2.320 | 1216.5 | 2.299 | 1516.3 | 2.172 |  |  |
| 1057.2 | 2.268 | 1225.3 | 2.298 | 1518.7 | 2.173 |  |  |
| 1059.8 | 2.252 | 1226.4 | 2.263 | 1533.2 | 2.168 |  |  |
| 1063.6 | 2.329 | 1230.5 | 2.22044 | 1543.1 | 2.166 |  |  |
| 1065.7 | 2.250 | 1237.1 | 2.2731 | 1543.1 | 2.166 |  |  |
| 1067.9 | 2.261 | 1246.6 | 2.2087 | 1556.2 | 2.177 |  |  |
| 1076.7 | 2.325 | 1252.5 | 2.22422 | 1561.2 | 2.167 |  |  |
| 1083.7 | 2.324 | 1254.5 | 2.25237 | 1568.2 | 2.158 |  |  |
| 1084.6 | 2.264 | 1269.9 | 2.26308 | 1574.9 | 2.159 |  |  |
| 1091.3 | 2.319 | 1279.7 | 2.21771 | 1578.2 | 2.149 |  |  |
| 1106.6 | 2.253 | 1282.9 | 2.2444 | 1595.9 | 2.161 |  |  |
| 1112.0 | 2.244 | 1295.6 | 2.25362 | 1609.8 | 2.154 |  |  |
|  |  | 1298.6 | 2.2103 |  |  |  |  |
|  |  | 1312.6 | 2.23337 |  |  |  |  |
|  |  | 1320.7 | 2.21212 |  |  |  |  |

Table A2: Density r of liquid Ti versus temperature T. The relative standard uncertainty is 2%.

| T [K] | r [g/cm3] | T [K] | r [g/cm3] |
| --- | --- | --- | --- |
| 1858.0 | 4.164 | 2035.2 | 4.109 |
| 1858.4 | 4.233 | 2036.7 | 4.106 |
| 1871.1 | 4.277 | 2036.8 | 4.190 |
| 1872.9 | 4.138 | 2037.5 | 4.125 |
| 1878.2 | 4.078 | 2042.4 | 4.191 |
| 1881.5 | 4.270 | 2046.5 | 4.128 |
| 1884.4 | 4.149 | 2047.6 | 4.157 |
| 1895.7 | 4.257 | 2048.1 | 4.027 |
| 1898.5 | 4.144 | 2050.4 | 4.188 |
| 1905.6 | 4.231 | 2052.4 | 4.104 |
| 1911.6 | 4.128 | 2055.7 | 4.014 |
| 1913.6 | 4.070 | 2056.5 | 4.126 |
| 1913.7 | 4.136 | 2057.8 | 4.123 |
| 1916.7 | 4.251 | 2060.4 | 4.025 |
| 1922.1 | 4.123 | 2061.1 | 4.109 |
| 1924.8 | 4.221 | 2061.4 | 4.113 |
| 1932.5 | 4.128 | 2061.5 | 4.183 |
| 1935.3 | 4.113 | 2062.8 | 4.099 |
| 1939.1 | 4.206 | 2063.4 | 4.126 |
| 1945.1 | 4.140 | 2063.6 | 4.024 |
| 1947.3 | 4.148 | 2065.1 | 4.020 |
| 1948.5 | 4.223 | 2068.2 | 4.194 |
| 1949.4 | 4.112 | 2069.0 | 4.101 |
| 1950.7 | 4.062 | 2070.5 | 4.116 |
| 1951.8 | 4.135 | 2072.4 | 4.021 |
| 1960.6 | 4.136 | 2074.2 | 4.117 |
| 1961.9 | 4.123 | 2077.3 | 4.178 |
| 1963.0 | 4.192 | 2077.5 | 4.177 |
| 1963.7 | 4.130 | 2078.1 | 4.207 |
| 1965.9 | 4.200 | 2078.1 | 4.037 |
| 1967.8 | 4.142 | 2079.2 | 3.996 |
| 1968.0 | 4.131 | 2079.8 | 4.118 |
| 1974.4 | 4.118 | 2080.0 | 4.123 |
| 1974.4 | 4.136 | 2083.0 | 4.163 |
| 1981.2 | 4.226 | 2083.7 | 4.026 |
| 1982.0 | 4.123 | 2085.7 | 4.013 |
| 1986.1 | 4.119 | 2087.5 | 4.018 |
| 1989.9 | 4.146 | 2087.9 | 4.192 |
| 1996.2 | 4.200 | 2091.0 | 4.018 |
| 2000.9 | 4.049 | 2107.0 | 4.129 |
| 2005.3 | 4.176 | 2114.9 | 4.113 |
| 2009.7 | 4.111 | 2121.9 | 4.080 |
| 2013.1 | 4.121 | 2138.3 | 4.082 |
| 2017.2 | 4.226 | 2153.3 | 4.115 |
| 2029.5 | 4.033 | 2036.8 | 4.190 |

Table A3: Density r of liquid Al90Ti10 versus temperature T. The relative standard uncertainty is 2%.

| T [K] | r [g/cm3] |
| --- | --- |
| 1330.6 | 2.538 |
| 1368.1 | 2.517 |
| 1400.0 | 2.515 |
| 1412.1 | 2.508 |
| 1441.5 | 2.506 |
| 1477.1 | 2.489 |
| 1483.3 | 2.489 |
| 1501.5 | 2.480 |
| 1520.9 | 2.484 |
| 1534.5 | 2.480 |
| 1554.1 | 2.478 |
| 1564.1 | 2.469 |
| 1605.6 | 2.456 |
| 1628.6 | 2.448 |
| 1645.0 | 2.447 |
| 1668.1 | 2.428 |
| 1700.4 | 2.418 |
| 1719.2 | 2.405 |
| 1768.2 | 2.384 |
| 1803.4 | 2.363 |

Table A4: Density r of liquid Al80Ti20 versus temperature T. The relative standard uncertainty is 2%.

| T [K] | r [g/cm3] |
| --- | --- |
| 1417.6 | 2.950 |
| 1493.2 | 2.927 |
| 1521.7 | 2.763 |
| 1551.4 | 2.757 |
| 1552.1 | 2.894 |
| 1569.8 | 2.884 |
| 1572.3 | 2.743 |
| 1579.5 | 2.866 |
| 1586.0 | 2.738 |
| 1593.2 | 2.738 |
| 1596.3 | 2.826 |
| 1598.3 | 2.865 |
| 1601.0 | 2.721 |
| 1616.1 | 2.715 |
| 1619.8 | 2.703 |
| 1620.5 | 2.818 |
| 1626.1 | 2.715 |
| 1632.4 | 2.825 |
| 1632.8 | 2.839 |
| 1634.4 | 2.718 |
| 1640.4 | 2.689 |
| 1641.3 | 2.687 |
| 1642.6 | 2.827 |
| 1645.2 | 2.702 |
| 1651.4 | 2.695 |
| 1656.7 | 2.827 |
| 1659.1 | 2.821 |
| 1667.3 | 2.677 |
| 1671.3 | 2.683 |
| 1671.4 | 2.821 |
| 1677.3 | 2.675 |
| 1680.9 | 2.815 |
| 1696.2 | 2.670 |
| 1696.6 | 2.673 |
| 1700.5 | 2.762 |
| 1709.5 | 2.671 |
| 1717.4 | 2.657 |
| 1722.9 | 2.648 |
| 1743.4 | 2.635 |
| 1754.7 | 2.628 |
| 1765.2 | 2.746 |
| 1771.3 | 2.750 |
| 1782.0 | 2.619 |

Table A4: Density r of liquid Al70Ti30 versus temperature T. The relative standard uncertainty is 2%.

| T [K] | r [g/cm3] |
| --- | --- |
| 1700.8 | 2.886 |
| 1626.4 | 2.889 |
| 1653.4 | 2.892 |
| 1666.7 | 2.895 |
| 1582.8 | 2.896 |
| 1686.0 | 2.899 |
| 1710.4 | 2.900 |
| 1639.7 | 2.901 |
| 1599.6 | 2.906 |
| 1696.4 | 2.908 |
| 1592.2 | 2.908 |
| 1620.1 | 2.913 |
| 1611.3 | 2.914 |
| 1562.9 | 2.917 |
| 1677.8 | 2.919 |
| 1571.4 | 2.919 |
| 1552.6 | 2.919 |
| 1577.2 | 2.922 |
| 1659.1 | 2.924 |
| 1546.7 | 2.925 |
| 1558.5 | 2.927 |
| 1541.3 | 2.928 |
| 1619.8 | 2.931 |
| 1595.4 | 2.939 |
| 1537.8 | 2.942 |
| 1517.5 | 2.943 |
| 1522.5 | 2.943 |
| 1584.1 | 2.945 |
| 1610.6 | 2.947 |
| 1501.0 | 2.949 |
| 1498.0 | 2.950 |
| 1574.2 | 2.959 |
| 1476.2 | 2.972 |
| 1528.1 | 2.973 |
| 1492.3 | 2.975 |
| 1517.5 | 2.975 |
| 1486.9 | 2.977 |
| 1466.2 | 2.987 |
| 1483.0 | 2.987 |
| 1467.6 | 2.994 |
| 1452.8 | 2.996 |

Table A5: Density r of liquid Al60Ti40 versus temperature T. The relative standard uncertainty is 2%.

| T [K] | r [g/cm3] |
| --- | --- |
| 1501.6 | 3.243 |
| 1524.9 | 3.237 |
| 1536.3 | 3.229 |
| 1547.8 | 3.222 |
| 1570.1 | 3.211 |
| 1582.0 | 3.207 |
| 1583.8 | 3.206 |
| 1598.3 | 3.197 |
| 1609.9 | 3.181 |
| 1622.9 | 3.178 |
| 1632.0 | 3.177 |
| 1638.3 | 3.174 |
| 1643.9 | 3.165 |
| 1650.6 | 3.161 |
| 1660.1 | 3.160 |
| 1670.9 | 3.155 |
| 1687.2 | 3.140 |
| 1709.2 | 3.130 |
| 1728.9 | 3.117 |

Table A6: Density r of liquid Al50Ti50 versus temperature T. The relative standard uncertainty is 2%.

| T [K] | r [g/cm3] |
| --- | --- |
| 1583.0 | 3.436 |
| 1586.6 | 3.441 |
| 1614.1 | 3.436 |
| 1621.5 | 3.423 |
| 1637.5 | 3.428 |
| 1639.7 | 3.416 |
| 1651.3 | 3.426 |
| 1656.7 | 3.424 |
| 1663.8 | 3.405 |
| 1673.3 | 3.418 |
| 1679.7 | 3.396 |
| 1680.3 | 3.415 |
| 1687.6 | 3.413 |
| 1694.9 | 3.409 |
| 1696.7 | 3.385 |
| 1703.1 | 3.405 |
| 1711.9 | 3.373 |
| 1718.0 | 3.376 |
| 1723.5 | 3.394 |
| 1733.0 | 3.390 |
| 1737.7 | 3.373 |
| 1743.6 | 3.382 |
| 1752.4 | 3.364 |
| 1755.1 | 3.380 |
| 1763.7 | 3.349 |
| 1766.4 | 3.370 |
| 1779.3 | 3.365 |
| 1780.7 | 3.346 |
| 1787.9 | 3.335 |
| 1789.9 | 3.330 |
| 1792.7 | 3.356 |
| 1807.3 | 3.349 |
| 1815.7 | 3.325 |
| 1822.7 | 3.345 |
| 1856.4 | 3.327 |
| 1859.8 | 3.310 |
| 1871.1 | 3.319 |
| 1907.0 | 3.309 |
| 1936.8 | 3.301 |

Table A7: Density r of liquid Al40Ti60 versus temperature T. The relative standard uncertainty is 2%.

| T [K] | r [g/cm3] |
| --- | --- |
| 1698.6 | 3.385 |
| 1708.3 | 3.380 |
| 1719.3 | 3.375 |
| 1720.3 | 3.381 |
| 1731.4 | 3.400 |
| 1734.0 | 3.384 |
| 1747.4 | 3.374 |
| 1749.0 | 3.386 |
| 1758.9 | 3.380 |
| 1763.0 | 3.357 |
| 1765.0 | 3.376 |
| 1770.6 | 3.374 |
| 1773.3 | 3.380 |
| 1775.6 | 3.379 |
| 1778.3 | 3.367 |
| 1784.3 | 3.367 |
| 1788.7 | 3.358 |
| 1789.5 | 3.346 |
| 1792.3 | 3.365 |
| 1795.8 | 3.362 |
| 1804.0 | 3.393 |
| 1805.2 | 3.370 |
| 1810.0 | 3.396 |
| 1812.5 | 3.364 |
| 1818.0 | 3.373 |
| 1833.4 | 3.395 |
| 1853.4 | 3.344 |
| 1877.1 | 3.361 |
| 1919.5 | 3.360 |

Table A8: Density r of liquid Al30Ti70 versus temperature T. The relative standard uncertainty is 2%.

| T [K] | r [g/cm3] |
| --- | --- |
| 1906.7 | 3.516 |
| 1888.3 | 3.534 |
| 1881.5 | 3.543 |
| 1854.9 | 3.557 |
| 1850.4 | 3.558 |
| 1846.4 | 3.570 |
| 1842.7 | 3.574 |
| 1835.7 | 3.576 |
| 1828.9 | 3.583 |
| 1824.1 | 3.580 |
| 1820.9 | 3.588 |
| 1815.0 | 3.602 |
| 1811.6 | 3.605 |
| 1805.2 | 3.602 |
| 1795.0 | 3.602 |
| 1788.5 | 3.619 |
| 1779.6 | 3.613 |
| 1774.3 | 3.613 |
| 1768.7 | 3.621 |
| 1762.0 | 3.633 |
| 1754.9 | 3.633 |
| 1925.3 | 3.533 |
| 1901.3 | 3.536 |
| 1879.8 | 3.521 |
| 1871.3 | 3.553 |
| 1857.6 | 3.541 |
| 1846.2 | 3.525 |
| 1844.3 | 3.554 |
| 1833.2 | 3.552 |
| 1827.0 | 3.559 |
| 1821.8 | 3.569 |
| 1815.5 | 3.569 |
| 1805.8 | 3.553 |
| 1803.0 | 3.558 |
| 1796.7 | 3.570 |
| 1791.5 | 3.572 |

Table A9: Density r of liquid Al25Ti75 versus temperature T. The relative standard uncertainty is 2%.

| T [K] | r [g/cm3] |
| --- | --- |
| 1757.0 | 3.707 |
| 1776.5 | 3.699 |
| 1781.2 | 3.706 |
| 1790.8 | 3.695 |
| 1790.9 | 3.690 |
| 1795.6 | 3.687 |
| 1802.4 | 3.698 |
| 1811.6 | 3.681 |
| 1815.4 | 3.692 |
| 1817.2 | 3.689 |
| 1826.1 | 3.692 |
| 1832.2 | 3.680 |
| 1834.3 | 3.674 |
| 1835.6 | 3.683 |
| 1838.4 | 3.671 |
| 1847.0 | 3.682 |
| 1850.7 | 3.668 |
| 1853.1 | 3.647 |
| 1869.5 | 3.636 |
| 1885.8 | 3.642 |
| 1891.1 | 3.633 |
| 1898.4 | 3.635 |
| 1910.0 | 3.624 |
| 1918.7 | 3.614 |
| 1923.9 | 3.614 |
| 1939.9 | 3.617 |
| 1948.8 | 3.614 |

Table A10: Density r of liquid Al20Ti80 versus temperature T. The relative standard uncertainty is 2%.

| T [K] | r [g/cm3] |
| --- | --- |
| 1808.1 | 3.681 |
| 1828.4 | 3.709 |
| 1829.9 | 3.696 |
| 1836.1 | 3.703 |
| 1842.8 | 3.663 |
| 1850.3 | 3.672 |
| 1866.6 | 3.667 |
| 1874.9 | 3.683 |
| 1878.5 | 3.679 |
| 1882.3 | 3.673 |
| 1893.3 | 3.699 |
| 1904.7 | 3.648 |
| 1912.8 | 3.654 |
| 1913.5 | 3.678 |
| 1915.3 | 3.630 |
| 1921.6 | 3.664 |
| 1928.3 | 3.666 |
| 1935.8 | 3.660 |
| 1943.2 | 3.632 |
| 1946.6 | 3.624 |
| 1947.3 | 3.666 |
| 1957.6 | 3.643 |
| 1958.3 | 3.658 |
| 1963.5 | 3.623 |
| 1968.5 | 3.615 |
| 1970.4 | 3.659 |
| 1994.1 | 3.665 |
| 2002.2 | 3.624 |
| 2025.1 | 3.609 |
| 1808.1 | 3.681 |
| 1828.4 | 3.709 |
| 1829.9 | 3.696 |
| 1836.1 | 3.703 |
| 1842.8 | 3.663 |
| 1850.4 | 3.672 |
| 1866.6 | 3.668 |
| 1874.9 | 3.683 |
| 1878.5 | 3.679 |
| 1882.3 | 3.673 |
| 1893.3 | 3.699 |
| 1904.7 | 3.648 |
| 1912.8 | 3.654 |
| 1913.5 | 3.678 |
| 1915.3 | 3.630 |
| 1921.6 | 3.664 |
| 1928.3 | 3.666 |
| 1935.8 | 3.660 |
| 1943.2 | 3.632 |
| 1946.6 | 3.624 |
| 1947.3 | 3.666 |
| 1957.6 | 3.643 |
| 1958.3 | 3.658 |
| 1963.5 | 3.623 |
| 1968.5 | 3.615 |
| 1970.4 | 3.659 |
| 1994.1 | 3.665 |
| 2002.2 | 3.624 |
| 2025.1 | 3.609 |

Table A11: Density r of liquid Al10Ti90 versus temperature T. The relative standard uncertainty is 2%.

| T [K] | r [g/cm3] |
| --- | --- |
| 1813.5 | 3.850 |
| 1826.2 | 3.981 |
| 1826.6 | 3.856 |
| 1835.3 | 3.972 |
| 1835.4 | 3.832 |
| 1849.2 | 3.977 |
| 1858.4 | 3.964 |
| 1869.0 | 3.940 |
| 1875.4 | 3.843 |
| 1883.3 | 3.948 |
| 1883.6 | 3.843 |
| 1903.4 | 3.853 |
| 1906.1 | 3.820 |
| 1912.0 | 3.949 |
| 1930.5 | 3.833 |
| 1943.8 | 3.828 |
| 1946.7 | 3.925 |
| 1950.6 | 3.820 |
| 1965.9 | 3.847 |
| 1974.2 | 3.911 |
| 1992.4 | 3.817 |
| 2000.7 | 3.883 |
| 2003.1 | 3.800 |
| 2007.2 | 3.751 |
| 2012.0 | 3.801 |
| 2021.6 | 3.794 |
| 2024.4 | 3.807 |
| 2033.6 | 3.834 |
| 2046.3 | 3.805 |
| 2049.1 | 3.758 |
| 2054.6 | 3.796 |
| 2099.4 | 3.787 |
| 2107.0 | 3.789 |
| 2113.3 | 3.747 |

Surface tension

Table A12: Surface tension g of liquid Al versus temperature T. The relative standard uncertainty is 5%.

| T [K] | g [N/m] | T [K] | g [N/m] | T [K] | g [N/m] |
| --- | --- | --- | --- | --- | --- |
| 1063.3 | 0.841 | 1359.1 | 0.826 | 1454.7 | 0.832 |
| 1076.3 | 0.847 | 1366.6 | 0.863 | 1464.3 | 0.834 |
| 1128.3 | 0.867 | 1369.8 | 0.812 | 1472.3 | 0.834 |
| 1146.5 | 0.832 | 1369.8 | 0.812 | 1472.8 | 0.795 |
| 1162.7 | 0.852 | 1379.3 | 0.798 | 1475.5 | 0.782 |
| 1162.7 | 0.878 | 1383.7 | 0.809 | 1477.7 | 0.788 |
| 1188.9 | 0.827 | 1384.6 | 0.863 | 1483.1 | 0.776 |
| 1194.9 | 0.839 | 1384.8 | 0.812 | 1485.9 | 0.838 |
| 1194.9 | 0.847 | 1384.9 | 0.851 | 1494.4 | 0.832 |
| 1204.1 | 0.822 | 1390.8 | 0.845 | 1495.5 | 0.785 |
| 1213.5 | 0.868 | 1395.9 | 0.805 | 1502.1 | 0.786 |
| 1213.5 | 0.837 | 1397.7 | 0.809 | 1506.8 | 0.831 |
| 1222.6 | 0.831 | 1399.4 | 0.857 | 1511.5 | 0.787 |
| 1225.2 | 0.875 | 1399.8 | 0.811 | 1513.6 | 0.814 |
| 1238.4 | 0.836 | 1406.9 | 0.783 | 1514.2 | 0.802 |
| 1238.4 | 0.827 | 1408.4 | 0.810 | 1522.8 | 0.797 |
| 1240.1 | 0.818 | 1408.6 | 0.853 | 1524.4 | 0.822 |
| 1240.6 | 0.847 | 1409.5 | 0.810 | 1525.1 | 0.790 |
| 1257.2 | 0.825 | 1410.7 | 0.784 | 1535.5 | 0.774 |
| 1257.2 | 0.847 | 1410.8 | 0.822 | 1536.0 | 0.836 |
| 1262.0 | 0.827 | 1416.2 | 0.846 | 1537.2 | 0.822 |
| 1276.6 | 0.857 | 1417.0 | 0.808 | 1548.0 | 0.801 |
| 1277.2 | 0.825 | 1417.0 | 0.808 | 1550.4 | 0.750 |
| 1300.2 | 0.819 | 1423.4 | 0.852 | 1558.1 | 0.805 |
| 1307.6 | 0.850 | 1423.5 | 0.781 | 1559.2 | 0.760 |
| 1310.8 | 0.871 | 1430.8 | 0.824 | 1586.6 | 0.759 |
| 1318.5 | 0.819 | 1431.8 | 0.844 |  |  |
| 1333.1 | 0.820 | 1433.1 | 0.807 |  |  |
| 1333.3 | 0.871 | 1433.4 | 0.802 |  |  |
| 1335.7 | 0.870 | 1434.1 | 0.802 |  |  |
| 1340.9 | 0.869 | 1439.7 | 0.804 |  |  |
| 1348.8 | 0.834 | 1441.4 | 0.855 |  |  |
| 1350.1 | 0.859 | 1444.1 | 0.828 |  |  |
| 1352.7 | 0.814 | 1447.0 | 0.804 |  |  |
| 1353.8 | 0.816 | 1447.8 | 0.796 |  |  |
| 1356.9 | 0.867 | 1450.3 | 0.803 |  |  |
| 1358.4 | 0.796 | 1454.4 | 0.791 |  |  |

Table A13: Surface tension g of liquid Ti versus temperature T. The relative standard uncertainty is 5%.

| T [K] | g [N/m] | T [K] | g [N/m] | T [K] | g [N/m] |
| --- | --- | --- | --- | --- | --- |
| 1823.0 | 1.536 | 1970.5 | 1.48359 | 2077.7 | 1.498 |
| 1825.2 | 1.520 | 1971.7 | 1.47957 | 2080.2 | 1.496 |
| 1838.8 | 1.525 | 1973.0 | 1.53799 | 2080.5 | 1.453 |
| 1841.0 | 1.510 | 1976 | 1.49529 | 2083.0 | 1.458 |
| 1841.2 | 1.522 | 1979.2 | 1.4896 | 2105.0 | 1.495 |
| 1843.4 | 1.507 | 1982.7 | 1.52125 | 2107.9 | 1.457 |
| 1854.0 | 1.607 | 1984.8 | 1.49269 | 2113.7 | 1.493 |
| 1859.4 | 1.527 | 1985.2 | 1.48335 | 2116.6 | 1.455 |
| 1861.6 | 1.513 | 1987.6 | 1.51201 | 2117.4 | 1.495 |
| 1861.8 | 1.514 | 1988.2 | 1.592 | 2120.4 | 1.446 |
| 1864.1 | 1.499 | 1990.2 | 1.483 | 2127.1 | 1.523 |
| 1886.2 | 1.585 | 1991.9 | 1.488 | 2127.4 | 1.493 |
| 1892.2 | 1.519 | 1999.5 | 1.441 | 2128.3 | 1.456 |
| 1894.5 | 1.504 | 2006.0 | 1.510 | 2130.3 | 1.455 |
| 1895.8 | 1.526 | 2006.6 | 1.487 | 2159.8 | 1.481 |
| 1898.2 | 1.483 | 2008.3 | 1.559 | 2161.1 | 1.480 |
| 1914.1 | 1.526 | 2008.5 | 1.508 | 2162.9 | 1.453 |
| 1916.5 | 1.512 | 2008.7 | 1.472 | 2164.1 | 1.467 |
| 1917.8 | 1.510 | 2011.1 | 1.471 | 2215.0 | 1.479 |
| 1920.2 | 1.495 | 2017.0 | 1.475 | 2217.5 | 1.482 |
| 1922.7 | 1.579 | 2018.9 | 1.594 | 2218.2 | 1.452 |
| 1930.6 | 1.546 | 2023.8 | 1.484 | 2220.7 | 1.442 |
| 1942.0 | 1.496 | 2024.2 | 1.476 | 2261.6 | 1.474 |
| 1943 | 1.4 | 2040.6 | 1.495 | 2265.0 | 1.436 |
| 1943.4 | 1.511 | 2043.0 | 1.506 | 2265.4 | 1.474 |
| 1944.8 | 1.521 | 2043.3 | 1.465 | 2304.6 | 1.468 |
| 1945.4 | 1.513 | 2045.8 | 1.476 | 2305.9 | 1.470 |
| 1945.9 | 1.497 | 2046.2 | 1.477 |  |  |
| 1947.1 | 1.483 | 2050.7 | 1.483 |  |  |
| 1950.0 | 1.607 | 2052.5 | 1.522 |  |  |
| 1954.2 | 1.570 | 2057.6 | 1.529 |  |  |
| 1961.4 | 1.489 | 2058.8 | 1.586 |  |  |
| 1966.8 | 1.443 | 2061.6 | 1.507 |  |  |
| 1967.9 | 1.522 | 2064.1 | 1.489 |  |  |
| 1969.2 | 1.522 | 2064.4 | 1.470 |  |  |
|  |  | 2066.8 | 1.448 |  |  |

Table A14: Surface tension g of liquid Al90Ti10 versus temperature T. The relative standard uncertainty is 5%.

| T [K] | g [N/m] |
| --- | --- |
| 1575.6 | 0.898 |
| 1595.4 | 0.865 |
| 1611.6 | 0.886 |
| 1624.2 | 0.884 |
| 1629.6 | 0.855 |
| 1642.2 | 0.842 |
| 1651.2 | 0.857 |
| 1665.6 | 0.874 |
| 1674.6 | 0.863 |
| 1692.5 | 0.837 |
| 1701.4 | 0.855 |

Table A15: Surface tension g of liquid Al80Ti20 versus temperature T. The relative standard uncertainty is 5%.

| T [K] | g [N/m] |
| --- | --- |
| 1426.4 | 0.960 |
| 1449.3 | 0.956 |
| 1472.0 | 0.956 |
| 1474.4 | 0.954 |
| 1499.4 | 0.944 |
| 1509.5 | 0.938 |
| 1511.1 | 0.951 |
| 1521.2 | 0.938 |
| 1529.7 | 0.943 |
| 1536.0 | 0.942 |
| 1538.3 | 0.935 |
| 1545.2 | 0.943 |
| 1549.9 | 0.940 |
| 1554.5 | 0.940 |
| 1559.9 | 0.946 |
| 1569.9 | 0.935 |

Table A16: Surface tension g of liquid Al70Ti30 versus temperature T. The relative standard uncertainty is 5%.

| T [K] | g [N/m] |
| --- | --- |
| 1784.0 | 0.919 |
| 1774.0 | 0.926 |
| 1758.8 | 0.921 |
| 1753.3 | 0.928 |
| 1747.7 | 0.929 |

Table A17: Surface tension g of liquid Al60Ti40 versus temperature T. The relative standard uncertainty is 5%.

| T [K] | g [N/m] |
| --- | --- |
| 1790.0 | 0.953 |
| 1803.1 | 0.966 |
| 1822.8 | 0.952 |
| 1855.7 | 0.962 |
| 1868.9 | 0.948 |

Table A18: Surface tension g of liquid Al50Ti50 versus temperature T. The relative standard uncertainty is 5%.

| T [K] | g [N/m] |
| --- | --- |
| 1555.4 | 1.137 |
| 1575.5 | 1.135 |
| 1593.9 | 1.126 |
| 1603.2 | 1.103 |
| 1616.2 | 1.136 |
| 1642.3 | 1.083 |
| 1657.4 | 1.074 |
| 1674.4 | 1.053 |
| 1699.1 | 1.055 |
| 1718.3 | 1.072 |
| 1739.5 | 1.086 |
| 1760.9 | 1.079 |
| 1784.4 | 1.055 |
| 1814.0 | 1.076 |

Table A19: Surface tension g of liquid Al50Ti50 versus temperature T. The data was obtained under microgravity. The relative standard uncertainty is 5%.

| T [K] | g [N/m] |
| --- | --- |
| 1643 | 1.261 |
| 1702 | 1.242 |
| 1706 | 1.339 |
| 1749.5 | 1.198 |
| 1754 | 1.325 |
| 1782.5 | 1.261 |
| 1793.5 | 1.204 |
| 1838.5 | 1.136 |
| 1845.5 | 1.204 |
| 1871 | 1.204 |
| 1894.5 | 1.188 |
| 1915.5 | 1.056 |

Table A20: Surface tension g of liquid Al40Ti60 versus temperature T. The relative standard uncertainty is 5%.

| T [K] | g [N/m] |
| --- | --- |
| 1819.1 | 1.251 |
| 1830.8 | 1.244 |
| 1865.8 | 1.247 |
| 1877.5 | 1.235 |

Table A21: Surface tension g of liquid Al30Ti70 versus temperature T. The relative standard uncertainty is 5%.

| T [K] | g [N/m] |
| --- | --- |
| 1828.3 | 1.366 |
| 1840.7 | 1.382 |
| 1853.0 | 1.355 |
| 1861.9 | 1.348 |
| 1865.4 | 1.357 |
| 1867.7 | 1.362 |
| 1877.8 | 1.335 |
| 1884.0 | 1.364 |
| 1890.9 | 1.326 |
| 1914.9 | 1.316 |
| 1921.1 | 1.346 |
| 1937.4 | 1.324 |
| 1939.6 | 1.311 |
| 1970.6 | 1.317 |
| 2020.2 | 1.318 |

Table A22: Surface tension g of liquid Al25Ti75 versus temperature T. The relative standard uncertainty is 5%.

| T [K] | g [N/m] |
| --- | --- |
| 1786.8 | 1.356 |
| 1805.2 | 1.29 |
| 1829.8 | 1.367 |
| 1860.5 | 1.286 |
| 1891.2 | 1.331 |
| 1908.8 | 1.369 |
| 1921.1 | 1.379 |
| 1922.0 | 1.314 |
| 1927.2 | 1.369 |
| 1934.3 | 1.288 |
| 1963.9 | 1.337 |
| 1971.3 | 1.296 |
| 1983.6 | 1.254 |
| 1988.3 | 1.323 |
| 2000.6 | 1.344 |
| 2012.8 | 1.355 |
| 2020.6 | 1.287 |
| 2045.3 | 1.287 |

Table A23: Surface tension g of liquid Al20Ti80 versus temperature T. The relative standard uncertainty is 5%.

| T [K] | g [N/m] |
| --- | --- |
| 1789.2 | 1.288 |
| 1825.6 | 1.279 |
| 1833.6 | 1.382 |
| 1849.9 | 1.357 |
| 1881.3 | 1.330 |
| 1893.3 | 1.309 |
| 1898.6 | 1.365 |
| 1910.8 | 1.268 |
| 1922.9 | 1.308 |
| 1935.1 | 1.284 |
| 1941.1 | 1.347 |
| 1953.0 | 1.355 |
| 1959.5 | 1.259 |
| 1983.8 | 1.288 |
| 1988.9 | 1.362 |
| 2008.2 | 1.241 |
| 2036.7 | 1.340 |
| 2072.6 | 1.297 |

Table A24: Surface tension g of liquid Al10Ti90 versus temperature T. The relative standard uncertainty is 5%.

| T [K] | g [N/m] |
| --- | --- |
| 1886.1 | 1.581 |
| 1906.8 | 1.541 |
| 1934.9 | 1.543 |
| 1949.6 | 1.499 |
| 1967.9 | 1.531 |
| 1972.8 | 1.506 |
| 1993.6 | 1.498 |
| 2005.7 | 1.466 |
| 2005.8 | 1.527 |
| 2015.6 | 1.501 |
| 2021.7 | 1.543 |
| 2038.5 | 1.378 |
| 2052.3 | 1.410 |
| 2057.5 | 1.409 |
| 2063.8 | 1.414 |
| 2067.0 | 1.451 |
| 2073.1 | 1.446 |
| 2080.2 | 1.429 |
| 2082.8 | 1.344 |
| 2091.5 | 1.457 |
| 2116.0 | 1.479 |
| 2124.6 | 1.501 |
| 2133.4 | 1.345 |
| 2152.4 | 1.405 |
| 2175.2 | 1.348 |
| 2190.5 | 1.305 |

Normal spectral emissivity

Table A25: Normal spectral emissivity e(l,T) of liquid Ti at l=940 nm versus temperature T. The relative standard uncertainty is 4%.

| T [K] | e(l=940 nm,T) |
| --- | --- |
| 1970 | 0.381 |
| 1963 | 0.370 |
| 1953 | 0.359 |
| 1943 | 0.368 |
| 1933 | 0.373 |

Table A26: Normal spectral emissivity e(l,T) of liquid Al20Ti80 at l=940 nm versus temperature T. The relative standard uncertainty is 4%.

| T [K] | e(l=940 nm,T) |
| --- | --- |
| 1999 | 0.386 |
| 1986.8 | 0.393 |
| 1966.4 | 0.403 |
| 1958.2 | 0.407 |
| 1949.0 | 0.403 |

Table A27: Normal spectral emissivity e(l,T) of liquid Al50Ti50 at l=940 nm versus temperature T. The relative standard uncertainty is 4%.

| T [K] | e(l=940 nm,T) |
| --- | --- |
| 1840.2 | 0.317 |
| 1827.2 | 0.317 |
| 1818.1 | 0.319 |
| 1808.1 | 0.316 |
| 1799.1 | 0.318 |
| 1788.1 | 0.319 |
| 1776.0 | 0.320 |
| 1766.0 | 0.322 |
| 1757 | 0.316 |
| 1744.0 | 0.316 |
| 1736.0 | 0.319 |

Table A28: Normal spectral emissivity e(l,T) of liquid Al70Ti30 at l=940 nm versus temperature T. The relative standard uncertainty is 4%.

| T [K] | e(l=940 nm,T) |
| --- | --- |
| 1825.2 | 0.287 |
| 1815.9 | 0.299 |
| 1798.5 | 0.302 |
| 1786.2 | 0.305 |
| 1769.9 | 0.310 |
| 1775.0 | 0.292 |
| 1766.8 | 0.300 |
| 1749.4 | 0.302 |
| 1735.0 | 0.302 |
| 1719.7 | 0.312 |
| 1706.4 | 0.310 |
| 1693.1 | 0.317 |

Molar heat capacity over normal spectral emissivity at 940 nm

Table A29: Molar heat capacity cp over normal spectral emissivity e(l=940 nm, T) of liquid Ti versus temperature T. The relative standard uncertainty is 2%.

| T [K] | cp/e(l=940 nm,T) [J/K/mol] |
| --- | --- |
| 1930 | 135.188 |
| 1975 | 135.558 |
| 1995 | 135.135 |
| 2015 | 131.428 |
| 2030 | 130.940 |

Table A30: Molar heat capacity cp over normal spectral emissivity e(l=940 nm, T) of liquid Al20Ti80 versus temperature T. The relative standard uncertainty is 3%.

| T [K] | cp/e(l=940 nm,T) [J/K/mol] |
| --- | --- |
| 2030 | 149.263 |
| 1990 | 148.174 |
| 1930 | 142.172 |
| 1960 | 143.044 |

Table A31: Molar heat capacity cp over normal spectral emissivity e(l=940 nm, T) of liquid Al50Ti50 versus temperature T. The relative standard uncertainty is 3%.

| T [K] | cp/e(l=940 nm,T) [J/K/mol] |
| --- | --- |
| 1886 | 167.043 |
| 1820 | 152.747 |
| 1808 | 143.508 |
| 1780 | 137.693 |
| 1765 | 138.647 |