Appendix
Table A1: Density r of liquid Al versus temperature T. The relative standard uncertainty is 2%.  
	T [K]
	r [g/cm3]
	T [K]
	r [g/cm3]
	T [K]
	r [g/cm3]
	T [K]
	r [g/cm3]

	909.8
	2.379
	1120.6
	2.317
	1332.6
	2.251
	1612.1
	2.167

	931.3
	2.303
	1122.6
	2.237
	1339.4
	2.222
	1637.4
	2.143

	939.7
	2.353
	1130.2
	2.290
	1341.8
	2.212
	1638.3
	2.142

	944.0
	2.360
	1130.9
	2.245
	1343.8
	2.184
	1644.5
	2.151

	945.2
	2.292
	1130.9
	2.237
	1344.4
	2.203
	1660.1
	2.129

	949.4
	2.289
	1131.3
	2.314
	1352.6
	2.199
	1674.4
	2.124

	956.7
	2.289
	1142.5
	2.312
	1363.4
	2.196
	1688.7
	2.139

	957.7
	2.278
	1155.0
	2.309
	1364.3
	2.197
	1692.2
	2.133

	962.1
	2.349
	1157.2
	2.234
	1365.8
	2.217
	
	

	962.4
	2.286
	1157.3
	2.230
	1368.0
	2.173
	
	

	974.7
	2.283
	1163.7
	2.234
	1379.2
	2.232
	
	

	980.4
	2.345
	1167.9
	2.279
	1383.2
	2.201
	
	

	985.5
	2.344
	1172.1
	2.237
	1392.9
	2.214
	
	

	986.7
	2.275
	1177.3
	2.305
	1402.1
	2.198
	
	

	987.9
	2.277
	1183.0
	2.237
	1403.6
	2.197
	
	

	1002.7
	2.275
	1186.9
	2.233
	1420.8
	2.201
	
	

	1003.9
	2.276
	1188.5
	2.236
	1432.6
	2.209
	
	

	1007.6
	2.268
	1192.3
	2.302
	1441.9
	2.185
	
	

	1010.9
	2.338
	1193.6
	2.302
	1448.0
	2.190
	
	

	1017.3
	2.331
	1195.7
	2.270
	1459.8
	2.185
	
	

	1021.6
	2.274
	1201.0
	2.302
	1467.5
	2.201
	
	

	1025.8
	2.275
	1206.2
	2.228
	1480.6
	2.184
	
	

	1046.1
	2.332
	1208.3
	2.217
	1483.0
	2.180
	
	

	1053.2
	2.266
	1211.7
	2.217
	1507.5
	2.196
	
	

	1054.5
	2.320
	1216.5
	2.299
	1516.3
	2.172
	
	

	1057.2
	2.268
	1225.3
	2.298
	1518.7
	2.173
	
	

	1059.8
	2.252
	1226.4
	2.263
	1533.2
	2.168
	
	

	1063.6
	2.329
	1230.5
	2.22044
	1543.1
	2.166
	
	

	1065.7
	2.250
	1237.1
	2.2731
	1543.1
	2.166
	
	

	1067.9
	2.261
	1246.6
	2.2087
	1556.2
	2.177
	
	

	1076.7
	2.325
	1252.5
	2.22422
	1561.2
	2.167
	
	

	1083.7
	2.324
	1254.5
	2.25237
	1568.2
	2.158
	
	

	1084.6
	2.264
	1269.9
	2.26308
	1574.9
	2.159
	
	

	1091.3
	2.319
	1279.7
	2.21771
	1578.2
	2.149
	
	

	1106.6
	2.253
	1282.9
	2.2444
	1595.9
	2.161
	
	

	1112.0
	2.244
	1295.6
	2.25362
	1609.8
	2.154
	
	

	
	
	1298.6
	2.2103
	
	
	
	

	
	
	1312.6
	2.23337
	
	
	
	

	
	
	1320.7
	2.21212
	
	
	
	






Table A2: Density r of liquid Ti versus temperature T. The relative standard uncertainty is 2%.  
	T [K]
	r [g/cm3]
	T [K]
	r [g/cm3]

	1858.0
	4.164
	2035.2
	4.109

	1858.4
	4.233
	2036.7
	4.106

	1871.1
	4.277
	2036.8
	4.190

	1872.9
	4.138
	2037.5
	4.125

	1878.2
	4.078
	2042.4
	4.191

	1881.5
	4.270
	2046.5
	4.128

	1884.4
	4.149
	2047.6
	4.157

	1895.7
	4.257
	2048.1
	4.027

	1898.5
	4.144
	2050.4
	4.188

	1905.6
	4.231
	2052.4
	4.104

	1911.6
	4.128
	2055.7
	4.014

	1913.6
	4.070
	2056.5
	4.126

	1913.7
	4.136
	2057.8
	4.123

	1916.7
	4.251
	2060.4
	4.025

	1922.1
	4.123
	2061.1
	4.109

	1924.8
	4.221
	2061.4
	4.113

	1932.5
	4.128
	2061.5
	4.183

	1935.3
	4.113
	2062.8
	4.099

	1939.1
	4.206
	2063.4
	4.126

	1945.1
	4.140
	2063.6
	4.024

	1947.3
	4.148
	2065.1
	4.020

	1948.5
	4.223
	2068.2
	4.194

	1949.4
	4.112
	2069.0
	4.101

	1950.7
	4.062
	2070.5
	4.116

	1951.8
	4.135
	2072.4
	4.021

	1960.6
	4.136
	2074.2
	4.117

	1961.9
	4.123
	2077.3
	4.178

	1963.0
	4.192
	2077.5
	4.177

	1963.7
	4.130
	2078.1
	4.207

	1965.9
	4.200
	2078.1
	4.037

	1967.8
	4.142
	2079.2
	3.996

	1968.0
	4.131
	2079.8
	4.118

	1974.4
	4.118
	2080.0
	4.123

	1974.4
	4.136
	2083.0
	4.163

	1981.2
	4.226
	2083.7
	4.026

	1982.0
	4.123
	2085.7
	4.013

	1986.1
	4.119
	2087.5
	4.018

	1989.9
	4.146
	2087.9
	4.192

	1996.2
	4.200
	2091.0
	4.018

	2000.9
	4.049
	2107.0
	4.129

	2005.3
	4.176
	2114.9
	4.113

	2009.7
	4.111
	2121.9
	4.080

	2013.1
	4.121
	2138.3
	4.082

	2017.2
	4.226
	2153.3
	4.115

	2029.5
	4.033
	2036.8
	4.190



Table A3: Density r of liquid Al90Ti10 versus temperature T. The relative standard uncertainty is 2%.  
	T [K]
	r [g/cm3]

	1330.6
	2.538

	1368.1
	2.517

	1400.0
	2.515

	1412.1
	2.508

	1441.5
	2.506

	1477.1
	2.489

	1483.3
	2.489

	1501.5
	2.480

	1520.9
	2.484

	1534.5
	2.480

	1554.1
	2.478

	1564.1
	2.469

	1605.6
	2.456

	1628.6
	2.448

	1645.0
	2.447

	1668.1
	2.428

	1700.4
	2.418

	1719.2
	2.405

	1768.2
	2.384

	1803.4
	2.363


















Table A4: Density r of liquid Al80Ti20 versus temperature T. The relative standard uncertainty is 2%.  
	T [K]
	r [g/cm3]

	1417.6
	2.950

	1493.2
	2.927

	1521.7
	2.763

	1551.4
	2.757

	1552.1
	2.894

	1569.8
	2.884

	1572.3
	2.743

	1579.5
	2.866

	1586.0
	2.738

	1593.2
	2.738

	1596.3
	2.826

	1598.3
	2.865

	1601.0
	2.721

	1616.1
	2.715

	1619.8
	2.703

	1620.5
	2.818

	1626.1
	2.715

	1632.4
	2.825

	1632.8
	2.839

	1634.4
	2.718

	1640.4
	2.689

	1641.3
	2.687

	1642.6
	2.827

	1645.2
	2.702

	1651.4
	2.695

	1656.7
	2.827

	1659.1
	2.821

	1667.3
	2.677

	1671.3
	2.683

	1671.4
	2.821

	1677.3
	2.675

	1680.9
	2.815

	1696.2
	2.670

	1696.6
	2.673

	1700.5
	2.762

	1709.5
	2.671

	1717.4
	2.657

	1722.9
	2.648

	1743.4
	2.635

	1754.7
	2.628

	1765.2
	2.746

	1771.3
	2.750

	1782.0
	2.619




Table A4: Density r of liquid Al70Ti30 versus temperature T. The relative standard uncertainty is 2%.  
	T [K]
	r [g/cm3]

	1700.8
	2.886

	1626.4
	2.889

	1653.4
	2.892

	1666.7
	2.895

	1582.8
	2.896

	1686.0
	2.899

	1710.4
	2.900

	1639.7
	2.901

	1599.6
	2.906

	1696.4
	2.908

	1592.2
	2.908

	1620.1
	2.913

	1611.3
	2.914

	1562.9
	2.917

	1677.8
	2.919

	1571.4
	2.919

	1552.6
	2.919

	1577.2
	2.922

	1659.1
	2.924

	1546.7
	2.925

	1558.5
	2.927

	1541.3
	2.928

	1619.8
	2.931

	1595.4
	2.939

	1537.8
	2.942

	1517.5
	2.943

	1522.5
	2.943

	1584.1
	2.945

	1610.6
	2.947

	1501.0
	2.949

	1498.0
	2.950

	1574.2
	2.959

	1476.2
	2.972

	1528.1
	2.973

	1492.3
	2.975

	1517.5
	2.975

	1486.9
	2.977

	1466.2
	2.987

	1483.0
	2.987

	1467.6
	2.994

	1452.8
	2.996






Table A5: Density r of liquid Al60Ti40 versus temperature T. The relative standard uncertainty is 2%.  
	T [K]
	r [g/cm3]

	1501.6
	3.243

	1524.9
	3.237

	1536.3
	3.229

	1547.8
	3.222

	1570.1
	3.211

	1582.0
	3.207

	1583.8
	3.206

	1598.3
	3.197

	1609.9
	3.181

	1622.9
	3.178

	1632.0
	3.177

	1638.3
	3.174

	1643.9
	3.165

	1650.6
	3.161

	1660.1
	3.160

	1670.9
	3.155

	1687.2
	3.140

	1709.2
	3.130

	1728.9
	3.117



















Table A6: Density r of liquid Al50Ti50 versus temperature T. The relative standard uncertainty is 2%.  
	T [K]
	r [g/cm3]

	1583.0
	3.436

	1586.6
	3.441

	1614.1
	3.436

	1621.5
	3.423

	1637.5
	3.428

	1639.7
	3.416

	1651.3
	3.426

	1656.7
	3.424

	1663.8
	3.405

	1673.3
	3.418

	1679.7
	3.396

	1680.3
	3.415

	1687.6
	3.413

	1694.9
	3.409

	1696.7
	3.385

	1703.1
	3.405

	1711.9
	3.373

	1718.0
	3.376

	1723.5
	3.394

	1733.0
	3.390

	1737.7
	3.373

	1743.6
	3.382

	1752.4
	3.364

	1755.1
	3.380

	1763.7
	3.349

	1766.4
	3.370

	1779.3
	3.365

	1780.7
	3.346

	1787.9
	3.335

	1789.9
	3.330

	1792.7
	3.356

	1807.3
	3.349

	1815.7
	3.325

	1822.7
	3.345

	1856.4
	3.327

	1859.8
	3.310

	1871.1
	3.319

	1907.0
	3.309

	1936.8
	3.301







Table A7: Density r of liquid Al40Ti60 versus temperature T. The relative standard uncertainty is 2%.  
	T [K]
	r [g/cm3]

	1698.6
	3.385

	1708.3
	3.380

	1719.3
	3.375

	1720.3
	3.381

	1731.4
	3.400

	1734.0
	3.384

	1747.4
	3.374

	1749.0
	3.386

	1758.9
	3.380

	1763.0
	3.357

	1765.0
	3.376

	1770.6
	3.374

	1773.3
	3.380

	1775.6
	3.379

	1778.3
	3.367

	1784.3
	3.367

	1788.7
	3.358

	1789.5
	3.346

	1792.3
	3.365

	1795.8
	3.362

	1804.0
	3.393

	1805.2
	3.370

	1810.0
	3.396

	1812.5
	3.364

	1818.0
	3.373

	1833.4
	3.395

	1853.4
	3.344

	1877.1
	3.361

	1919.5
	3.360













Table A8: Density r of liquid Al30Ti70 versus temperature T. The relative standard uncertainty is 2%.  
	T [K]
	r [g/cm3]

	1906.7
	3.516

	1888.3
	3.534

	1881.5
	3.543

	1854.9
	3.557

	1850.4
	3.558

	1846.4
	3.570

	1842.7
	3.574

	1835.7
	3.576

	1828.9
	3.583

	1824.1
	3.580

	1820.9
	3.588

	1815.0
	3.602

	1811.6
	3.605

	1805.2
	3.602

	1795.0
	3.602

	1788.5
	3.619

	1779.6
	3.613

	1774.3
	3.613

	1768.7
	3.621

	1762.0
	3.633

	1754.9
	3.633

	1925.3
	3.533

	1901.3
	3.536

	1879.8
	3.521

	1871.3
	3.553

	1857.6
	3.541

	1846.2
	3.525

	1844.3
	3.554

	1833.2
	3.552

	1827.0
	3.559

	1821.8
	3.569

	1815.5
	3.569

	1805.8
	3.553

	1803.0
	3.558

	1796.7
	3.570

	1791.5
	3.572








Table A9: Density r of liquid Al25Ti75 versus temperature T. The relative standard uncertainty is 2%.  
	T [K]
	r [g/cm3]

	1757.0
	3.707

	1776.5
	3.699

	1781.2
	3.706

	1790.8
	3.695

	1790.9
	3.690

	1795.6
	3.687

	1802.4
	3.698

	1811.6
	3.681

	1815.4
	3.692

	1817.2
	3.689

	1826.1
	3.692

	1832.2
	3.680

	1834.3
	3.674

	1835.6
	3.683

	1838.4
	3.671

	1847.0
	3.682

	1850.7
	3.668

	1853.1
	3.647

	1869.5
	3.636

	1885.8
	3.642

	1891.1
	3.633

	1898.4
	3.635

	1910.0
	3.624

	1918.7
	3.614

	1923.9
	3.614

	1939.9
	3.617

	1948.8
	3.614














Table A10: Density r of liquid Al20Ti80 versus temperature T. The relative standard uncertainty is 2%.  
	T [K]
	r [g/cm3]

	1808.1
	3.681

	1828.4
	3.709

	1829.9
	3.696

	1836.1
	3.703

	1842.8
	3.663

	1850.3
	3.672

	1866.6
	3.667

	1874.9
	3.683

	1878.5
	3.679

	1882.3
	3.673

	1893.3
	3.699

	1904.7
	3.648

	1912.8
	3.654

	1913.5
	3.678

	1915.3
	3.630

	1921.6
	3.664

	1928.3
	3.666

	1935.8
	3.660

	1943.2
	3.632

	1946.6
	3.624

	1947.3
	3.666

	1957.6
	3.643

	1958.3
	3.658

	1963.5
	3.623

	1968.5
	3.615

	1970.4
	3.659

	1994.1
	3.665

	2002.2
	3.624

	2025.1
	3.609

	1808.1
	3.681

	1828.4
	3.709

	1829.9
	3.696

	1836.1
	3.703

	1842.8
	3.663

	1850.4
	3.672

	1866.6
	3.668

	1874.9
	3.683

	1878.5
	3.679

	1882.3
	3.673

	1893.3
	3.699

	1904.7
	3.648

	1912.8
	3.654

	1913.5
	3.678

	1915.3
	3.630

	1921.6
	3.664

	1928.3
	3.666

	1935.8
	3.660

	1943.2
	3.632

	1946.6
	3.624

	1947.3
	3.666

	1957.6
	3.643

	1958.3
	3.658

	1963.5
	3.623

	1968.5
	3.615

	1970.4
	3.659

	1994.1
	3.665

	2002.2
	3.624

	2025.1
	3.609


























Table A11: Density r of liquid Al10Ti90 versus temperature T. The relative standard uncertainty is 2%.  
	T [K]
	r [g/cm3]

	1813.5
	3.850

	1826.2
	3.981

	1826.6
	3.856

	1835.3
	3.972

	1835.4
	3.832

	1849.2
	3.977

	1858.4
	3.964

	1869.0
	3.940

	1875.4
	3.843

	1883.3
	3.948

	1883.6
	3.843

	1903.4
	3.853

	1906.1
	3.820

	1912.0
	3.949

	1930.5
	3.833

	1943.8
	3.828

	1946.7
	3.925

	1950.6
	3.820

	1965.9
	3.847

	1974.2
	3.911

	1992.4
	3.817

	2000.7
	3.883

	2003.1
	3.800

	2007.2
	3.751

	2012.0
	3.801

	2021.6
	3.794

	2024.4
	3.807

	2033.6
	3.834

	2046.3
	3.805

	2049.1
	3.758

	2054.6
	3.796

	2099.4
	3.787

	2107.0
	3.789

	2113.3
	3.747










Surface tension
Table A12: Surface tension g of liquid Al versus temperature T. The relative standard uncertainty is 5%.  
	T [K]
	g [N/m]
	T [K]
	g [N/m]
	T [K]
	g [N/m]

	1063.3
	0.841
	1359.1
	0.826
	1454.7
	0.832

	1076.3
	0.847
	1366.6
	0.863
	1464.3
	0.834

	1128.3
	0.867
	1369.8
	0.812
	1472.3
	0.834

	1146.5
	0.832
	1369.8
	0.812
	1472.8
	0.795

	1162.7
	0.852
	1379.3
	0.798
	1475.5
	0.782

	1162.7
	0.878
	1383.7
	0.809
	1477.7
	0.788

	1188.9
	0.827
	1384.6
	0.863
	1483.1
	0.776

	1194.9
	0.839
	1384.8
	0.812
	1485.9
	0.838

	1194.9
	0.847
	1384.9
	0.851
	1494.4
	0.832

	1204.1
	0.822
	1390.8
	0.845
	1495.5
	0.785

	1213.5
	0.868
	1395.9
	0.805
	1502.1
	0.786

	1213.5
	0.837
	1397.7
	0.809
	1506.8
	0.831

	1222.6
	0.831
	1399.4
	0.857
	1511.5
	0.787

	1225.2
	0.875
	1399.8
	0.811
	1513.6
	0.814

	1238.4
	0.836
	1406.9
	0.783
	1514.2
	0.802

	1238.4
	0.827
	1408.4
	0.810
	1522.8
	0.797

	1240.1
	0.818
	1408.6
	0.853
	1524.4
	0.822

	1240.6
	0.847
	1409.5
	0.810
	1525.1
	0.790

	1257.2
	0.825
	1410.7
	0.784
	1535.5
	0.774

	1257.2
	0.847
	1410.8
	0.822
	1536.0
	0.836

	1262.0
	0.827
	1416.2
	0.846
	1537.2
	0.822

	1276.6
	0.857
	1417.0
	0.808
	1548.0
	0.801

	1277.2
	0.825
	1417.0
	0.808
	1550.4
	0.750

	1300.2
	0.819
	1423.4
	0.852
	1558.1
	0.805

	1307.6
	0.850
	1423.5
	0.781
	1559.2
	0.760

	1310.8
	0.871
	1430.8
	0.824
	1586.6
	0.759

	1318.5
	0.819
	1431.8
	0.844
	
	

	1333.1
	0.820
	1433.1
	0.807
	
	

	1333.3
	0.871
	1433.4
	0.802
	
	

	1335.7
	0.870
	1434.1
	0.802
	
	

	1340.9
	0.869
	1439.7
	0.804
	
	

	1348.8
	0.834
	1441.4
	0.855
	
	

	1350.1
	0.859
	1444.1
	0.828
	
	

	1352.7
	0.814
	1447.0
	0.804
	
	

	1353.8
	0.816
	1447.8
	0.796
	
	

	1356.9
	0.867
	1450.3
	0.803
	
	

	1358.4
	0.796
	1454.4
	0.791
	
	







Table A13: Surface tension g of liquid Ti versus temperature T. The relative standard uncertainty is 5%.  
	T [K]
	g [N/m]
	T [K]
	g [N/m]
	T [K]
	g [N/m]

	1823.0
	1.536
	1970.5
	1.48359
	2077.7
	1.498

	1825.2
	1.520
	1971.7
	1.47957
	2080.2
	1.496

	1838.8
	1.525
	1973.0
	1.53799
	2080.5
	1.453

	1841.0
	1.510
	1976
	1.49529
	2083.0
	1.458

	1841.2
	1.522
	1979.2
	1.4896
	2105.0
	1.495

	1843.4
	1.507
	1982.7
	1.52125
	2107.9
	1.457

	1854.0
	1.607
	1984.8
	1.49269
	2113.7
	1.493

	1859.4
	1.527
	1985.2
	1.48335
	2116.6
	1.455

	1861.6
	1.513
	1987.6
	1.51201
	2117.4
	1.495

	1861.8
	1.514
	1988.2
	1.592
	2120.4
	1.446

	1864.1
	1.499
	1990.2
	1.483
	2127.1
	1.523

	1886.2
	1.585
	1991.9
	1.488
	2127.4
	1.493

	1892.2
	1.519
	1999.5
	1.441
	2128.3
	1.456

	1894.5
	1.504
	2006.0
	1.510
	2130.3
	1.455

	1895.8
	1.526
	2006.6
	1.487
	2159.8
	1.481

	1898.2
	1.483
	2008.3
	1.559
	2161.1
	1.480

	1914.1
	1.526
	2008.5
	1.508
	2162.9
	1.453

	1916.5
	1.512
	2008.7
	1.472
	2164.1
	1.467

	1917.8
	1.510
	2011.1
	1.471
	2215.0
	1.479

	1920.2
	1.495
	2017.0
	1.475
	2217.5
	1.482

	1922.7
	1.579
	2018.9
	1.594
	2218.2
	1.452

	1930.6
	1.546
	2023.8
	1.484
	2220.7
	1.442

	1942.0
	1.496
	2024.2
	1.476
	2261.6
	1.474

	1943
	1.4
	2040.6
	1.495
	2265.0
	1.436

	1943.4
	1.511
	2043.0
	1.506
	2265.4
	1.474

	1944.8
	1.521
	2043.3
	1.465
	2304.6
	1.468

	1945.4
	1.513
	2045.8
	1.476
	2305.9
	1.470

	1945.9
	1.497
	2046.2
	1.477
	
	

	1947.1
	1.483
	2050.7
	1.483
	
	

	1950.0
	1.607
	2052.5
	1.522
	
	

	1954.2
	1.570
	2057.6
	1.529
	
	

	1961.4
	1.489
	2058.8
	1.586
	
	

	1966.8
	1.443
	2061.6
	1.507
	
	

	1967.9
	1.522
	2064.1
	1.489
	
	

	1969.2
	1.522
	2064.4
	1.470
	
	

	
	
	2066.8
	1.448
	
	








Table A14: Surface tension g of liquid Al90Ti10 versus temperature T. The relative standard uncertainty is 5%.  
	T [K]
	g [N/m]

	1575.6
	0.898

	1595.4
	0.865

	1611.6
	0.886

	1624.2
	0.884

	1629.6
	0.855

	1642.2
	0.842

	1651.2
	0.857

	1665.6
	0.874

	1674.6
	0.863

	1692.5
	0.837

	1701.4
	0.855























Table A15: Surface tension g of liquid Al80Ti20 versus temperature T. The relative standard uncertainty is 5%.  
	T [K]
	g [N/m]

	1426.4
	0.960

	1449.3
	0.956

	1472.0
	0.956

	1474.4
	0.954

	1499.4
	0.944

	1509.5
	0.938

	1511.1
	0.951

	1521.2
	0.938

	1529.7
	0.943

	1536.0
	0.942

	1538.3
	0.935

	1545.2
	0.943

	1549.9
	0.940

	1554.5
	0.940

	1559.9
	0.946

	1569.9
	0.935




















Table A16: Surface tension g of liquid Al70Ti30 versus temperature T. The relative standard uncertainty is 5%.  
	T [K]
	g [N/m]

	1784.0
	0.919

	1774.0
	0.926

	1758.8
	0.921

	1753.3
	0.928

	1747.7
	0.929



























Table A17: Surface tension g of liquid Al60Ti40 versus temperature T. The relative standard uncertainty is 5%.  
	T [K]
	g [N/m]

	1790.0
	0.953

	1803.1
	0.966

	1822.8
	0.952

	1855.7
	0.962

	1868.9
	0.948



























Table A18: Surface tension g of liquid Al50Ti50 versus temperature T. The relative standard uncertainty is 5%.  
	T [K]
	g [N/m]

	1555.4
	1.137

	1575.5
	1.135

	1593.9
	1.126

	1603.2
	1.103

	1616.2
	1.136

	1642.3
	1.083

	1657.4
	1.074

	1674.4
	1.053

	1699.1
	1.055

	1718.3
	1.072

	1739.5
	1.086

	1760.9
	1.079

	1784.4
	1.055

	1814.0
	1.076






















Table A19: Surface tension g of liquid Al50Ti50 versus temperature T. The data was obtained under microgravity. The relative standard uncertainty is 5%.  
	T [K]
	g [N/m]

	1643
	1.261

	1702
	1.242

	1706
	1.339

	1749.5
	1.198

	1754
	1.325

	1782.5
	1.261

	1793.5
	1.204

	1838.5
	1.136

	1845.5
	1.204

	1871
	1.204

	1894.5
	1.188

	1915.5
	1.056























Table A20: Surface tension g of liquid Al40Ti60 versus temperature T. The relative standard uncertainty is 5%.  
	T [K]
	g [N/m]

	1819.1
	1.251

	1830.8
	1.244

	1865.8
	1.247

	1877.5
	1.235




























Table A21: Surface tension g of liquid Al30Ti70 versus temperature T. The relative standard uncertainty is 5%.  
	T [K]
	g [N/m]

	1828.3
	1.366

	1840.7
	1.382

	1853.0
	1.355

	1861.9
	1.348

	1865.4
	1.357

	1867.7
	1.362

	1877.8
	1.335

	1884.0
	1.364

	1890.9
	1.326

	1914.9
	1.316

	1921.1
	1.346

	1937.4
	1.324

	1939.6
	1.311

	1970.6
	1.317

	2020.2
	1.318





















Table A22: Surface tension g of liquid Al25Ti75 versus temperature T. The relative standard uncertainty is 5%.  
	T [K]
	g [N/m]

	1786.8
	1.356

	1805.2
	1.29

	1829.8
	1.367

	1860.5
	1.286

	1891.2
	1.331

	1908.8
	1.369

	1921.1
	1.379

	1922.0
	1.314

	1927.2
	1.369

	1934.3
	1.288

	1963.9
	1.337

	1971.3
	1.296

	1983.6
	1.254

	1988.3
	1.323

	2000.6
	1.344

	2012.8
	1.355

	2020.6
	1.287

	2045.3
	1.287



















Table A23: Surface tension g of liquid Al20Ti80 versus temperature T. The relative standard uncertainty is 5%.  
	T [K]
	g [N/m]

	1789.2
	1.288

	1825.6
	1.279

	1833.6
	1.382

	1849.9
	1.357

	1881.3
	1.330

	1893.3
	1.309

	1898.6
	1.365

	1910.8
	1.268

	1922.9
	1.308

	1935.1
	1.284

	1941.1
	1.347

	1953.0
	1.355

	1959.5
	1.259

	1983.8
	1.288

	1988.9
	1.362

	2008.2
	1.241

	2036.7
	1.340

	2072.6
	1.297



















Table A24: Surface tension g of liquid Al10Ti90 versus temperature T. The relative standard uncertainty is 5%.  
	T [K]
	g [N/m]

	1886.1
	1.581

	1906.8
	1.541

	1934.9
	1.543

	1949.6
	1.499

	1967.9
	1.531

	1972.8
	1.506

	1993.6
	1.498

	2005.7
	1.466

	2005.8
	1.527

	2015.6
	1.501

	2021.7
	1.543

	2038.5
	1.378

	2052.3
	1.410

	2057.5
	1.409

	2063.8
	1.414

	2067.0
	1.451

	2073.1
	1.446

	2080.2
	1.429

	2082.8
	1.344

	2091.5
	1.457

	2116.0
	1.479

	2124.6
	1.501

	2133.4
	1.345

	2152.4
	1.405

	2175.2
	1.348

	2190.5
	1.305















Normal spectral emissivity
Table A25: Normal spectral emissivity e(l,T) of liquid Ti at l=940 nm versus temperature T. The relative standard uncertainty is 4%.  
	T [K]
	e(l=940 nm,T)

	1970
	0.381

	1963
	0.370

	1953
	0.359

	1943
	0.368

	1933
	0.373


























Table A26: Normal spectral emissivity e(l,T) of liquid Al20Ti80 at l=940 nm versus temperature T. The relative standard uncertainty is 4%.  
	T [K]
	e(l=940 nm,T)

	1999
	0.386

	1986.8
	0.393

	1966.4
	0.403

	1958.2
	0.407

	1949.0
	0.403



























Table A27: Normal spectral emissivity e(l,T) of liquid Al50Ti50 at l=940 nm versus temperature T. The relative standard uncertainty is 4%.  
	T [K]
	e(l=940 nm,T)

	1840.2
	0.317

	1827.2
	0.317

	1818.1
	0.319

	1808.1
	0.316

	1799.1
	0.318

	1788.1
	0.319

	1776.0
	0.320

	1766.0
	0.322

	1757
	0.316

	1744.0
	0.316

	1736.0
	0.319























Table A28: Normal spectral emissivity e(l,T) of liquid Al70Ti30 at l=940 nm versus temperature T. The relative standard uncertainty is 4%.  
	T [K]
	e(l=940 nm,T)

	1825.2
	0.287

	1815.9
	0.299

	1798.5
	0.302

	1786.2
	0.305

	1769.9
	0.310

	1775.0
	0.292

	1766.8
	0.300

	1749.4
	0.302

	1735.0
	0.302

	1719.7
	0.312

	1706.4
	0.310

	1693.1
	0.317























Molar heat capacity over normal spectral emissivity at 940 nm
Table A29: Molar heat capacity cp over normal spectral emissivity e(l=940 nm, T) of liquid Ti versus temperature T. The relative standard uncertainty is 2%.  
	T [K]
	cp/e(l=940 nm,T) [J/K/mol]

	1930
	135.188

	1975
	135.558

	1995
	135.135

	2015
	131.428

	2030
	130.940


























Table A30: Molar heat capacity cp over normal spectral emissivity e(l=940 nm, T) of liquid Al20Ti80 versus temperature T. The relative standard uncertainty is 3%.  
	T [K]
	cp/e(l=940 nm,T) [J/K/mol]

	2030
	149.263

	1990
	148.174

	1930
	142.172

	1960
	143.044




























Table A31: Molar heat capacity cp over normal spectral emissivity e(l=940 nm, T) of liquid Al50Ti50 versus temperature T. The relative standard uncertainty is 3%.  
	T [K]
	cp/e(l=940 nm,T) [J/K/mol]

	1886
	167.043

	1820
	152.747

	1808
	143.508

	1780
	137.693

	1765
	138.647







 
