Supplementary info

Supplementary Table 1. Characteristics of ~ 2mm ø twines used for experimentation.

| Material | Form | Decitex (g·10 km) | Supplier |
| --- | --- | --- | --- |
| Cotton | Braided | n.m. | Homebase, UK |
| Jute | Twisted | n.m. | Homebase, UK |
| Kuralon (PVA) | Braided or twisted | 1330 | Tecnored, ES |
| PA | Braided or twisted | 470 | Tecnored, ES |
| PES1 | Braided or twisted | 1100 | Sioen Industries NV, BE |
| PES2 | Braided or twisted | 1670 | Tecnored, ES |
| PP | Braided or twisted | 1670 | Tecnored, ES |
| Sisal | Twisted | n.m. | Homebase, UK |

PA – polyamide, PES1/PES2 – polyester from two suppliers, PP – polypropylene, PVA – polyvinylalcohol, n.m. – not measured.

Supplementary Figure 1 - Ladder system to deploy 1 m ropes sections at Kerrera experimental seaweed farm, Scotland (56.3820o N, 5.5370o E). Each rope was spaced 1 m apart and carried twine grown in experiment 1 and 2. The ropes were grown horizontally at 1.5 m depth, not vertically as indicated by picture.

|  | 4 wk |  | 6 wk |  |
| --- | --- | --- | --- | --- |
|  | Braided | Twisted | Braided | Twisted |
| PA |  |  |  |  |
| PES1 |  |  |  |  |
| PES2 |  |  |  |  |
| PP |  |  |  |  |
| PVA |  |  |  |  |
| Cotton |  |  |  |  |
| Jute |  |  |  |  |
| Sisal |  |  |  |  |

Supplementary Figure 2. Saccharina latissima sporophyte development on different ~ 2 mm ø twine, 4 and 5 wk after seeding with meiospores in E1.  Shown is the median result of five replicates. PA – polyamide, PES1/2 – polyester from two suppliers, PP – polypropylene, PVA – polyvinylalcohol.

|  | 4 wk |  | 6 wk |  |
| --- | --- | --- | --- | --- |
|  | Untreated | Corona | Braided | Twisted |
| PA |  |  |  |  |
| PES1 |  |  |  |  |
| PP |  |  |  |  |
| PVA |  |  |  |  |

Supplementary Figure 3. Saccharina latissima sporophyte development on different ~ 2 mm ø twine, 4 and 6 wk after seeding with meiospores in E1.  Shown is the median result of five replicates. PA – polyamide, PES1/2 – polyester from two suppliers, PP – polypropylene, PVA – polyvinylalcohol.

Supplementary Table 2. Physiognomy of Saccharina latissima 3 mo following seeding as sporophytes onto different polymer twines, used for detachment trials. Shown is mean ± standard deviation.

| Polymer | Frond length (mm) | Frond width (mm) | Stipe length (mm) | Hapterae length (mm) | Samples taken |
| --- | --- | --- | --- | --- | --- |
| PA Br | 154 ± 50 | 36 ± 7 | 5.9 ± 3.4 | 23 ± 4 | 3 |
| PES Br | 118 ± 54 | 34 ± 8 | 4.0 ± 0.1 | 25 ± 1 | 2 |
| PES Tw | 146 ± 52 | 39 ± 13 | 11.1 ± 7.6 | 17 ± 11 | 6 |
| PP Br | 169 ± 52 | 48 ± 10 | 6.4 ± 1.9 | 19 ± 9 | 6 |
| PP Tw | 233 ± 166 | 48 ± 17 | 8.8 ± 6.5 | 32 ± 12 | 6 |
| PVA Br | 238 ± 57 | 61 ± 13 | 9.6 ± 3.4 | 29 ± 10 | 6 |
| PVA Tw | 150 ± 113 | 44 ± 18 | 7.6 ± 3.4 | 23 ± 7 | 6 |
| Cotton | 212 ± 20 | 59 ± 9 | 10.6 ± 4.3 | 23 ± 6 | 6 |
| Jute | 111 ± 8 | 35 ± 4 | 5.4 ± 0.6 | 12 ± 4 | 6 |
| Sisal | 95 ± 35 | 39 ± 6 | 5.5 ± 0.4 | 25 ± 6 | 2 |

PA – polyamide, PES – polyester, PP – polypropylene, PVA – polyvinylalcohol, Br – braided, Tw – twisted.