Exploring basalt: A Methodological Framework for Analysing Wear Traces on Basalt Tools

Lena Asryan1 and Veerle Rots1,2

1TraceoLab, University of Liège, Place du 20-août 7, 4000 Liège, Belgium

2F.R.S.-FNRS, Belgium

Corresponding author: L. Asryan (lasryan@uliege.be)

ORCID numbers: 0000-0002-7895-8812 (Lena Asryan); 0000-0002-6404-3160 (Veerle Rots)

Supplementary information

Supplementary table S1: Basalt varieties used in this study and their elemental composition determined through SEM-EDS analysis

| Basalt varieties | Macro image (analysed portion in red) | SEM micrograph with EDS analysis points |
| --- | --- | --- |
| Basalt 1 (AM7-16) Ethiopian basalt |  |  |
|  | Elemental composition of analysed points Basalt 1 |  |
| Points; C; O; Na; Mg; Al; Si; P; S; K; Ca; Ti; Mn; Fe; Mass%. 1; 3,14; 41,97; 0,69; 6,87; 2,95; 22,03; 0,19; ND; 0,08; 12,91; 0,79; 0,24; 8,13; 100. 2; 5,83; 43,64; 2,57; 0,5; 12,34; 20,58; 0,12; 0,04; 0,36; 10,27; 0,5; ND; 3,27; 100. 3; 4,97; 46,82; 2,4; 0,34; 13,3; 20,36; 0,07; 0,05; 0,16; 8,41; 0,3; 0,05; 2,77; 100. 4; 7,22; 46,81; 0,3; 13,23; 1,12; 14,06; 0,07; 0,06; 0,17; 2,29; 0,11; 0,32; 14,26; 100. 5; 3,33; 23,78; 1,53; 1; 4,6; 10,69; 0,16; ND; 0,3; 3,32; 7,29; 0,46; 43,54; 100. 6; 4,75; 45,74; 3,76; 0,55; 11,78; 22,68; 0,18; ND; 0,4; 6,37; 0,34; 0,02; 3,43; 100. 7; 5,89; 42,95; 0,98; 1,66; 3,89; 17,62; 1,48; 0,01; 0,37; 7,4; 0,72; 0,24; 16,78; 100. 8; 6,13; 38,56; 2,56; 1,19; 7,15; 17,1; 0,44; 0,02; 0,41; 5,55; 1,94; 0,31; 18,63; 100. 9; 4,01; 44,44; 3,08; 0,59; 12,33; 22,49; 0,08; 0,03; 0,32; 8,08; 0,53; 0,01; 3,99; 100. 10; 11,02; 40,64; 0,96; 0,55; 3,15; 9,18; 0,49; 0,14; 0,23; 4,76; 5,81; 0,39; 22,69; 100. 11; 4,76; 49,78; 3,28; 0,23; 11,98; 20,64; 0,17; ND; 0,24; 5,76; 0,36; 0,02; 2,78; 100. |
| Basalt 2 (OldBas4) Olduvai basalt |  |  |
|  | Elemental composition of analysed points Basalt 2 |  |
| Points; C; O; Na; Mg; Al; Si; P; S; K; Ca; Ti; Mn; Fe; Mass%. 1; 10,39; 46,64; 3,08; 1,56; 5,64; 17,12; 0,36; 0,07; 1,69; 5,37; 0,78; 0,82; 6,48; 100. 2; 9,75; 50,44; 1,13; 3,33; 3,49; 10,89; 0,18; 0,16; 2,31; 1,97; 1,53; 4,73; 10,11; 100. 3; 9,85; 40,98; 2,71; 1,24; 5,32; 14,29; 0,44; 0,1; 1,54; 4,63; 0,86; 3,73; 14,32; 100. 4; 6,79; 45,91; 4,17; 0,47; 8,73; 24,01; 0,13; ND; 3,34; 2,69; 0,49; 0,71; 2,56; 100. 5; 8,47; 40,36; 2,46; 0,64; 6,55; 21,66; 0,29; 0,03; 5,06; 4,01; 0,82; 2,49; 7,15; 100. 6; 9,92; 46,51; 3,09; 0,75; 6,05; 16,85; 0,42; ND; 2,01; 5,51; 0,93; 1,07; 6,89; 100. 7; 11,21; 44,64; 3,27; 0,81; 6,01; 15,55; 0,3; 0,13; 1,72; 4,95; 0,78; 2,04; 8,61; 100. 8; 9,87; 46,99; 3,32; 1,25; 5,84; 17,34; 0,56; 0; 1,75; 5,17; 0,74; 0,75; 6,41; 100. 9; 8,5; 47,15; 3,67; 0,64; 6,94; 19,08; 0,17; ND; 2,66; 4,28; 0,8; 1,07; 5,03; 100. 10; 7,81; 44,63; 2,7; 0,55; 6,95; 21; 0,15; 0,1; 3,41; 3,03; 0,49; 2,59; 6,58; 100. 11; 8,61; 43,2; 1,35; 0,57; 3,08; 8,09; 1,14; 0,17; 0,85; 9,43; 1,8; 6,2; 15,53; 100. 12; 5,92; 44,42; 3,84; 0,49; 8,51; 23,12; 0,17; 0,02; 3,46; 4,47; 0,78; 0,79; 4,03; 100. 13; 9,23; 46,4; 1,78; 0,44; 3,91; 11,02; 0,25; 0,17; 1,44; 2,93; 1,38; 6,78; 14,28; 100. 14; 8,84; 48,36; 3,82; 0,34; 7,05; 19,64; 0,19; 0,03; 2,49; 2,86; 0,49; 1,78; 4,12; 100. 15; 7,91; 43,22; 2,74; 0,79; 5,55; 15,36; 0,33; 0,09; 1,82; 6,62; 0,62; 2,94; 12,02; 100. |
| Basalt 3 (BagBas1) Armenian basalt |  |  |
|  | Elemental composition of analysed points Basalt 3 |  |
| Points; C; O; Na; Mg; Al; Si; P; S; K; Ca; Ti; Mn; Fe; Total (Mass%). Point 33; 2.73; 36.86; 0.94; 2.57; 3.97; 12.1; 0.14; ND; 0.08; 2.01; 0.31; 0.08; 38.23; 100. Point 34; 4.71; 46.25; 0.81; 1.82; 3.5; 34.04; 0.13; ND; 0.23; 2.25; 0.38; 0.32; 5.57; 100. Point 35; 3.63; 43.32; 0.92; 1.96; 3.8; 21.96; 0.05; 0.01; 0.22; 1.9; 0.46; ND; 21.78; 100. Point 36; 4.62; 54.05; 0.62; 2.32; 3.26; 13.28; 0.06; 0.03; 0.12; 8.59; 8.35; 0.06; 4.65; 100. Point 37; 3.95; 50.28; 0.7; 1.81; 3.01; 32.54; 0.03; ND; 0.1; 1.89; 0.19; 0.22; 5.27; 100. Point 38; 3.12; 43.2; 0.83; 4.42; 4.8; 9.58; 0.13; 0.01; 0.14; 1.8; 0.25; 0.13; 31.58; 100. Point 39; 3.04; 49.37; 0.78; 9.28; 7.39; 16.04; 0.07; 0.01; 0.18; 2.21; 0.48; 0.34; 10.81; 100. Point 40; 3.39; 50.41; 1.52; 3.77; 10.82; 16.93; 0.06; ND; 0.35; 6.75; 0.29; 0.38; 5.32; 100. Point 41; 4.45; 46.05; 1.36; 2.29; 5.01; 8.68; ND; ND; 0.15; 2.19; 1.11; 0.03; 28.69; 100. Point 42; 4.45; 53.26; 1.1; 2.38; 6.56; 15.25; ND; 0.02; 0.15; 7.82; 5.81; 0.03; 3.17; 100. Point 43; 3.66; 54.56; 1.42; 5.07; 9.98; 16.2; 0.11; ND; 0.25; 4.21; 0.15; ND; 4.38; 100. Point 44; 4.6; 51.68; 1.88; 2.82; 11.38; 17.14; 0.08; 0.07; 0.3; 5.65; 0.36; 0.23; 3.81; 100. Point 45; 4.47; 49.88; 2.37; 1.56; 12.4; 19.13; 0.02; 0.03; 0.34; 6.37; 0.23; 0.13; 3.08; 100. Point 46; 4.59; 47.32; 1.97; 3.92; 10.19; 19.67; 0.15; 0.05; 0.71; 5.17; 0.35; ND; 5.91; 100. Point 47; 5.18; 52.25; 1.53; 3.52; 10.96; 16.66; 0.06; 0.02; 0.23; 5.07; 0.39; 0.13; 3.99; 100. Point 48; 4.21; 53.7; 1.12; 6.98; 8.72; 15.17; 0.06; ND; 0.17; 2.7; 0.23; 0.13; 6.8; 100. Point 49; 3.87; 50.87; 2.48; 1.35; 12.62; 19.04; ND; 0.04; 0.45; 6.09; 0.35; ND; 2.85; 100. Point 50; 4.23; 51.73; 3.21; 3.02; 9.57; 19.03; ND; 0.03; 0.61; 4.16; 0.4; 0.08; 3.93; 100. Point 51; 4.55; 49.62; 1.67; 1.82; 9.3; 21.5; 0.11; 0.1; 4.46; 2.74; 0.36; 0.12; 3.65; 100. Point 52; 3.21; 49.24; 2.01; 1.68; 13; 19.51; 0.13; 0; 0.37; 7.15; 0.38; 0.14; 3.18; 100. |
| Basalt 4 (MC3) French basalt |  |  |
|  | Elemental composition of analysed points Basalt 4 |  |
| Points; C; O; Na; Mg; Al; Si; P; S; K; Ca; Ti; Mn; Fe; Mass%. 19; 4,75; 40,74; 1,51; 1,56; 3,81; 6,26; 0,19; ND; 0,44; 2,01; 8,88; 0,43; 29,41; 100. 20; 5,99; 48,63; 1,03; 11,81; 2,42; 13,19; 0,05; ND; 0,28; 1,92; 0,39; 0,32; 13,97; 100. 21; 6,54; 46,76; 1,12; 1,83; 2,69; 4,99; 0,06; ND; 0,33; 2,27; 7,51; 0,36; 25,53; 100. 22; 10,24; 38,18; 1,29; 1,5; 2,33; 4,81; 0,11; 0,02; 0,26; 8,86; 0,31; 0,74; 31,36; 100. 23; 12; 48,28; 1,06; 1,38; 1,91; 3,83; 0,08; ND; 0,31; 6,87; 0,26; 0,5; 23,53; 100. 24; 14,36; 52,61; 0,52; 1,5; 1,17; 2,39; 0,13; 0,04; 0,18; 19,12; 0,15; 0,59; 7,23; 100. 25; 15,34; 52,57; 0,56; 2,55; 0,96; 3,09; 0,38; 0,04; 0,2; 4,76; 0,07; 0,28; 19,18; 100. |