# Supplementary Material

# Table of data used to compile Fig 2

| Material | Energy density (by volume or weight, as specified) | Density (kg/m3) | Horizontal launch speed (m/s) | Range (m) |
| --- | --- | --- | --- | --- |
| Muscle | 70J/kg[1] | 1060[2] | 1.41 | 0.31 |
| Spring Steel | 1.08MJ/m [3] | 7900[4] | 1.81 | 0.53 |
| Filaree | 761 kJ/m3 ‡ | 500 ‡ | 3.93 | 2.62 |
| Yew wood(dry) | 500 kJ/m3[5] | 611 [6] | 5.06 | 4.36 |
| Shape memory alloy | 1.1 kJ/kg [7] | 6450 [8] | 5.73 | 5.58 |
| Poly (dimethyl) siloxane (PDMS) | 1300 [9] | 965[9] | 6.09 | 6.3 |
| Tendon | 2.5 kJ/kg [5] | 1120[10] | 8.44 | 12.1 |
| Kelp | 2.6MJ/kg [5] | 985 [11] | 8.67 | 12.8 |
| Rubber (natural) | 3MJ/kg [5] | 910 [12] | 9.69 | 16.0 |
| CNT yarn | 3MJ/m3 [13] | 1400[13] | 9.84 | 16.55 |
| Polystyrene SMP | 3261 J/kg [14] † | 920[14] | 17.11 | 50.07 |
| Dual-network hydrogel | 1160 J/kg [15]† | 1000 (approximated as water, the major component of the hydrogel, due to lack of data) | 18.60 | 59.16 |
| Elastin | 95 [3] | 1300 [3] | 24.18 | 100.0 |
| Kevlar | 40MJ/kg [5] | 1440 [16] | 29.24 | 146 |
| Spider Silk | 120 MJ/m2 [17] | 1250 [17] | 52.30 | 468 |
| CNT at 15% strain | 7800 MJ/m3 [18] | 1400 [13] | 398.47 | 27200 |

† Strain energy calculated from maximum strain in Hookean region, as:

E=12YVε2

Where E is stored elastic energy (Joules), Y=Young’s modulus (Pascals) , V = volume (metres cubed) and ε = strain (dimensionless). This yields J/kg when divided by the density in kg/m3.

‡See below for assumptions underlying these figures.

Following the work of Evangelista et al., we assume 2.4% of stored energy is translated into horizontal movement. Standard equations of motion for constant acceleration are used to calculate trajectory, with drag neglected. Volume of the awn was taken to be 1x10-8m3, assuming (in the absence of density data) a density of 500kg/m3, intermediate between grass (1400 kg/m2) and balsa (160kg/m3). While this is not rigorous, the results are not very sensitive to such small changes in mass. Since the effect is constant across all calculations it does not affect the intercomparison of materials.