Supporting information:

# Silane-functionalized graphene nanoplatelets for silicone rubber nanocomposites

He Ren1,4†, Eunice Cunha2†, Zheling Li2, Lei Wang1,4, Ian A. Kinloch2, Dian Yi2,3, Andrew Kretinin2, Quanji Sun1,4, Zhaodong Fan1,4** and Robert J. Young2*

1Beijing Institute of Aeronautical Materials (BIAM), Beijing, 10095, China

2National Graphene Institute and Department of Materials, University of Manchester, Manchester M13 9PL, UK

3School of Physics and Astronomy, University of Manchester, Manchester M13 9PL, UK

4Beijing Engineering Research Centre of Graphene Application, Beijing, 100095, China

Corresponding authors: *robert.young@manchester.ac.uk; **fanzhaodong99@sohu.com

†These authors contributed equally

Table S1: XPS atomic concentration and atomic ratio of the chemical elements on the GNP, f-GNP and f-GNP-Si.

|  | At (%) |  |  |  | ratio |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | C | O | N | Si | [N]:[O] | [Si]:[O] | [Si]:[N] |
| GNP | 98.4 | 1.6 |  |  |  |  |  |
| f-GNP | 87.4 | 7.9 | 4.7 |  | 0.6 |  |  |
| f-GNP-Si | 76.8 | 12.5 | 7.2 | 3.5 | 0.6 | 0.3 | 0.5 |

Table S2: Melting temperatures, melting enthalpies and degree of crystallization of the neat SR, GNP and f-GNP-Si SR composites at different loadings

|  | Tm (οC) | ΔHm (J/g) | χc (%) |
| --- | --- | --- | --- |
| SR | -45.4 | 13.6 | 36.4 |
| SR GNP 0.5 phr | -44.9 | 12.9 | 34.7 |
| SR GNP 1.0 phr | -44.6 | 12.6 | 34.0 |
| SR GNP 2.0 phr | -43.3 | 11.2 | 30.6 |
| SR GNP 5.0 phr | -43.3 | 11.1 | 31.2 |
| SR f-GNP-Si 0.5 phr | -44.6 | 13.2 | 35.5 |
| SR f-GNP-Si 1.0 phr | -43.9 | 12.3 | 33.2 |
| SR f-GNP-Si 2.0 phr | -43.4 | 11.8 | 32.2 |
| SR f-GNP-Si 5.0 phr | -43.3 | 11.7 | 32.9 |