Supplementary information for

Modelling the growth and filling of creep-induced grain-boundary cavities in self-healing alloys

Y. Fu, S. van der Zwaag, N.H. van Dijk

Summary of the calculation process

1. Calculation of the stress-induced vacancy flux

(S1)

in which xv = 7.4×10-4 is the vacancy concentration at the grain boundary, Dgbv=1.74×10-12 m2s-1 is the vacancy diffusivity, σn is calculated using Linear Elastic Material module with stationary node.

Governing equations:

(S2)

(S3)

(S4)

in which F is the body force per unit volume, σ is the Cauchy stress tensor, ε is the elastic strain tensor, u is the displacement and C is the fourth order of stiffness tensor.

Boundary conditions:

Symmetry: the z axis is the rotational symmetry axis; the horizontal plane of z = 0 is set as the symmetry plane.

Boundary load: a constant stress with the magnitude of σ0 is applied uniformly to the top edge of the simulation volume (see Fig. 1 in main text).

Other input: the material is regarded as isotropic with the density ρ of 7800 kg/m3, Young’s modulus E of 165 GPa [40] and the Poisson’s ratio ν of 0.33 [40].

After the calculation, the z component of the stress tensor is taken as the normal stress σn.

2. Calculation of the Kirkendall vacancy flux

From eqs. 4 – 5,

(S5)

in which Js (solute flux) is calculated using the Transport of Diluted Species module.

Governing equations:

(S6)

(S7)

where xs is the concentration of the solute s (atom fraction), Js is the flux (atom∙m-2∙s-1)

Boundary conditions:

Symmetry: the z axis is the rotational symmetry axis; the horizontal plane of z = 0 is set as the symmetry plane.

Concentration at the edge of the cavity: xs at cavity edge = 0.07 at.%.

Initial concentration: xs(t = 0) = 0.25, 0.5, 1, 2, 3, and 4 at.%

Diffusivity: 	Dms=7.39 × 10-19m2/s  (in the bulk, i.e. |z|>δ/2)

Dgbs=10n∙Dms (in the grain boundary, i.e. |z|≤δ/2, n = 1 – 9)

Dmh=1.50 × 10-21 m2/s  (in the bulk, i.e. |z|>δ/2)

Dgbh=10n∙Dmh (in the grain boundary, i.e. |z|≤δ/2, n = 1 – 9)

3. Calculation of the net vacancy flux

The net vacancy flux is the sum of the stress-driven vacancy flux and the Kirkendall vacancy flux:

(S8)