Controllable Si oxidation mediated by annealing temperature and atmosphere

Feitao Li1, Dong Wang1, *, Malte Klingenhof2, Dominik Flock1, Honglei Wang1, Peter Strasser2, Peter Schaaf1

1 TU Ilmenau, Chair Materials for Electrical Engineering and Electronics, Institute of Materials Science and Engineering and Institute of Micro- and Nanotechnologies MacroNano, Gustav-Kirchhoff-Strasse 5, 98693 Ilmenau, Germany

2 TU Berlin, Department of Chemistry, Chemical Engineering Division, 10623 Berlin, Germany

*Corresponding authors: dong.wang@tu-ilmenau.de (D. Wang)

Figure S1 Experimental temperature profiles for the isothermal treatments in RTP at 500, 650, 800, 950 and 1050 ℃ for 1 min holding time, respectively. The dashed line corresponds to the Au-Si eutectic temperature (～363 ℃)

Figure S2 Cross section of TEM lamella for 800-H, and the STEM-EDS mapping of one particle is shown in Figure 2(a).

Figure S3 SEM micrographs in plan view for the various dewetted samples. Temperature and atmosphere are stated. Percentages of dewetting (dewetted area/total area, as analyzed by ImageJ) are shown in the upper right corners of each micrograph.

Figure S4 Enlarged details of local areas in Figure 3(c, d). Thin covering layers are marked by arrows.

Figure S5 Phase diagram showing the oxidation of Si as a function of O2 concentration and temperature. Reprinted from Ref. [19] in main text with permission from AIP publishing.

The existence of Si active oxidation:

A diagram in Figure S5 shows the oxidation of Si as a function of O2 concentration and temperature.

In the present work, the purities of used Ar and H2 are 6.0N (99.9999%) and 5.0N (99.999%), respectively. The volume ratio of Ar and H2 is 30:1. The partial oxygen pressure should be related to the residual gas and to the impurities of the Ar and H2, and it can be estimated as follow:

VO2Vtotal=pO2ptotal 		(1)

As we use Ar and H2 in a 30:1 volume ratio, we can consider that we have 31 parts of volume. In the case of Ar, a purity of 99.9999% leads to a 0.0001% of impurities, and the same applies to H2. Assuming that the impurities of the gases are air, with a 21% of oxygen, the amount of oxygen in those 31 parts can be estimated as:

21%VAr·impuritiesAr+VH2·impuritiesH2=2110030·10-6+1·10-5=8.4·10-4

parts of oxygen in 31 parts of volume.

From eq. (1) the partial pressure of oxygen in our chamber during the annealing process will be:

pO2=ptotal·VO2Vtotal=1 bar·8.4·10-431= 2.7·10-7 bar=0.27 ppm

As marked in the diagram (red dots), the value (0.27 ppm) is lower than the critical partial pressure (0.4 ppm) that allows for the active oxidation of Si at 950 °C. This means that the annealing parameters that we used make the Si active oxidation possible at 950 °C. By contrast, this value is much larger than the critical partial pressure at 800 °C, and, therefore, stripe-like structures (SiOx) can be observed in 800-H since the Si passive oxidation happens at 800 °C.