Supporting information

Insights into the electrocatalytic behavior of nitrogen and sulfur co-doped carbon nanotubes toward oxygen reduction reaction in alkaline media

Gutru Rambabua,b,c,*, Zarina Turtayevab, Feina Xub, Gael Maranzanab, Mélanie Emoa, Sébastien Huponta, Mohamed Mamloukc, Alexandre Desforgesa Brigitte Vigoloa,

a Université de Lorraine, CNRS, Institut Jean Lamour, F-54000 Nancy, France

bUniversité de Lorraine, CNRS, LEMTA, F-54000 Nancy, France

c School of Engineering, Newcastle University, Newcastle Upon Tyne, United Kingdom

* Corresponding author

I. Estimation of the metal-based impurity content after the purification/oxidation treatment

The precise quantification of the metal-based impurities in the CNT samples is in general not direct. And this is especially the case for the used MWCNT sample since they contain a mixture of metal-based impurities. The information we have from the supplier specifies that around 8 wt.% of alumina come from the CVD support remains after their post-synthesis treatment (applied by the supplier). Cobalt and iron were used as CVD catalyst for the MWCNT growth, their form in the raw MWCNT sample (metal, oxide or carbide or a mixture of them) is not clearly known. In the oxidized sample, it is not possible to know which of these metal-based compounds remain. The estimation the metal-based impurities in the MWCNTs required we make some hypotheses. These hypotheses are given below:

- the remaining alumina which is certainly outside the MWCNTs, thus accessible to acids can be efficiently removed. Alumina is assumed to be completely removed after oxidation.

- for the sake of simplification, let’s assume that iron and cobalt are under their metal form in the treated MWCNT sample. Indeed, the remaining metal impurities are obviously not accessible to the reactants otherwise they would have been removed from the sample. They are certainly located inside the inner channel of the MWCNTs, isolated from any oxidative surrounding medium.

- And, we assume that the same quantity of iron and cobalt was used for the CVD synthesis.

The stable metal oxides after TGA are Fe2O3 and Co3O4.

That means that the increase in weight when Fe oxidizes is 2MFe+3MO-2MFe2MFe=42.97%

For Co3O4, the gain in weight is: 3MCo+4MO-3MCo3MCo=36.02%

That means that the increase in weight for the oxidized CNTs is an average of these two gains in weight, i.e. 39.59 %

By following these hypotheses, the oxidized MWCNTs contain: 3.02 wt.% of metal-based impurities.

II. XPS analysis

Figure S1. XPS survey spectra for pristine CNTs and oxidized CNTs

Figure S2. XPS survey spectra for N-Ox-CNTs

Figure S3. XPS survey spectra for NS-Ox-CNTs

| Sample | C (at.%) | O (at.%) | N (at.%) | S (at.%) |
| --- | --- | --- | --- | --- |
| Pristine CNTs | 99.01 | 0.99 | - | - |
| OX-CNTs | 92.03 | 7.97 | - | - |
| N-Ox-CNTs | 97.03 | 1.28 | 1.69 | - |
| NS-Ox-CNTs | 96.15 | 2.26 | 0.94 | 0.65 |

Table S1 Quantification of elements from XPS

Cdl=0.03mF

(b)

(b)

(a)

(a)

Cdl=0.14mF

(d)

(d)

(c)

Cdl=0.20mF

(e)

(f)

Cdl=0.23mF

(g)

(h)

(j)

Cdl=0.36 mF

Figure S4: Cyclic voltammograms in non-faradaic region with the scan rate of 20-100 mV/S (a) Pristine CNTs, (c) N-CNTs, (e) NS-CNTs, (g) N-Ox-CNTs and (i) NS-OX-CNTs and linear fitting of current density vs scan rate to derive double layer capacitance (b) Pristine CNTs, (d) N-CNTs, (f) NS-CNTs, (h) N-Ox-CNTs and (j) NS-Ox-CNTs. (Cdl=Slope 2×Area )