Electronic Supplementary Material

Fluorine-free superhydrophobic PDMS-coated silica particles for oil-water separation and liquid marbles

Swithin Hanosha, Unnikrishnan V. Kb, Sajan D. Georgea*

* Corresponding Author E-mail:  sajan.george@manipal.edu

a Centre for Applied Nanosicence, Department of Atomic and Molecular Physics, Manipal Academy of Higher Education, Manipal 576104, India.

b Department of Atomic and Molecular Physics,  Manipal Academy of Higher Education, Manipal 576104, India.

The oleophilic behavior of the hydrophobic cotton fabric can be seen from figure S1 as various oils (n-decane, n-hexane, and chloroform completely wets the fabric and make contact angle 0 º.

Figure S1: Spreading of various oils over the hydrophobic fabric.

A home-made set-up as shown in figure S2 was used for oil-water separation.  After 50 cycles of oil-water separation the hydrophobic cotton fabric exhibited remarkable stability as the water contact angle remained same 143 º (figure S3).

Figure S2: Homemade set-up for oil-water separation.

Figure S3: WCA of fabric at ~ 145 º after 50 cycles of oil-water separation followed by cleaning with ethanol.

Liquid marble could be prepared with various viscosity liquids from water, milk, glycerol, and ketchup (figure S4).

Figure S4: Liquid marble with different viscosity solutions.

Movies

Movie V1: 10 µl Liquid marble dropped from a height of 3 cm.

Movie V2: 5 µl Liquid marble dropped from a height of 4 cm.

Movie V3: Liquid marble formation with water.

Movie V4: Liquid marble formation with milk.

Movie V5: Liquid marble formation with glycerol.

Movie V6: Liquid marble formation with ketchup.