Crystallization behavior and thermal properties of octa phenyl-substituted silsesquioxane-modified polylactide (PLA)

Supplementary information

Table. S1. Parameters of linear fitting of spherulite growth curves.

| Material / temp. of isotherm | Function | R2 |
| --- | --- | --- |
| PLA/135 | y=3.9167x-2.8951 | 0.9997 |
| 0.5 wt% phSQ/135 | y=2.4722x-4.5359 | 0.9988 |
| 1 wt% phSQ/135 | y=3.7446x-1.0088 | 0.9989 |
| 2 wt% phSQ/135 | y=3.7437x-1.5036 | 0.9877 |
| 5 wt% phSQ/135 | y=4.1702x-1.4307 | 0.9978 |
| PLA/140 | y=3.335x-6.1504 | 0.9999 |
| 0.5 wt% phSQ/140 | y=2.1945x-3.4577 | 0.9991 |
| 1 wt% phSQ/140 | y=3.4317x-6.7600 | 0.9999 |
| 2 wt% phSQ/140 | y=4.3682x-6.4548 | 0.9995 |
| 5 wt% phSQ/140 | y=3.8652x-13.3250 | 0.9994 |