Supplementary File

Laser Induced Graphene electrode-based supercapacitors: Insight on the influence of aqueous electrolytes on its energy storage potential
Jadan Resnik Jaleel UC1, Somashekara Bhat2*, Sudhakar Y N1, Ankitha Rao2,Vipin Cyriac3, Shounak De2

1Department of Chemistry, Manipal Institute of Technology, Manipal Academy of Higher Education, Manipal, Karnataka, India

2Department of Electronics and Communication Engineering, Manipal Institute of Technology, Manipal Academy of Higher Education, Manipal, Karnataka, India.

3Department of Physics, Manipal Institute of Technology, Manipal Academy of Higher Education, Manipal, Karnataka, India

*Corresponding author: E-mail address: soma.bhat@manipal.edu (Somashekara Bhat)

Figure S1. CV of supercapacitors prepared using various laser parameters as part of the optimization study

Figure S2. GCD curves at a current density of 0.1 mAcm-2 for supercapacitors prepared using various laser parameters as part of the optimization study.

Figure S3. Nyquist plots obtained from EIS for LIG electrodes fabricated under different laser power and speed conditions. The spectrum of the best-performing electrode is shown in the inset.

Figure S4. EDS Spectrum Showing Elemental Composition of LIG

Table S1. Laser Speeds and Powers used in obtaining the LIG

|  |  | Laser Power (W) |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | 35 | 40 | 45 | 50 | 55 |
| Lasing Speed (mm s-1) | 175 | i | ii |  |  |  |
|  | 180 | iii | iv | v | vi |  |
|  | 185 |  | vii | viii | ix |  |
|  | 190 |  | x | xi | xii | xiii |
|  | 195 |  |  |  | xiv | xv |

Table S2. Calculated areal capacitance of LIG prepared using different laser parameters, based on GCD curves at a current density of 0.1 mAcm-2

| Areal Capacitance (mF cm-2) |  | Laser Power (W) |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | 35 | 40 | 45 | 50 | 55 |
| Lasing speed (mm s-1) | 175 | 17 | 30 | *** | *** | *** |
|  | 180 | 24 | 34 | 20 | 24 | *** |
|  | 185 | ** | 14 | 26 | 09 | *** |
|  | 190 | ** | 9 | 25 | 30 | 29 |
|  | 195 | ** | ** | ** | 19 | 20 |

**The LIG is not formed due to underexposure *** The PI sheet melted due to overexposure

Table S3. Summary of surface parameters from various plots

| Plots | Surface Area (m2 g-1) | Total Pore Volume (cm3 g-1) | Average Pore Diameter (nm) |
| --- | --- | --- | --- |
| BET | 25.15 | 5.77 | 13.74 |
| Langmuir | 207.19 | 47.60 | ** |
| BJH | ** | ** | 1104.70 |
| MP | ** | ** | 2.37 |

Table S4. Elemental Composition of LIG from EDS Analysis

| Element | Weight% | Atomic% |
| --- | --- | --- |
| Carbon | 95.14 | 96.31 |
| Oxygen | 4.86 | 3.69 |
| Totals | 100.00 |  |

Table S5. Areal Capacitance of LIG Electrodes at

Different Scan Rates (Three-Electrode System)

| Scan rate (mVs-1) | Areal capacitance (mFcm-2) |
| --- | --- |
| 100 | 2.30 |
| 75 | 5.40 |
| 50 | 7.80 |
| 25 | 11.00 |
| 10 | 15.90 |
| 5 | 17.40 |