Utilising design of experiment to design an optimised bioink for 3D-bioprinting  -

Supplementary Information

Table S1 - Factorial DoE Sample Running Order

Sample running order and sample component combinations (w/v%) outputs generated by the factorial DoE (which did not include Phenol Free DMEM as a factor).

| Sample Number | Sample Concentration (w/v %) |  |  |
| --- | --- | --- | --- |
|  | Hyaluronic Acid | Sodium Alginate | Dextran-40 |
| 1 | 2.00 | 5.00 | 0.50 |
| 2 | 2.00 | 5.00 | 2.00 |
| 3 | 0.50 | 5.00 | 0.50 |
| 4 | 2.00 | 0.50 | 0.50 |
| 5 | 0.50 | 0.50 | 2.00 |
| 6 | 0.50 | 0.50 | 0.50 |
| 7 | 1.25 | 2.75 | 1.25 |
| 8 | 0.50 | 5.00 | 2.00 |
| 9 | 2.00 | 0.50 | 2.00 |

Table S2 - Mixture DoE Sample Running Order

Sample running order and sample component combinations (w/v%) outputs generated by the Mixture DoE (which included Phenol Free DMEM as a factor).

| Sample No. | Sample Concentration (w/v %) |  |  |  |
| --- | --- | --- | --- | --- |
|  | Hyaluronic Acid | Sodium Alginate | Dextran-40 | Phenol Free DMEM Culture Media |
| 1 | 0.500 | 0.500 | 2.000 | 97.000 |
| 2 | 2.000 | 0.500 | 2.000 | 95.500 |
| 3 | 2.000 | 2.750 | 2.000 | 93.250 |
| 4 | 0.500 | 2.750 | 1.250 | 95.500 |
| 5 | 0.875 | 1.625 | 1.625 | 95.875 |
| 6 | 0.500 | 2.750 | 2.000 | 94.750 |
| 7 | 0.875 | 3.875 | 1.625 | 93.625 |
| 8 | 2.000 | 2.750 | 1.250 | 94.000 |
| 9 | 2.000 | 5.000 | 1.250 | 91.750 |
| 10 | 2.000 | 0.500 | 1.250 | 96.250 |
| 11 | 1.250 | 5.000 | 0.500 | 93.250 |
| 12 | 0.875 | 1.625 | 0.875 | 96.625 |
| 13 | 1.250 | 0.500 | 2.000 | 96.250 |
| 14 | 1.625 | 3.875 | 1.625 | 92.875 |
| 15 | 1.250 | 2.750 | 2.000 | 94.000 |
| 16 | 0.875 | 3.875 | 0.875 | 94.375 |
| 17 | 1.250 | 0.500 | 0.500 | 97.750 |
| 18 | 0.500 | 5.000 | 0.500 | 94.000 |
| 19 | 0.500 | 0.500 | 0.500 | 98.500 |
| 20 | 2.000 | 5.000 | 0.500 | 92.500 |
| 21 | 1.250 | 5.000 | 1.250 | 92.500 |
| 22 | 1.250 | 5.000 | 2.000 | 91.75 |
| 23 | 0.500 | 5.000 | 2.000 | 92.5 |
| 24 | 1.250 | 0.500 | 1.250 | 97 |
| 25 | 1.625 | 1.625 | 0.875 | 95.875 |
| 26 | 0.500 | 5.00 | 1.250 | 93.25 |
| 27 | 1.250 | 2.750 | 1.250 | 94.75 |
| 28 | 1.625 | 3.875 | 0.875 | 93.625 |
| 29 | 2.000 | 0.500 | 0.500 | 97.000 |
| 30 | 0.500 | 2.750 | 0.500 | 96.250 |
| 31 | 2.000 | 5.000 | 2.000 | 91.000 |
| 32 | 2.000 | 2.750 | 0.500 | 94.750 |
| 33 | 1.625 | 1.625 | 1.625 | 95.125 |
| 34 | 1.250 | 2.750 | 0.500 | 95.500 |
| 35 | 0.500 | 0.500 | 1.250 | 97.750 |