Supplementary information

### Review: Cobalt-Nanoparticles as Bioactive and Sustainable Species - Development, Environmental Risk assessment, and Future Prospects

Olena Tsyganovych1, Olena Goncharuk1,2, Konrad Terpiłowski3, Vitalii Prokopenko1, Ganna Yanovska2,4, Katarzyna Szewczuk-Karpisz2*

1F.D. Ovcharenko Institute of Biocolloidal Chemistry, NAS of Ukraine, 42 Vernadskogo Blvd., 03142 Kyiv, Ukraine;

2Institute of Agrophysics, Polish Academy of Sciences, Doświadczalna 4, 20-290 Lublin, Poland;

3Maria Curie-Sklodowska University, M.C. Sklodowska Sq.3, 20-031  Lublin, Poland;

4Theoretical and Applied Chemistry Department, Sumy State University,116, Kharkivska st., 40007 Sumy, Ukraine.

*corresponding author:k.szewczuk-karpisz@ipan.lublin.pl

Table S1. Reaction conditions of chemical reduction for the Co-NPs synthesis

| Crystalline Structure | Particle Size | Reducing Agent | Cobalt Precursor | Stabilizers/Conditions | Ref. |
| --- | --- | --- | --- | --- | --- |
| Mixture of hcp and fcc Co phases | 30-70 nm | Hydrazine hydrate | Cobalt sulfate | NaOH concentration 0.5-2.5 M; precursor concentration influences size; ratio Co:N₂H₄ = 1:16; 70 °C; pH ~13 | Alex et al., 2011 |
| 83% hcp, 17% fcc Co | 30 nm (thickness) | Hydrazine hydrate | Cobalt(II) chloride | Strong alkaline medium; pH ~13; 70 °C; nanoplates with hcp/fcc content ratio tuned by synthesis conditions | Khusnuriyalova et al., 2021 |
| Face-centered cubic (fcc) Co | 5 nm | Sodium borohydride (NaBH₄) | Cobalt(II) chloride | Ethanol solvent; mineral oil layer; annealing at 600 °C; no Co–B alloy detected | Zhao et al., 2003 |
| ε-Co metallic cobalt (interplanar distances in the HRTEM images were 2.17 Å) | 6.2-7.2 nm (monospherical); 3.64 ± 0.64 nm | 1,2-Dodecanediol, NaBH4 | Cobalt acetate; cobalt carbonyl | (i) Oleic acid (OA) and trioctylphosphine (TOP) stabilizers; reaction at 250 °C in N₂ atmosphere; (ii) heating cobalt carbonyl in TOP under vacuum with 1,2-dichlorobenzene (DCB), varying amounts of OA at 180 °C; (iii) addition of a mixture of NaBH4 and ethanol to a solution of cobalt acetate, ethanol and oleic acid in a drop-like manner, at room temperature | Glavee et al., 1993; Zola et al., 2014; Rotstein et al., 2002; Puntes et al., 2001 |
| Amorphous | 4.5-9.4 nm | Sodium borohydride (NaBH₄) | Cobalt(II) chloride | Trimesyl core dendrimer matrix; size decreases with increasing dendrimer generation (G3.0 to G6.0); hydrodynamic interaction influences morphology | Wu et al., 2010 |
| εCo (soft magnetic material) | 2-11 nm | Dioctylether solution of superhydride (LiBEt3H) | Cobalt(II) chloride | oleic acid, trialkylphosphines, 200 °C | Sun et al., 1999 |
| Spherical metallic Co-NPs | 80-100 nm | Sodium borohydride (NaBH₄) | CoSO4 | tetrabutyl ammonium bromide (TBAB) as stabilizer; at room temperature | Mondal et al., 2015 |
| Co(OH)₂ and Co₃O₄ phases | 20-40 nm | - | Cobalt sulfate | Histidine (0.1-0.3 mg/ml); water-ethanol solvent; rhombohedral Co(OH)₂ transitioned to Co₃O₄ with increasing histidine concentration and ethanol. | Zhao et al., 2012 |
| Co-NPs spherical nanocrystals of metallic cobalt | diameter of crystallites 8 and 5 nm with stabilizers, and 3-60 without stabilizers | 1,2-hexadecandiol | Cobalt acetate tetrahydrate Co(CH3COO)2·4H2O | Oleic and lauric acids as stabilizers; 0.013 mmol of platinum(II) acetylacetonate) was added to attain heterogeneous nucleation; 300 °C under stirring and refluxing in a nitrogen atmosphere, within 10 min | Luna et al., 2003 |
| hexagonal close-packed (hcp) Cobalt NCs structure, with a fraction containing face-centered cubic (fcc) characteristics | 6-8 nm when TOP was used and 10-13 nm when TBP was used | 1,2-diols | cobalt acetate tetrahydrate Co(CH3COO)2·4H2O | Oleic acid, trioctylphosphine (TOP), and tributylphosphine (TBP) due to the ratio of strongly and weakly binding surfactants controls nanoparticle size and serve as stabilizer | Murray et al., 2001 |
| hcp ε-Co | 400 nm | Hydrazine hydrate | Cobalt (II) sulfate | Citric acid stabilizer; varying hydrazine concentration affects morphology; room temperature synthesis resulted in spherical particles. | Smyrnioti et al., 2017 |
| Zerovalent metal Co NPs | 20-60 nm | NaBH4 | CoSO4· 7H2O | carboxymethyl cellulose (CMC) as stabilizer; room temperature synthesis | Ngo et al., 2014 |

Table S2. Reaction conditions of sol-gel method for the Co-NPs synthesis

| Crystalline Structure | Particle Size | Precursor | Stabilizers/Synthesis Conditions | Reference |
| --- | --- | --- | --- | --- |
| Co₃O₄ | 60-85 nm | Cobalt nitrate hexahydrate in ethylene glycol (1:3) | Sintering at 700 °C for 1-3 h, optimized at 2 h | Sardjono et al., 2020 |
| Co₃O₄ (fcc structure, lattice constant a = 8.09 Å, space group Fd-3m) | 67 nm (500 °C); 80 nm (550 °C) | Metal salt (type unspecified) | Tetrahydrofuran, 25% ammonia solution; calcination at 500-550 °C. | Jagtap et al., 2017 |
| CoO, Co₃O₄ | ~85 nm | Cobalt nitrate or cobalt chloride | Sol-gel synthesis in 1-propanol and ethyl acetate with surfactants (PDMS, Triton X-100, NaDS, etc.); pH and precursor concentration adjusted. | Sinko et al., 2011 |
| CoFe₂O₄ (spinel structure; FTIR peaks at 460-603 cm⁻¹) confirms Co-O and Fe-O bonds. | 100-220 nm | Cobalt (II) acetate tetrahydrate and iron (III) nitrate | Methoxyethanol and diethanolamine; boiled at 125 °C for 24 h, centrifuged at 5000 rpm | Saragi et al., 2015 |

Table S3. Reaction conditions of thermal decomposition method for the Co-NPs synthesis

| Crystalline Structure | Particle Size | Precursor | Stabilizers/Synthesis Conditions | Reference |
| --- | --- | --- | --- | --- |
| Multiply twinned fcc (mt-fcc) | 8-10 nm | Cobalt octacarbonyl (Co₂(CO)₈) | Dioctyl ether solvent, oleic acid and tributylphosphine as stabilizers, heated to 200 °C under N₂ stream, slow solvent evaporation to achieve ordered superlattices | Murray et al., 2001; Blums et al., 1996 |
| fcc Co, protected by amorphous matrix | 12-15 nm | Cobalt acrylamide complex | Thermolysis at 873–1073 K after frontal polymerization; amorphous matrix prevents oxidation; coercivity depends on temperature | Sówka et al., 2006 |
| ε-Co (cubic structure) | 3-17 nm | Cobalt octacarbonyl (Co₂(CO)₈) | Mixture of oleic, lauric, and trioctylphosphonic acids as surfactants; rapid pyrolysis in an inert atmosphere; size controlled by precursor/surfactant ratio, temperature, and injection time | Puntes et al., 2001 |
| fcc Co; hcp + fcc mixture | 13.9 nm; 86.0 nm (triangular prisms) | Cobalt acetate | Dissolved in 2-pyrrolidinone with trioctylphosphine (TOP), oleylamine, and oleic acid; reaction at 260 °C for 90 min under N₂ stream. Addition of 1,2-dodecanediol as reducing agent, heated in the presence of surfactants. Higher coercive force observed but less suitable for high-density magnetic applications compared to smaller particles | Lu et al., 2015 |
| Pure cubic Co | 25-35 nm | Bis(salicylidene) cobalt(II) | Oleylamine and triphenylphosphine (TPP) as stabilizers; dry argon atmosphere at 100 °C for 90 min; high yield (70%) with uniform size distribution | Salavati-Niasari et al., 2008 |

Table S4. Reaction conditions of the ‘green synthesis’ methods for Co-NPs synthesis

| Crystalline Structure | Particle Size | Plant Extract | Precursor (Cobalt Compound) | Stabilizers/Conditions | Ref. |
| --- | --- | --- | --- | --- | --- |
| Co₃O₄ (Cubic Spinel) | 20-80 nm | Azadirachta indica leaves | Cobalt nitrate | Large content of flavonoids; reaction at ambient temperature | Singh et al., 2024 |
| Co₃O₄ | 60-85 nm | Spent coffee extract (SCE) | Cobalt nitrate | pH-neutral to alkaline; annealing at 75 °C increased particle yield; lower temperatures reduced particle size | Drummer et al., 2024 |
| Co₃O₄ | 34.9 nm | Hibiscus rosa-sinensis flowers | Cobalt nitrate | Neutral pH; functional groups capped NPs; antimicrobial properties against Xanthomonas oryzae | Govindasamy et al., 2021 |
| Co₃O₄ (Cubic Spinel) | 26 nm | Curcuma longa (Turmeric) | Cobalt nitrate | pH 7-10; enhanced crystallinity due to annealing at 100 °C; antibacterial and photocatalytic dye degradation activity | Ryntathiang et al., 2024 |
| Co₃O₄ | 21.7-77.5 nm | Piper nigrum (Black Pepper) | Cobalt nitrate | Calcination at 100-900 °C; increasing temperature reduced antibacterial activity but increased crystallinity | Chelliah et al., 2023 |
| Co and Co-Zn BMNPs; Spherical morphology; Co/Zn BMNPs | 22.77 nm (Co), 14.8 nm | Cymbopogan citratus (Lemongrass) | Cobalt chloride | SEM images showed spherical cluster-shaped monometallic and bimetallic NPs, which is explained by their polymeric nature. EDX analysis of bimetallic NPs confirmed that the sample was enriched in cobalt (69.94%) compared to zinc (30.06%). | Haq et al., 2021 |
| Co₃O₄ | 20-30 nm | Allium sativum and Allium cepa husk | Cobalt nitrate | pH 6-7; zeta potential ~-20.4 mV; effective antimicrobial activity against E. coli, Proteus, S. aureus, Klebsiella pneumonia | Riaz et al., 20221 |
| Co₃O₄ | 21-72 nm | Celery stem and green tea leaves | Cobalt nitrate | pH 14; strong antimicrobial activity against GNB and GPB | Ali et al., 2023 |
| Co₃O₄ (Cubic Spinel) | 31.3-68.9 nm | Aerva javanica plant extracts | Cobalt chloride | Aqueous and methanolic extracts showed varying sizes; methanol extracts produced smaller particles; antibacterial activity varied based on reducing agent source | Najrul Islam et al., 2013 |
| Co (fcc) | 21 nm | Periconia prolifica culture extract | Cobalt chloride | Stabilization by proteins; FTIR confirmed functional group capping; effective antibacterial activity due to Co²⁺ ion release on bacterial membranes | Mubraiz et al., 2021 |

Table S5. Optimal combinations of methods for comprehensive characterization of Co-NP

| Property | Primary Method(s) | Complementary Method(s) | Reference |
| --- | --- | --- | --- |
| Crystalline Structure | XRD | TEM | Khusnuriyalova et al., 2021; Lisiecki et al., 2003; Zhao et al., 2012; Smyrnioti et al., 2017; Sardjono et al., 2020; Kumar et al., 2017; Saragi et al., 2015; Lu et al., 2015; Salavati-Niasari et al., 2008; Govindasamy et al., 2021; Ryntathiang et al., 2024; Haq et al., 2021; Ali et al., 2023; Najrul Islam et al., 2020; Fultz et al., 2012; Abu-Abdeen et al., 2020; Zhludenko et al., 2018; Ischenko et al., 2008; Pryhunova et al., 2023; Dyachenko et al., 2024 |
| Particle Size and Shape | TEM, SEM | DLS | Zola et al., 2014; Zhao et al., 2012; Luna et al., 2003; Sówka et al., 2006; Puntes et al., 2002; Lu et al., 2015; Fultz et al., 2012; (TEM), Puntes et al., 2001; Kumar et al., 2015; Zhludenko et al., 2018; Pryhunova et al., 2023; Dyachenko et al., 2024 (SEM); Riaz et al., 2022 (DLS) |
| Surface Chemistry | FTIR, XPS | EDX | Mondal et al., 2015; Lu et al., 2015; Govindasamy et al., 2021; Ogunyemi et al., 2023; Ryntathiang et al., 2024; Fultz et al., 2012; Almeida Junior et al., 2024 (FTIR), Khusnuriyalova et al., 2021; Pryhunova et al., 2023; Dyachenko et al., 2024 (XPS); Sardjono et al., 2020; Dyachenko et al., 2024 (EDX) Kamal et al., 2017; Kumar et al., 2017. |
| Elemental Composition | EDX | XPS | Sardjono et al., 2020; Dyachenko et al., 2024 (EDX), Pryhunova et al., 2023; Dyachenko et al., 2024 (XPS) |
| Magnetic Properties | VSM | XRD (for phase identification) | Klabunde et al., 1996; Giri et al., 2002; Saragi et al., 2015 |
| Colloidal Stability | DLS | Zeta Potential Measurement | Velmani et al., 2025 |

Table S6. Biologically active properties of Co-NPs relative to plants

| Crystalline Structure & Size | Plant | Comments | Reference |
| --- | --- | --- | --- |
| Co (Metallic), 20-60 nm | Soybean (Glycine max) | Stimulated seed germination, increased seedling growth by 2.4x, enhanced chlorophyll content (by 7-15%), and increased yield by up to 16%. | Ngo et al., 2014 |
| Co₃O₄, 34.9 nm | Rice (Oryza sativa) | Reduced bacterial leaf blight by 79%, improved plant growth (shoot length, fresh and dry weight), and enhanced photosynthetic efficiency. | Govindasamy et al., 2022 |
| Spherical Co₃O₄ NPs, 50 nm | Brassica napus L. (canola) | Low concentrations (50-100 mg/L) stimulated shoot growth and chlorophyll content; high concentrations (4 g/L) revealed phytotoxicity, increasing oxidative stress and reducing membrane stability | Janmohammadi et al., 2017 |
| Co₃O₄ NPs, various sizes | Brassica napus L. (canola) | Low concentrations improved growth and chlorophyll levels; high concentrations (>0.5 g/L) induced oxidative stress and reduced glutathione levels | Jahani et al., 2019 |
| CoFe₂O₄ NPs | Solanum lycopersicum (tomato) | Increased Fe and Co contents in plant tissues; plants tolerated concentrations up to 1000 mg/L without toxicity symptoms | Jahani, 2020 |
| Co₃O₄ NPs, 25 nm, hexagonal wurtzite | Acacia jacquemontii and Acacia nilotica | Counteracted zinc toxicity, improving root/shoot growth, biomass, and physiological parameters | Mahmood et al., 2023 |
| Zero-valence Co NPs, 30-70 nm | Zea mays (corn) | Reduced germination rate, selective impact on different growth stages, enhanced anthocyanin content | He et al., 2017 |
| Cobalt sulfate (CoSO₄) | Cucumis sativus (cucumber) | Stimulated growth and yield at 10-20 mg/L in saline soils | Shrivastava et al., 2015 |
| Cobalt (various forms) | Allium cepa (onion) | Improved growth and yield under salt stress at 12.5 mg/L; higher concentrations reduced effect | Gad et al., 2018 |
| Cobalt (various forms) | Solanum lycopersicum (tomato) | 7.5 mg/L cobalt enhanced growth, yield, and fruit quality | Gad et al., 2020 |
| Cobalt in organic fertilizer | Vigna unguiculata (cowpea) | Increased legume yield by 30% | Gad et al., 2005 |
| Cobalt (various forms) | Solanum lycopersicum (tomato) | 7.5 mg/L cobalt enhanced growth, yield, and fruit quality | Gad et al., 2020 |

Table S7. Antimicrobial properties of Co-NPs

| Crystalline Structure & Size | Synthesis Method | Microorganism Culture | Comments | Reference |
| --- | --- | --- | --- | --- |
| Co₃O₄ (Cubic Spinel), 20-80 nm | Green synthesis (Azadirachta indica leaves) | C. albicans, A. niger | Effective against fungal pathogens, useful for treating local human fungal infections. | Singh et al., 2024 |
| Co₃O₄, 34.9 nm | Green synthesis (Hibiscus rosa-sinensis flower extract) | X. oryzae | Inhibited biofilm formation by 79%; reduced rice leaf infection. Increased plant growth metrics (shoot length, weight, etc.). | Govindasamy et al., 2021 |
| Co₃O₄ (Cubic Spinel), 26 nm | Green synthesis (Curcuma longa extract) | S. aureus, E. coli | Strong antibacterial and dye degradation activity. Medicinal properties of extract enhance particle stability. | Ryntathiang et al., 2024 |
| Co₃O₄, 21.7-77.5 nm | Green synthesis (Piper nigrum leaf extract) | E. coli, S. aureus | Calcination affected activity; lower calcination temperatures showed better antibacterial effects. | Chelliah et al., 2023 |
| Co and Co-Zn BMNPs, 22.8-14.8 nm | Green synthesis (Cymbopogan citratus extract) | S. aureus, E.coli | Superior antibacterial properties due to large surface area and ROS generation, and bacterial membrane disruption. | Haq et al., 2021 |
| Co₃O₄, 20-30 nm | Combined synthesis (Allium sativum and Allium cepa husk extract) | E. coli, Proteus, S. aureus, K. pneumonia | Large activity due to increased surface oxide ions, disrupting bacterial membranes. | Riaz et al., 2022 |
| Co₃O₄, 21-72 nm | Green synthesis (Celery and green tea extracts) | P. aeruginosa, S. aureus | Strong antibacterial effects due to size and high surface-to-volume ratio. | Ali et al., 2023 |
| Co₃O₄, 31.3-68.9 nm | Green synthesis (Aerva javanica methanol extract) | B. subtilis, P. aeruginosa, S. aureus | Smaller particles from methanol extracts/microbial synthesis showed stronger antibacterial activity. | Najrul Islam et al., 2020 |
| Co (Face-centered cubic), 21 nm | Microbial synthesis (Periconia prolifica extract) | E. coli, S. aureus | Release of Co2⁺ ions disrupted bacterial membranes; effective against drug-resistant strains like MRSA. | Mubraiz et al., 2021 |
| Co-NPs, spherical shape, 54-125 nm | Green synthesis (biosynthesis) | Not specified; reported as potential antibacterial agents | Spherical NPs synthesized via a green route, demonstrating potential antibacterial activity. | Slavin et al., 2017 |
| Co₃O₄ NPs, cobalt oxide (size not specified) | Green synthesis (biosynthesis using leaf extract) | B. licheniformis, K. pneumoniae, B. subtilis, E. coli | An increase in the concentration of Co₃O₄ NPs enhances antibacterial activity. | Ribeiro et al., 2022; Razavi et al., 2020 |
| Co₃O₄ NPs, size < 100 nm | Chemical precipitation (according to Arsalan et al.) | S. aureus, E. coli | Co₃O₄ NPs alter the outer membrane of GPB via the release of Co-ions, which disrupt membrane integrity. | Christy et al., 2015 |
| Co₃O₄ nanograins, Co₃(PO₄)₂ microflakes, and Co(OH)₂ nanoflakes | Chemical synthesis under specific conditions forming distinct morphologies | Acanthamoeba | Amoebicidal, encystation, excystation, and host cell cytopathogenic studies. The results indicate potential antiamoebic effects, suggesting these NPs could be developed for antiamoebic nanomedicine. | Safaei et al., 2019; Arsalan et al., 2020 |
| CoFe₂O₄ NPs (ferrite phase; size not specified) | Chemical synthesis (as described by Rashmi et al.) | GPB and GNB | The antimicrobial mechanism involves generation of reactive oxygen species (ROS) such as hydroxyl radicals and superoxide anions, inducing oxidative stress, membrane rupture, cytoplasmic leakage, and ultimately cell death. GNB are more susceptible due to differences in the cell wall composition. | Anupong et al., 2023; Anwar et al., 2019; Sulaiman et al., 2021; Sharma et al., 2019 |
| Mixed nanocomposite (NC): Zn₀.75Co₀.25Fe₂O₄ | Synthesis as a mixed NC | S. aureus, E. columbae, A. viridians | The most efficient NC composition (20.0 ppm) exhibits the best antibacterial activity among the tested formulations. | Tamboli et al., 2023 |
| Co-oxide NPs (cobalt oxide form; exact size not specified) | Synthesis according to Raza et al. | E. coli, P. aeruginosa, B. subtilis | Higher concentrations of the NPs result in improved antibacterial performance. | Chandekar et al., 2021 |
| Co3O4 NPs, 50 nm | Sol-gel | S.aureus, E. coli, P. aeruginosa | Caused a significant antibacterial effect on both GPB and GNB strains. The most antibacterial effect was observed on S. aureus and E. coli, referring to more changes in the outer membrane of GPB in the presence of Co2+ ions. | Maksoud et al., 2019 |
| Co-NPs, 50-100 nm | Sigma Aldrich | - coli | Possible mechanisms: (i) increased lipophilicity of the metal enhances its interactions with bacterial membranes; (ii) metal positive charge interacts with ligand atoms, leading to π-electron delocalization; (iii) factors like dipole moment, conductivity, and solubility influence metal ion activity. | Raza et al., 2016 |
| Co-NPs, cubic spinel phase, 50-55 nm | - | S. aureus, Proteus spp., E. coli | Can help kill multidrug-resistant (MDR) bacteria and be suitable for treating disease; effective for both GPB and GNB. The optimum concentration of Co-NPs was 100 μg/ml | Arsalan et al., 2020 |

Fig. S1. Bactericidal properties of Co-NPs.