Microstructure evolution, dielectric response, and conduction mechanism of La1-xYxFeO3, (0<x<0.3) annealed perovskites synthesized via a sol-gel combustion technique

Ahmed H. Ibrahim a,*, S. Mosaad a, E. Elesh b

a Materials Science Laboratory, Department of Physics, Faculty of Science, Suez Canal University, 41511, Ismailia, Egypt.

b Department of Physics, Faculty of Science, 41522, Port Said University, Egypt.

Supplementary material

- Results and discussion

  - Structural characteristics

The Rietveld profile fitting of the La1-xYxFeO3, (x= 0.05, 0.10, 0.15, 0.25, and 0.30) perovskite are presented in Fig. S1(a–e) (Supplementary materials). The background parameters were refined using a Fourier series and a polynomial function with six coefficients. A pseudo-Voigt function was used to refine the shape of the diffraction peak. This function combines the Gaussian and Lorentzian functions. It is frequently used in the study of diffraction peaks to understand how their broadening is affected by factors such as size and microstrain. Refining background parameters was first carried out, followed by many rounds to improve peak positions and correct zero-shift correction. Consequently, refinement was carried out on the structural and microstructural parameters, including the unit cell parameters, position parameters, occupancy, scale factor, and structure factor.

Fig. S1(a–e) Rietveld refinement profile of XRD of as prepared (a) LFOY05, (b) LFOY10, (c) LFOY15, (d) LFOY25, and (e) LFOY30. The black line represents the observed patterns, the red points represent the calculated patterns, the green vertical line represents the position of Bragg reflections, and the violet line represents the difference between observed and calculated intensities.

The data presented in Table S1 reveal that the structural and fitting parameters were accurately determined, thus ensuring high-quality fittings. The goodness of fit parameter, represented by χ2, was less than 2, indicating a highly accurate fitting of the experimental diffraction profile as illustrated in Table S1.

The size-strain plots (SSP) for the other perovskite compositions are illustrated in Fig. S2(a–e) (Supplementary materials). The slopes and intercepts were calculated using linear fitting of the experimental data points. The mean crystalline size values were acquired directly from the slope values, while the lattice strain values were produced by calculating the square root of the intercepts.

Table S1 Structural parameters [the lattice parameters (a, b, c), the unit cell volume (V), the particle size (DXRD), non-uniform microstrain (ε), and Rietveld refinement parameters], of L1-xYxFeO3 ceramics.

| Sample code | Composition | Lattice parameter |  |  |  |  |  |  | Refinement parameters |  |  |  | Tolerance factor (t) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | a (Å) | b (Å) | c (Å) | V(Å) | D (nm) | ε (×10-3) |  | Rwp | RP | RF (%) | χ2 |  |
| LFO | LaFeO3 | 5.5445 | 7.8339 | 5.5534 | 241.21 | 15.6 ±0.01 | 6.0 ±0.001 |  | 27.8 | 26.2 | 2.75 | 1.10 | 0.945 |
| LFOY05 | La0.95Y0.05FeO3 | 5.5552 | 7.8287 | 5.5427 | 241.05 | 13.4 ±0.01 | 4.0 ±0.001 |  | 28.5 | 26.0 | 5.51 | 1.02 | 0.944 |
| LFOY10 | La0.90Y0.10FeO3 | 5.5608 | 7.8324 | 5.5328 | 240.98 | 18.5 ±0.02 | 7.8 ±1.000 |  | 27.3 | 24.8 | 5.02 | 1.10 | 0.941 |
| LFOY15 | La0.85Y0.15FeO3 | 5.5666 | 7.8220 | 5.5291 | 240.75 | 12.6 ±0.01 | 8.5 ±0.002 |  | 28.7 | 26.9 | 5.45 | 1.10 | 0.938 |
| LFOY25 | La0.75Y0.25FeO3 | 5.5753 | 7.8113 | 5.5029 | 239.65 | 16.2 ±0.01 | 6.8 ±1.200 |  | 34.0 | 34.0 | 5.23 | 1.03 | 0.933 |
| LFOY30 | La0.70Y0.30FeO3 | 5.5766 | 7.8101 | 5.4896 | 239.09 | 11.9 ±0.01 | 7.3 ± 1.700 |  | 36.9 | 37.9 | 8.11 | 1.11 | 0.931 |

Fig. S2 The calculation of crystallite size and lattice strain using size–strain plots (SSP) for perovskites (a) LFOY05, (b) LFOY10, (c) LFOY15, (d) LFOY25, and (e) LFOY30.