MXene/rGO/sulfur loaded separator based current collector-free lithium sulfur batteries with high sulfur loading and cycle life

K. Sandeep Rao,1,2 Dipa Dutta Pathak*,1 Balaji P Mandal*,1,2 and A. K. Tyagi*1,2

1Chemistry Division, Bhabha Atomic Research Center, Mumbai – 400085, India

2Homi Bhabha National Institute, Anushaktinagar, Mumbai – 400094, India

*Corresponding Authors:

bpmandal@barc.gov.in (BPM), drdipa01@gmail.com (DDP), aktyagi@barc.gov.in (AKT)

Phone: +91-22-25592201

# Supporting Information

Synthesis

Synthesis of Mxene/S (MS) composite

15 mg of Mxene was dispersed in 100 mL distilled water by ultra-sonication till a uniform suspension was formed. Thereafter the same procedure as above for MGS was followed.

Synthesis of rGO/S (GS) composite

15 mg of rGO was dispersed in 100 mL distilled water by ultra-sonication till a uniform suspension was formed. Thereafter the same procedure as above for MGS was followed.

Calculation of active mass of sulfur

Weight of each 12 mm microfiber disc with MGS coating = 21.35 mg

Weight loss fraction attributed to S8 (from TG) = 17 wt %

Hence, weight of S8 on each coated disc = 0.17 * 21.35  = 3.63 mg

Figure S1. Digital photographs of (a) Li anode facing separator (b) separator facing anode.