Supplementary Information

MoSe2 nanosheets-based electrochemical sensor for simultaneous determination of ascorbic acid, dopamine and uric acid

Deniz Coban1, Yasin Tangal2, Sadik Cogal3

1Burdur Mehmet Akif Ersoy University, The Graduate School of Natural and Applied Sciences, Department of Material Technology Engineering, 15030, Burdur, Turkey

2Burdur Mehmet Akif Ersoy University, The Graduate School of Natural and Applied Sciences, Department of Chemistry, 15030, Burdur, Turkey

3Burdur Mehmet Akif Ersoy University, Faculty of Arts and Science, Department of Chemistry, 15030, Burdur, Turkey

Figure S1. Cyclic voltammograms (CVs) of various GCE-MoSe2 electrodes in 0.1 M KCl containing 5 mM [Fe(CN)6]3-/4-

Figure S2. Cyclic voltammograms (CVs) of various GCE-MoSe2 electrodes in PBS solution containing 1.13 mM ascorbic acid (AA), 0.19 mM dopamine (DA), and 0.38 mM uric acid (UA)

Figure S3. Differential pulse voltammograms (DPVs) of various GCE-MoSe2 electrodes in PBS solution containing 1.13 mM ascorbic acid (AA), 0.19 mM dopamine (DA), and 0.38 mM uric acid (UA)

Table S1. Comparison of various electrodes for electrochemical determination of ascorbic acid (AA), dopamine (DA), and uric acid (UA)

| Electrode | Linear range (µM) |  |  | LOD (µM) |  |  | Reference |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | AA | DA | UA | AA | DA | UA |  |
| AuNPs@MoS2 | 50-1.0x105 | 0.05-30 | 50-4.0x104 | 100 | 0.05 | 10 | [1] |
| 3D-MoS2/rGO/Au | 2-5400 | 0.3-198.3 | 5-2215 | 0.93 | 0.11 | 0.74 | [2] |
| MoS2/rGO | 12-5402 | 5-545 | 25-2745 | 0.72 | 0.05 | 0.46 | [3] |
| MoS2/PEDOT | 20-140 | 1-80 | 2-25 | 5.83 | 0.52 | 0.95 | [4] |
| AuNPs@MoS2-NSs | 20-300 | 5-200 | 20-400 | 3 | 1 | 5 | [5] |
| 3D MoS2-PANI/rGO | 50-8.0x103 | 5-500 | 1-500 | 22.20 | 0.70 | 0.36 | [6] |
| S-MoSe2/NSG/Au/MIPs |  | 0.05-1000 |  |  | 0.02 |  | [7] |
| CB-CNT/PI | 1000-24000 | 3-300 | 5-500 | 154 | 1.86 | 3 | [8] |
| WSe2@C | 8-2456 | 1.0-49 72.8-381.4 | 1-24.8 36,9-185.2 | 3.2 | 0.18 | 0.42 | [9] |
| Co/MoSe2/PPy@CNF | 30–3212 | 1.2–536 | 10–1071 | 6.32 | 0.45 | 0.81 | [10] |
| AuNps@MoSe2/SPCE |  | 3-20 |  |  | 0.21 |  | [11] |
| MoSe2 | 50-3440 | 1-333 | 5-1146 | 13.7 | 0.57 | 1.75 | This work |

References

1. H. Sun, J. Chao, X. Zuo, S. Su, X. Liu, L. Yuwen, C. Fan, and L. Wang, RSC Adv. 4, 27625 (2014).

2. Y. Zhao, J. Zhou, Z. Jia, D. Huo, Q. Liu, D. Zhong, Y. Hu, M. Yang, M. Bian, and C. Hou, Microchim. Acta 186, 1 (2019).

3. L. Xing and Z. Ma, Microchim. Acta 183, 257 (2016).

4. Y. Li, H. Lin, H. Peng, R. Qi, and C. Luo, Microchim. Acta 183, 2517 (2016).

5. H. L. Zou, B. L. Li, H. Q. Luo, and N. B. Li, Sensors Actuators B Chem. 253, 352 (2017).

6. S. Li, Y. Ma, Y. Liu, G. Xin, M. Wang, Z. Zhang, and Z. Liu, RSC Adv. 9, 2997 (2019).

7. Y. jiao Zang, J. Nie, B. He, W. Yin, J. Zheng, C. jun Hou, D. qun Huo, M. Yang, F. mei Liu, Q. qian Sun, Y. ling Qin, and H. bao Fa, Microchem. J. 156, 104845 (2020).

8. Y. Wang, T. Yang, Y. Hasebe, Z. Zhang, and D. Tao, Mater. 2018, Vol. 11, Page 1691 11, 1691 (2018).

9. S. Cogal and V. R. Bhethanabotla, IEEE Sens. J. 22, 14952 (2022).

10. G. Celik Cogal, S. Cogal, P. Machata, A. Uygun Oksuz, and M. Omastová, Microchim. Acta 191, 1 (2024).

11. K. Abid, A. Foti, A. Khaskhoussi, C. Celesti, C. D’Andrea, P. Polykretis, P. Matteini, D. Iannazzo, R. Maalej, P. G. Gucciardi, and G. Neri, Electrochim. Acta 475, 143371 (2024).