Supporting Information

Effect of Synthesis Conditions on Morphology, Surface Chemistry and Electrochemical Performance of Nickel Ferrite Nanoparticles for Lithium-ion Battery Applications.

Reshma S Babu1, Eszter Madai2, Durga S Nair3, Prasad Gonugunta2, Seyedamirhossein Mohseni Armaki2, Ruud Hendrikx2, Thamayanthi Panneerselvam1, Ramaswamy Murugan1, V.V. Ravi Kanth Kumar1, Peyman Taheri2, Arjan Mol2, N. Satyanarayana1*, Prasaanth Ravi Anusuyadevi2*.

1Department of Physics, Pondicherry University, Puducherry 605014, India.

2Department of Materials Science and Engineering (MSE), Faculty of Mechanical Engineering (ME), Delft University of Technology, Mekelweg 2, 2628 CD, Delft, The Netherlands.

3Department of Physics, Puducherry Technological University, Puducherry 605014, India

E-mail: nallanis2011@gmail.com; P.RaviAnusuyadevi@tudelft.nl or ranu.prasaanth@gmail.com

Supplementary Figure S1: Flowchart of detailed synthesis of NiFe2O4 nanoparticles

Supplementary Figure S2: SEM-EDX mapping of elements Ni, Fe and O in NFO-C sample

Supplementary Figure S3: Rate performance of NFO-S, NFO-G and NFO-C

Supplementary Table S1: Equivalent circuit components of NiFe2O4 samples

| Sample |  | Rel | Rct | RSEI | Qdl | adl | QSEI | aSEI | Warburg coefficient | Qint | aint | χ2 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | (Ω) | (Ω) | (Ω) | (F.s(a-1)) |  | (F.s(a-1)) |  | (Ω. s-1/2) | (F.s(a-1)) |  |  |  |
| NFO-S | Before 1st cycle | 5.622 | 23.51 | - | 55.22 x10-6 | 0.725 | - | - | 10.95 | 54.78 x10-3 | 0.356 | 14.05 x10-3 |  |
|  | After 100th cycle | 4.385 | 208.4 | 14.53 | 10.08 x10-6 | 0.803 | 2.541 x10-3 | 0.898 | 5.604 | 0.291 x10-3 | 0.699 | 1.568 x10-3 |  |
| NFO-U | Before 1st cycle | 7.902 | 117.2 | - | 48.08 x10-6 | 0.66 | - | - | -1845 | 0.134 x10-3 | 0.658 | 2.598 x10-3 |  |
|  | After 100th cycle | 9.007 | 190.9 | 1.416 | 25.13 x10-6 | 0.731 | 0.351 x10-3 | 1 | -290.8 | 0.105 x10-3 | 0.702 | 0.434 x10-3 |  |
| NFO-G | Before 1st cycle | 4.076 | 67.61 | - | 31.83 x10-6 | 0.75 | - | - | 26.54 | 0.962 x10-3 | 0.878 | 5.455 x10-3 |  |
|  | After 100th cycle | 4.941 | 197.5 | 0.298 | 27.09 x10-6 | 0.745 | 0.352 x10-3 | 0.401 | 198.2 | 0.488 x10-3 | 0.648 | 3.342 x10-3 |  |
| NFO-C | Before 1st cycle | 12.16 | 200 | - | 21.22 x10-6 | 0.687 | - | - | 2.29 x10-12 | 0.128 x10-3 | 0.895 | 3.808 x10-3 |  |
|  | After 100th cycle | 341.9 | 253.9 | 0.455 | 44.66 x10-6 | 0.619 | 1.287 x10-6 | 0.595 | 1608 | 96.9 x10-6 | 0.732 | 0.287 x10-3 |  |

Supplementary Table S2: Comparison of electrochemical performance of NiFe2O4 anode materials from the literature.

| Material | Electrochemical Performance | Ref |
| --- | --- | --- |
| NiFe2O4 | 400 mAh/g after 10 cycles at C/5 rate | [1] |
| NiFe2O4 thin film | 355 mAh/g after 100 cycles at 10 µA/cm2 | [2] |
| NiFe2O4 | 470 mAh/g after 20 cycles at C/8 rate | [3] |
| NiFe2O4 | 600 mAh/g after 80 cycles at 1 C rate | [4] |
| NiFe2O4 nanoparticles | 709 mAh/g after 3 cycles at 0.2 mA/cm2 | [5] |
| NiFe2O4 nanorods | 887 mAh/g at 1st discharge at 0.1 mA/cm2 | [6] |
| 3D ordered microporous NiFe2O4 | 670 mAh/g after 50 cycles at 0.2 mA/cm2 | [7] |
| NiFe2O4 nanofiber | 1000 mAh/g after 100 cycles at 100 mA/g | [8] |
| NiFe2O4/C | 780 mAh/g after 40 cycles at 1/8 C | [9] |
| NiFe2O4 | 600 mAh/g after 10 cycles at 0.2 mA/cm2 | [10] |
| NiFe2O4 nanoparticles | 880 mAh/g after 30 cycles at 0.1 C | [11] |
| NiFe2O4 nanorods | 520 mAh/g after 300 cycles at 1000 mA/g | [12] |
| 1D NiFe2O4 | 1349 mAh/g after 220 cycles at 100 mA/g | [13] |
| NiFe2O4 thin film | 1000 mAh/g after 100 cycles at 0.1 C | [14] |
| NiFe2O4 | 502.3 mAh/g after 100 cycles at 100 mA/g | [15] |
| NiFe2O4 Nanoparticles (NFO-S) | 2258 mAh/g at first discharge at 100 mA/g | This work |
|  | 116 mAh/g after 100 cycles at 100 mA/g |  |

References

1. 	Alcántara R, Jaraba M, Lavela P, Tirado JL, Jumas JC, Olivier-Fourcade J (2003) Changes in oxidation state and magnetic order of iron atoms during the electrochemical reaction of lithium with NiFe2O4. Electrochem commun 5:16–21. https://doi.org/https://doi.org/10.1016/S1388-2481(02)00520-9

2. 	NuLi Y-N, Qin Q-Z (2005) Nanocrystalline transition metal ferrite thin films prepared by an electrochemical route for Li-ion batteries. J Power Sources 142:292–297. https://doi.org/10.1016/j.jpowsour.2004.10.015

3. 	Li XD, Yang WS, Li F, Evans DG, Duan X (2006) Stoichiometric synthesis of pure NiFe2O4 spinel from layered double hydroxide precursors for use as the anode material in lithium-ion batteries. Journal of Physics and Chemistry of Solids 67:1286–1290. https://doi.org/10.1016/j.jpcs.2006.01.096

4. 	Lavela P, Tirado JL (2007) CoFe2O4 and NiFe2O4 synthesized by sol-gel procedures for their use as anode materials for Li ion batteries. J Power Sources 172:379–387. https://doi.org/10.1016/j.jpowsour.2007.07.055

5. 	Zhao H, Zheng Z, Wong KW, Wang S, Huang B, Li D (2007) Fabrication and electrochemical performance of nickel ferrite nanoparticles as anode material in lithium ion batteries. Electrochem commun 9:2606–2610. https://doi.org/10.1016/j.elecom.2007.08.007

6. 	Zhang D, Tong Z, Xu G, Li S, Ma J (2009) Templated fabrication of NiFe2O4 nanorods: Characterization, magnetic and electrochemical properties. Solid State Sci 11:113–117. https://doi.org/10.1016/j.solidstatesciences.2008.05.001

7. 	Zhang T, Cao H, Peng J, Xiao Q, Li Z, Lei G (2011) Excellent cycling performance of three-dimensional-ordered macroporous nife 2O 4 as anode material for lithium ion batteries. Functional Materials Letters 4:327–331. https://doi.org/10.1142/S1793604711002196

8. 	Cherian CT, Sundaramurthy J, Reddy M V., Suresh Kumar P, Mani K, Pliszka D, Sow CH, Ramakrishna S, Chowdari BVR (2013) Morphologically robust NiFe2O4 nanofibers as high capacity Li-Ion battery anode material. ACS Appl Mater Interfaces 5:9957–9963. https://doi.org/10.1021/am401779p

9. 	Ding Y, Yang Y, Shao H (2013) One-pot synthesis of NiFe2O4/C composite as an anode material for lithium-ion batteries. J Power Sources 244:610–613. https://doi.org/10.1016/j.jpowsour.2013.01.043

10. 	Liu H, Zhu H, Yang H (2013) A low temperature synthesis of nanocrystalline spinel NiFe 2O4 and its electrochemical performance as anode of lithium-ion batteries. Mater Res Bull 48:1587–1592. https://doi.org/10.1016/j.materresbull.2012.12.072

11. 	Kumar PR, Mitra S (2013) Nickel ferrite as a stable, high capacity and high rate anode for Li-ion battery applications. RSC Adv 3:25058–25064. https://doi.org/10.1039/c3ra44001j

12. 	Wang N, Xu H, Chen L, Gu X, Yang J, Qian Y (2014) A general approach for MFe2O4 (M = Zn, Co, Ni) nanorods and their high performance as anode materials for lithium ion batteries. J Power Sources 247:163–169. https://doi.org/10.1016/j.jpowsour.2013.08.109

13. 	Wang J, Yang G, Wang L, Yan W (2016) Synthesis of one-dimensional NiFe2O4 nanostructures: Tunable morphology and high-performance anode materials for Li ion batteries. J Mater Chem A Mater 4:8620–8629. https://doi.org/10.1039/c6ta02655a

14. 	Choi M, Lee SH, Jung Y Il, Jung JY, Park JS, Choi WK, Park SY, Won HJ, Moon JK, Choi J, Kim SB (2017) The high capacity and cycle stability of NiFe2O4 thin film prepared by E-beam evaporation method for lithium ion batteries. J Alloys Compd 729:802–808. https://doi.org/10.1016/j.jallcom.2017.06.334

15. 	Dai S, Tang X, Li X, Zhang J, Shao Z (2022) Synthesis of NiFe2O4 with different precipitation agents for Li-ion battery anode material by co-precipitation. Journal of Solid State Electrochemistry 26:1211–1220. https://doi.org/10.1007/s10008-022-05158-2