Methoxy-Substituted Phenylacrylonitrile Bearing an m-CF3 Group: Crystal Structure and Solvent-Dependent Excitonic-Thermodynamic Behavior

Leyla Babali Özena, Öner Ekicib*, Bayram Gündüzc, Cem Cüneyt Ersanlıd, Günseli Turgut Cina, Furkan Özene*

aDepartment of Chemistry, Faculty of Science, Akdeniz University, Antalya, Türkiye

E-mail: leyla.babaliozen1@gmail.com (ORCID: 0000-0001-9023-6604) gturgut@akdeniz.edu.tr (ORCID: 0000-0001-9658-8344)

bDepartment of Pharmacy Services, Durağan Vocational School, Sinop University, Sinop, Türkiye

(ORCID: 0000-0001-9658-8344)

cDepartment of Engineering Basic Sciences, Faculty of Engineering and Natural Sciences, Malatya Turgut Ozal University, Malatya, Türkiye

E-mail: bayram.gunduz@ozal.edu.tr (ORCID: 0000-0002-1447-7534)

dDepartment of Physics, Faculty of Arts and Science, Sinop University, Sinop, Türkiye

E-mail: ccersanli@sinop.edu.tr (ORCID: 0000-0002-8113-5091)

eDepartment of Mathematics and Science, Faculty of Education, Akdeniz University, Antalya, Türkiye E-mail: furkanozen@akdeniz.edu.tr (ORCID: 0000-0003-1178-1167)

*Corresponding author: oekici@sinop.edu.tr

Synthesis procedure of MTFMAN

3-(4-Methoxyphenyl)-2-(3-(trifluoromethyl)phenyl)acrylonitrile (MTFMAN)

A mixture of 4-methoxybenzaldehyde (5.0 g, 36.72 mmol) and 3-(trifluoromethyl)phenylacetonitrile (6.80 g, 36.72 mmol) was dissolved in ethanol in a 100 mL reaction flask and heated to 70 °C. At this temperature, 20% NaOH was gradually added to the reaction mixture until opacity was observed. The reaction was continued with stirring for 30 minutes. The resulting precipitate of 3-(4-methoxyphenyl)-2-(3-trifluoromethylphenyl)acrylonitrile (MTFMAN) was collected by filtration after cooling to room temperature, washed thoroughly with water, and recrystallized from ethanol to afford a pure product. It was crystallized from methanol, yielding thin block-shaped crystals. Yield: 90 % (0.84 g). m.p. = 87 °C. Anal. Calc. for C17H12F3NO (MW= 303.28): C, 67.33; H, 3.99; N, 4.62. Found: C, 67.30; H, 3.96; N, 4.60.

The synthesized compound were characterized by elemental analysis, FT-IR, 1H-NMR and 13C-APT-NMR spectroscopic techniques.

In the FT-IR (KBr, cm-1) spectra shown in Fig. S1;

FT-IR (KBr, cm-1): 3059 and 3023νC-H(Ar.), 2215νC≡N, 1595 and 1537νC=C and 1334νC-F.

In the 1H-NMR spectra shown in Fig. S2;

1H-NMR (400 MHz, CDCl3-d1) δ/ppm: 3.92 (3H, s, H1), 7.03 (2H, d, J=8.8, H3), 7.55 (1H, s, H6), 7.60 (1H, t, j=7.6, H10), 7.66 (1H, d, j=8.0, H12), 7.87 (1H, d, j=8.0, H14), 7.91 (1H, s, H10) and 7.96 (2H, d, j=9.2, H4).

In the 13C-APT-NMR spectra shown in Fig. S3;

13C-APT-NMR (400 MHz, CDCl3) δ/ppm: 55.52 C1, 107.08 C7, 114.53 C3, 118.11 C8, 122.38 C11, 125.31 C12, 125.34 C5, 126.00 C11, 126.86 C15, 129.14 C13, 129.64 C14, 130.27 C15, 131.54 C4, 135.80 C9, 143.44 C6, 161.89 C2.

Scheme 1. General synthesis scheme of compound.

Characterization of MTFMAN

The synthesized compound were characterized by elemental analysis, FT-IR, 1H-NMR and 13C-NMR spectroscopy techniques.

In the FT-IR spectrum, the absence of the carbonyl peak at around 1654 cm-1, which belongs to 4-methoxybenzaldehyde, indicates the absence of aldehyde in the medium. Additionally, the shift of the nitrile peak from 2255 cm-1, which belongs to 3-(trifluoromethyl)phenylacetonitrile, to 2215 cm-1 in the synthesized compound confirms the formation of the structure. In the 1H NMR spectrum, the most characteristic signals are the singlet at 3.92 ppm corresponding to the methoxy protons (–OCH3) and the absence of the aldehydic proton signal of 4-methoxybenzaldehyde at 10.3 ppm. In the 13C-APT-NMR spectra, the most characteristic signals are the observation of a peak at 55.52 ppm for the methoxy carbon and the absence of a peak for the carbonyl carbon of 4-methoxybenzaldehyde at 190.70 ppm.

Fig. S1. FT-IR spectrum of 2-(3-trifluoromethylphenyl)-3-(4-methoxyphenyl) acrylonitrile (KBr disk).

Fig. S2. 1H-NMR spectrum of 2-(3-trifluoromethylphenyl)-3-(4-methoxyphenyl)acrylonitrile (400 MHz, CDCl3, ppm).

Fig. S3.  13C-APT NMR spectrum of 2-(3-trifluoromethylphenyl)-3-(4-methoxyphenyl) acrylonitrile (400 MHz, CDCl3, ppm).

Table S1. Fractional atomic coordinates (x, y, z x 104), and equivalent isotropic displacement parameter Ueq (Å2 x 103) of MTFMAN.

| Atom | x | y | z | Ueq |
| --- | --- | --- | --- | --- |
| O1 | 2079.7(17) | 9863(3) | 3598.0(10) | 115.8(7) |
| N1 | 6115.7(19) | -1445(3) | 4149.8(12) | 92.3(7) |
| F1 | 4747(10) | 870(30) | 785(9) | 181(9) |
| F1A | 5500(20) | 1998(14) | 497(4) | 148(5) |
| F2 | 5965(16) | -1037(12) | 1175(4) | 115(5) |
| F2A | 5058(17) | -540(30) | 1077(6) | 214(9) |
| F3 | 6337(16) | 1380(30) | 546(6) | 154(8) |
| F3A | 6608(7) | -30(30) | 914(9) | 206(8) |
| C1 | 5743(4) | 835(6) | 1064.5(16) | 91.1(9) |
| C2 | 5876.4(18) | 2106(3) | 1726.3(12) | 63.8(6) |
| C3 | 6383.2(19) | 3950(4) | 1704.9(13) | 75.6(7) |
| C4 | 6517.8(19) | 5107(4) | 2317.5(14) | 76.7(7) |
| C5 | 6144.8(18) | 4436(3) | 2947.3(13) | 67.6(6) |
| C6 | 5625.7(17) | 2588(3) | 2976.9(11) | 55.8(6) |
| C7 | 5501.6(17) | 1425(3) | 2357.3(12) | 61.7(6) |
| C8 | 5230.1(18) | 1864(3) | 3664.0(11) | 58.9(6) |
| C9 | 5710(2) | 20(4) | 3939.1(12) | 70.3(7) |
| C10 | 4529.8(19) | 2804(3) | 4062.9(12) | 66.1(6) |
| C11 | 3894.9(17) | 4641(3) | 3924.0(12) | 60.4(6) |
| C12 | 3649.5(18) | 5479(4) | 3246.4(12) | 70.8(7) |
| C13 | 3045(2) | 7200(4) | 3157.4(13) | 83.4(8) |
| C14 | 2667(2) | 8154(4) | 3741.9(15) | 77.1(7) |
| C15 | 2873(2) | 7339(4) | 4416.1(14) | 80.2(7) |
| C16 | 3483.7(19) | 5584(4) | 4500.0(13) | 71.0(7) |
| C17 | 1636(2) | 10897(4) | 4178.7(19) | 125.9(12) |

Table S2. Anisotropic displacement parameters (Å2 x 103) for MTFMANa.

| Atom | U11 | U22 | U33 | U12 | U13 | U23 |
| --- | --- | --- | --- | --- | --- | --- |
| O1 | 129.8(17) | 111.5(15) | 104.7(15) | 57.5(13) | 3.3(13) | -7.5(12) |
| N1 | 125.5(19) | 75.1(15) | 78.9(15) | 21.2(14) | 23.3(13) | 8.1(12) |
| F1 | 126(7) | 216(13) | 186(11) | 37(8) | -74(7) | -120(10) |
| F2 | 189(12) | 80(6) | 77(4) | 34(6) | 13(6) | -25(3) |
| F3 | 208(16) | 184(11) | 82(6) | -100(11) | 86(8) | -37(6) |
| F1A | 222(14) | 174(6) | 45(3) | -32(9) | 1(5) | -5(3) |
| F2A | 255(17) | 241(15) | 159(8) | -170(13) | 101(10) | -126(9) |
| F3A | 145(6) | 301(16) | 178(11) | 7(9) | 48(7) | -158(11) |
| C1 | 110(3) | 106(3) | 58(2) | -25(3) | 17(2) | -10.4(19) |
| C2 | 69.0(15) | 70.7(15) | 51.9(14) | -7.1(13) | 6.8(12) | -7.5(12) |
| C3 | 80.7(17) | 83.6(17) | 64.4(17) | -11.5(14) | 17.4(14) | 7.6(14) |
| C4 | 84.0(18) | 63.8(15) | 84.0(19) | -16.5(13) | 17.1(15) | -0.7(14) |
| C5 | 72.9(15) | 61.0(15) | 69.9(17) | -2.6(12) | 11.1(13) | -11.8(12) |
| C6 | 62.8(14) | 53.8(14) | 51.4(13) | 2.6(11) | 9.5(11) | -4.1(11) |
| C7 | 70.7(15) | 58.3(14) | 56.9(14) | -5.5(11) | 10.8(12) | -5.7(11) |
| C8 | 72.4(15) | 56.3(14) | 49.2(13) | 2.3(12) | 12.1(12) | -6.0(11) |
| C9 | 91.8(19) | 64.3(16) | 56.9(15) | 3.4(15) | 18.2(13) | -1.7(13) |
| C10 | 80.2(16) | 69.5(15) | 49.8(13) | -1.9(13) | 12.0(12) | 1.2(11) |
| C11 | 62.0(15) | 65.8(15) | 54.5(14) | 3.0(12) | 11.2(12) | -5.9(12) |
| C12 | 69.4(16) | 89.4(17) | 53.1(15) | 15.0(14) | 1.9(12) | -8.0(13) |
| C13 | 80.6(18) | 105(2) | 63.8(17) | 29.3(16) | 5.1(14) | 3.0(15) |
| C14 | 74.8(17) | 79.6(18) | 75.7(19) | 22.4(14) | 0.2(14) | -3.6(15) |
| C15 | 85.0(18) | 88.4(18) | 69.3(18) | 11.6(15) | 18.7(14) | -20.8(14) |
| C16 | 81.3(17) | 77.9(16) | 55.4(14) | 10.4(14) | 14.5(12) | -1.3(12) |
| C17 | 122(3) | 111(2) | 145(3) | 49(2) | 15(2) | -32(2) |

a The exponent of the anisotropic displacement factor is of the form: -2π2h2a*2U11+2hka*b*U12+… where Uij are the anisotropic displacement tensor elements and h, k, and l are the Miller indices.

Table S3. Hydrogen atom coordinates (Å x 104) and ısotropic displacement parameters (Å2 x 103) for MTFMAN.

| Atom | x | y | z | Ueq |
| --- | --- | --- | --- | --- |
| H3 | 6633.1(19) | 4411(4) | 1278.2(13) | 90.7(8) |
| H4 | 6863.5(19) | 6351(4) | 2305.7(14) | 92.1(9) |
| H5 | 6241.4(18) | 5231(3) | 3359.1(13) | 81.2(8) |
| H7 | 5162.3(17) | 175(3) | 2367.4(12) | 74.0(7) |
| H10 | 4433.6(19) | 2181(3) | 4499.8(12) | 79.3(8) |
| H12 | 3901.1(18) | 4858(4) | 2846.0(12) | 85.0(8) |
| H13 | 2888(2) | 7733(4) | 2698.3(13) | 100.0(9) |
| H15 | 2606(2) | 7955(4) | 4812.6(14) | 96.2(9) |
| H16 | 3619.2(19) | 5030(4) | 4957.5(13) | 85.3(8) |
| H17A | 1280(17) | 12110(20) | 4001(3) | 188.9(18) |
| H17B | 1119(15) | 10040(15) | 4385(9) | 188.9(18) |
| H17C | 2210(3) | 11240(30) | 4540(6) | 188.9(18) |

Table S4. Bond lengths for MTFMAN (Å).

| Atom | Atom | Length | Atom | Atom | Length |
| --- | --- | --- | --- | --- | --- |
| O1 | C14 | 1.359(3) | C2 | C1 | 1.491(3) |
| O1 | C17 | 1.431(3) | C16 | C15 | 1.3883) |
| C6 | C7 | 1.385(3) | C12 | C13 | 1.366(3) |
| C6 | C8 | 1.491(3) | C4 | C5 | 1.373(3) |
| C6 | C5 | 1.386(3) | C4 | C3 | 1.373(3) |
| C11 | C10 | 1.459(3) | C15 | C14 | 1.370(3) |
| C11 | C16 | 1.378(3) | C13 | C14 | 1.377(3) |
| C11 | C12 | 1.388(3) | C1 | F1 | 1.293(8) |
| C7 | C2 | 1.378(3) | C1 | F2 | 1.284(7) |
| N1 | C9 | 1.146(3) | C1 | F3 | 1.316(9) |
| C8 | C10 | 1.343(3) | C1 | F1A | 1.321(8) |
| C8 | C9 | 1.433(3) | C1 | F2A | 1.247(6) |
| C2 | C3 | 1.376(3) | C1 | F3A | 1.265(8) |

Table S5. MTFMAN bond angles (o).

| Atom | Atom | Atom | Angle | Atom | Atom | Atom | Angle |
| --- | --- | --- | --- | --- | --- | --- | --- |
| C17 | O1 | C14 | 118.9(2) | C13 | C14 | O1 | 116.1(2 |
| C8 | C6 | C7 | 121.11(19) | C13 | C14 | C15 | 119.8(2) |
| C5 | C6 | C7 | 118.4(2) | F1 | C1 | C2 | 110.7(5) |
| C5 | C6 | C8 | 120.47(19) | F3 | C1 | C2 | 115.1(5) |
| C16 | C11 | C10 | 118.0(2) | F3 | C1 | F1 | 105.7(11) |
| C12 | C11 | C10 | 124.5(2) | F2 | C1 | C2 | 114.1(4) |
| C12 | C11 | C16 | 117.5(2) | F2 | C1 | F1 | 105.3(9) |
| C2 | C7 | C6 | 120.6(2) | F2 | C1 | F3 | 105.1(7) |
| C10 | C8 | C6 | 127.1(2) | F3A | C1 | C2 | 114.0(4) |
| C9 | C8 | C6 | 115.17(18) | F3A | C1 | F1 | 135.3(5) |
| C9 | C8 | C10 | 117.65(19) | F3A | C1 | F3 | 54.9(6) |
| C3 | C2 | C7 | 120.3(2) | F3A | C1 | F2 | 55.0(6) |
| C1 | C2 | C7 | 120.0(2) | F2A | C1 | C2 | 115.0(4) |
| C1 | C2 | C3 | 119.7(2) | F2A | C1 | F1 | 53.0(11) |
| C8 | C10 | C11 | 130.7(2) | F2A | C1 | F3 | 129.8(5) |
| C15 | C16 | C11 | 121.8(2) | F2A | C1 | F2 | 54.8(6) |
| C13 | C12 | C11 | 121.2(2) | F2A | C1 | F3A | 105.1(7) |
| C3 | C4 | C5 | 120.4(2) | F1A | C1 | C2 | 109.4(5) |
| C8 | C9 | N1 | 178.3(3) | F1A | C1 | F1 | 61.8(6) |
| C4 | C5 | C6 | 120.8(2) | F1A | C1 | F3 | 49.6(9) |
| C4 | C3 | C2 | 119.6(2) | F1A | C1 | F2 | 136.2(5) |
| C14 | C15 | C16 | 119.2(2) | F1A | C1 | F3A | 102.8(11) |
| C14 | C13 | C12 | 120.5(2) | F1A | C1 | F2A | 109.7(10) |
| C15 | C14 | O1 | 124.1(2) |  |  |  |  |

Table S6. Torsion angles for MTFMAN (o).

| Atom | Atom | Atom | Atom | Angle | Atom | Atom | Atom | Atom | Angle |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| O1 | C14 | C15 | C16 | 180.0(3) | C8 | C10 | C11 | C16 | -161.7(3) |
| O1 | C14 | C13 | C12 | 179.6(2) | C8 | C10 | C11 | C12 | 20.1(3) |
| C6 | C7 | C2 | C3 | 0.2(3) | C2 | C7 | C6 | C5 | -0.7(2) |
| C6 | C7 | C2 | C1 | 179.6(3) | C2 | C3 | C4 | C5 | -0.3(3) |
| C6 | C8 | C10 | C11 | 6.0(3) | C10 | C11 | C16 | C15 | 179.9(2) |
| C6 | C5 | C4 | C3 | -0.1(3) | C10 | C11 | C12 | C13 | 179.7(2) |
| C11 | C10 | C8 | C9 | -178.1(2) | C10 | C8 | C6 | C5 | 57.3(3) |
| C11 | C16 | C15 | C14 | 0.3(3) | C16 | C11 | C12 | C13 | 1.5(2) |
| C11 | C12 | C13 | C14 | 0.3(3) | C16 | C15 | C14 | C13 | 1.5(3) |
| C7 | C6 | C8 | C10 | -123.7(2) | C12 | C11 | C16 | C15 | -1.8(3) |
| C7 | C6 | C8 | C9 | 60.3(2) | C12 | C13 | C14 | C15 | -1.8(3) |
| C7 | C6 | C5 | C4 | 0.6(2) | C4 | C3 | C2 | C1 | -179.1(3) |
| C7 | C2 | C3 | C4 | 0.3(3) | C9 | C8 | C6 | C5 | -118.7(2) |
| C7 | C2 | C1 | F1 | 75.2(12) | C3 | C2 | C1 | F1 | -105.4(12) |
| C7 | C2 | C1 | F3 | -165.0(13) | C3 | C2 | C1 | F3 | 14.4(13) |
| C7 | C2 | C1 | F2 | -43.4(10) | C3 | C2 | C1 | F2 | 136.0(10) |
| C7 | C2 | C1 | F3A | -104.1(14) | C3 | C2 | C1 | F3A | 75.3(14) |
| C7 | C2 | C1 | F2A | 17.4(14) | C3 | C2 | C1 | F2A | -163.2(14) |
| C7 | C2 | C1 | F1A | 141.4(12) | C3 | C2 | C1 | F1A | -39.2(12) |
| C8 | C6 | C7 | C2 | -179.6(2) | C15 | C14 | O1 | C17 | -0.3(3) |
| C8 | C6 | C5 | C4 | 179.6(2) | C13 | C14 | O1 | C17 | 178.2(2) |

Table S7. π···π Stacking interaction parameters.

| Interaction Pair | Cg–Cg Distance (Å) | Dihedral Angle (α, o) | Beta (o) | Gamma (o) | Cg(I) ⊥ (Å) | Cg(J) ⊥ (Å) |
| --- | --- | --- | --- | --- | --- | --- |
| Cg(1)···Cg(1)* | 4.9535 | 52.05 | 16.95 | 68.34 | 1.829 | 4.738 |

Note: The Cg(1) ring is a six-membered aromatic ring containing by atoms C2–C7. The asterisk (*) mark denotes the symmetry-related equivalent position given by the symmetry operation: -½-x, -½+y, ½-z.

Table S8. C–H···π Interaction parameters.

| Interaction | H···Cg (Å) | H ⊥ (Å) | Gamma (o) | X–H···Cg (o) | X···Cg (Å) |
| --- | --- | --- | --- | --- | --- |
| C(4)–H(4)...Cg(1) | 2.9417 | 2.940 | 1.66 | 141.34 | 3.7135 |

Note: This interaction is between the hydrogen atom H4 bonded to C4 directing towards the centroid of the aromatic ring in the symmetry-related position: -½-x, ½+y, ½-z.