Table S1. XRF compositions of raw powders (wt%).

| Powder | Fe (wt%) | Si (wt%) | Cr (wt%) | P (wt%) | Remarks |
| --- | --- | --- | --- | --- | --- |
| FeSiCr (matrix) | 88.5 | 5.1 | 6.1 | — | Fe–Si–Cr solid solution |
| RIP (SiO₂-coated) | > 98 | trace | — | — | Si from silica shell |
| CIP (SiO₂-coated) | > 98 | trace | — | — | Si from silica shell |
| CIP-P (phosphate-coated) | > 98 | — | — | trace | P from phosphate shell |

Table S2 Particle-size distribution metrics (laser diffraction).

| Powder | D10 (µm) | D50 (µm) | D90 (µm) | Span = (D90 − D10)/D50 |
| --- | --- | --- | --- | --- |
| FeSiCr | 12.4 | 17.8 | 30.6 | 1.02 |
| RIP | 2.4 | 4.6 | 9.1 | 1.46 |
| CIP | 2.7 | 5.5 | 9.8 | 1.29 |
| CIP-P | 2.5 | 4.9 | 9 | 1.33 |

Fig.S1 SEM images of the raw materials.

| CIP | RIP |
| --- | --- |
| CIP-P | FeSiCr |
| Fig.S2 Volume-based particle-size distribution (PSD) curves of the raw materials. |  |

Fig.S3 Variation of initial permeability (μi) with the measuring frequency (100-1000 kHz).