Stable sol–gel hydroxyapatite coating on zirconia dental implant for improved osseointegration

Jinyoung Kim1, In-Gu Kang1, Kwang-Hee Cheon1, Sungmi Lee2, Suhyung Park1, Hyoun-Ee Kim1, Cheol-Min Han*,3

1Department of Materials Science and Engineering, Seoul National University, Seoul 08826, Republic of Korea

2Biomedical Implant Convergence Research Center, Advanced Institutes of Convergence Technology, Suwon 16229, Republic of Korea

3Department of Carbon and Nano Materials Engineering, Jeonju University, Jeonju 55069, Republic of Korea

*Corresponding Author

Cheol-Min Han, Jeonju University

Email : hancm@jj.ac.kr

Tel : +82-63-220-2208

Postal Address : 303 Cheonjam-ro, Wansan-gu, Jeonju-si, Jeollabuk-do, 55069, Republic of Korea

Figure S1. Transmission electron microscopy images of dried HA sol after 1 day of aging observed with (a) low (× 40,000) and (b) high (× 600,000) magnifications. Scale bars are (a) 100 nm and (b) 5 nm.

Figure S2. X-ray photoelectron spectroscopy data of (a, c) HA800 and (b, d) HA1000. (a, b : survey spectra, c, d : O 1s).

Figure S3. Scanning electron microscopy images of HA-coated zirconia screw sintered at 800 °C after implantation on synthetic bone; (a) ridge and (b) groove of screw. scale bars are 2 mm.