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[bookmark: OLE_LINK19][bookmark: OLE_LINK20]Fig.S1. (Williamson Hall Plot: Goethite (Unannealed sample) 500oC(a). Hematite (annealed) sample (b). 
[image: Chart

Description automatically generated]








Fig.S2. FT-IR of α- Fe2O3 and α- Fe2O3-PEG.
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Fig.S3. UV- vis spectra of the hematite nanorods: (a) Absorption spectra (b) Reflectance spectra.
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Fig.S4. Tauc plot showing band gap energy of hematite nanorods.
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[bookmark: _GoBack]Fig.S5. (a)Solubility of α-Fe2O3 and α-Fe2O3-PEG in water and PBS over a time period of 72 hours (b) Zeta potential of α-Fe2O3-PEG in water, PBS and FBS.
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Fig.6S (a) Tumor weight after extraction of different treatment groups, (b) Survival rate of various treatment groups.


Calculation of Photothermal conversion efficiency
Photothermal conversion efficiency of the α-Fe2O3-PEG was calculated by recording the change in the temperature of the NP aqueous dispersion as a function of time under continuous irradiation of a 808 nm laser (0.5 W/cm2) for 5 mins until the solution reached a steady-state temperature. The photothermal conversion efficiency (ƞ) was calculated according to Equation S1: 


[image: ]   Equation S1.



Where, h represents the heat transfer coefficient, A is the surface area of the container, Tmax represents the maximum steady-state temperature (60 °C), Tsurr is the ambient temperature of the environment (25 °C), Qdis represents the heat dissipation from the light absorbed by the solvent and the quartz sample cell, I is the incident laser power (0.5 W/cm2), and A660 is the absorbance of the sample at 740 nm (1.776). The value of hA is derived from Equation S2:
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                                  Equation S2.                        

 Where τ is the time constant for heat transfer of the system which was determined to be τ =390.96 from Fig 6d. mD and cD are respectively the mass (1.0 g) and heat capacity (4.2 J/g) of the deionized water used to disperse the α-Fe2O3-PEG. So, the hA was determined to be 0.0201 W. Qdis represents the heat dissipation from the light absorbed by the water and the quartz sample cell, so Qdis was calculated according to Equation S3:

[image: ]  Equation S3.


Where Tmax(water)is 26.8 °C, τ (water) is 259.25, so Qdis was calculated to be 0.0211 W. 
According to the obtained data and Equation (1), the photothermal conversion efficiency of the α-Fe2O3-PEG was determined to be 39.5%.
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