Supplementary Table 7. Mean ± standard deviation and statistical analysis of the Vickers hardness.

| Group |  | Mean ± SD (VH) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Control |  | First-aged | P |  | Second-aged | P † |  | P ‡ |
| L | 1406.58 ± 44.13a |  | 1349.94 ± 45.90a | <.001* | 1301.93 ± 40.66a |  | <.001* |  | <.001* |
| M | 1491.34 ± 29.76b |  | 1469.34 ± 39.49b | .004* | 1453.10 ± 44.42b |  | <.001* |  | .070 |
| T | 1516.78 ± 36.60c |  | 1477.00 ± 45.30b | <.001* | 1450.56 ± 46.33b |  | <.001* |  | .007* |
| P | 1451.06 ± 52.64d |  | 1402.48 ± 39.08c | <.001* | 1352.41 ± 45.73c |  | <.001* |  | <.001* |
| E | 1518.84 ± 41.12c |  | 1453.80 ± 40.37b | <.001* | 1430.37 ± 35.24b |  | <.001* |  | .004* |

SD, standard deviation; L, 3Y-TZP of IPS E.max ZirCAD LT; M, 4Y-TZP of IPS E.max ZirCAD MT; T, 5Y-TZP of IPS E.max ZirCAD MT Multi; P, 3Y/5Y-TZP of IPS E.max ZirCAD Prime; E, 4Y/5Y-TZP of IPS E.max ZirCAD Prime esthetic

Significant differences between the values in each column are denoted by different superscript letters, indicating statistical significance (P < .05)

P values were calculated using independent t-test results of samples from the control and first aged groups

P† values were calculated using independent t-test results of the samples from the control and second aged groups

P‡ values were calculated using the independent t-test results of the samples of the first and second aged groups

*denotes a significant difference at P < .05