Supplementary Table 13C. Mean ± standard deviation and statistical elemental analysis of the IPS E.max ZirCAD MT Multi groups using EDS.
	Group
	Mean ± SD (wt%)

	
	Zr
	O
	Y
	Hf
	Al

	TC
	67.33 ± 0.41c
	24.47 ± 0.40a
	6.55 ± 0.17c
	1.64 ± 0.06c
	0.02 ± 0.03b

	TAF
	67.31 ± 0.34c
	24.74 ± 0.21b
	6.26 ± 0.19c
	1.67 ± 0.07c
	0.02 ± 0.02b

	P
	.863
	.003*
	<.001*
	.062
	.180

	TAS
	67.30 ± 0.23c
	24.63 ± 0.21a
	6.40 ± 0.23c
	1.64 ± 0.10b
	0.03 ± 0.02b

	P†
	.780
	.065
	.009*
	1.000
	.385

	P ‡
	 .922
	.053
	.021*
	.160
	 .012*


SD, standard deviation; L, 3Y-TZP of IPS E.max ZirCAD LT; M, 4Y-TZP of IPS E.max ZirCAD MT; T, 5Y-TZP of IPS E.max ZirCAD MT Multi; P, 3Y/5Y-TZP of IPS E.max ZirCAD Prime; E, 4Y/5Y-TZP of IPS E.max ZirCAD Prime esthetic
Significant differences between the values in each column are denoted by different superscript letters, indicating statistical significance (P < .05)
P values were calculated using independent t-test results of samples from the control and first aged groups
P† values were calculated using independent t-test results of the samples from the control and second aged groups
P‡ values were calculated using the independent t-test results of the samples of the first and second aged groups
*denotes a significant difference at P < .05
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