Supplementary Table 13C. Mean ± standard deviation and statistical elemental analysis of the IPS E.max ZirCAD MT Multi groups using EDS.

| Group | Mean ± SD (wt%) |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | Zr | O | Y | Hf | Al |
| TC | 67.33 ± 0.41c | 24.47 ± 0.40a | 6.55 ± 0.17c | 1.64 ± 0.06c | 0.02 ± 0.03b |
| TAF | 67.31 ± 0.34c | 24.74 ± 0.21b | 6.26 ± 0.19c | 1.67 ± 0.07c | 0.02 ± 0.02b |
| P | .863 | .003* | <.001* | .062 | .180 |
| TAS | 67.30 ± 0.23c | 24.63 ± 0.21a | 6.40 ± 0.23c | 1.64 ± 0.10b | 0.03 ± 0.02b |
| P† | .780 | .065 | .009* | 1.000 | .385 |
| P ‡ | .922 | .053 | .021* | .160 | .012* |

SD, standard deviation; L, 3Y-TZP of IPS E.max ZirCAD LT; M, 4Y-TZP of IPS E.max ZirCAD MT; T, 5Y-TZP of IPS E.max ZirCAD MT Multi; P, 3Y/5Y-TZP of IPS E.max ZirCAD Prime; E, 4Y/5Y-TZP of IPS E.max ZirCAD Prime esthetic

Significant differences between the values in each column are denoted by different superscript letters, indicating statistical significance (P < .05)

P values were calculated using independent t-test results of samples from the control and first aged groups

P† values were calculated using independent t-test results of the samples from the control and second aged groups

P‡ values were calculated using the independent t-test results of the samples of the first and second aged groups

*denotes a significant difference at P < .05