Supplementary Table 13D. Mean ± standard deviation and statistical elemental analysis of the IPS E.max ZirCAD Prime groups using EDS.

| Group | Mean ± SD (wt%) |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | Zr | O | Y | Hf | Al |
| PC | 69.41 ± 0.70b | 25.13 ± 0.14c | 3.69 ± 0.73d | 1.74 ± 0.10ab | 0.03 ± 0.02b |
| PAF | 69.02 ± 0.95b | 24.95 ± 0.16c | 4.31 ± 1.02d | 1.70 ± 0.06bc | 0.02 ± 0.02b |
| P | .090 | <.001* | .013* | .083 | .022* |
| PAS | 69.89 ± 0.20a | 25.06 ± 0.16b | 4.46 ± 0.44d | 1.68 ± 0.08ab | 0.02 ± 0.02b |
| P† | <.001* | .079 | <.001* | .026* | .002* |
| P ‡ | .253 | .016* | .504 | .365 | .426 |

SD, standard deviation; L, 3Y-TZP of IPS E.max ZirCAD LT; M, 4Y-TZP of IPS E.max ZirCAD MT; T, 5Y-TZP of IPS E.max ZirCAD MT Multi; P, 3Y/5Y-TZP of IPS E.max ZirCAD Prime; E, 4Y/5Y-TZP of IPS E.max ZirCAD Prime esthetic

Significant differences between the values in each column are denoted by different superscript letters, indicating statistical significance (P < .05)

P values were calculated using independent t-test results of samples from the control and first aged groups

P† values were calculated using independent t-test results of the samples from the control and second aged groups

P‡ values were calculated using the independent t-test results of the samples of the first and second aged groups

*denotes a significant difference at P < .05