Supplementary Table 13D. Mean ± standard deviation and statistical elemental analysis of the IPS E.max ZirCAD Prime groups using EDS.
	Group
	Mean ± SD (wt%)

	
	Zr
	O
	Y
	Hf
	Al

	PC
	69.41 ± 0.70b
	25.13 ± 0.14c
	3.69 ± 0.73d
	1.74 ± 0.10ab
	0.03 ± 0.02b

	PAF
	69.02 ± 0.95b
	24.95 ± 0.16c
	4.31 ± 1.02d
	1.70 ± 0.06bc
	0.02 ± 0.02b

	P
	.090
	<.001*
	.013*
	.083
	.022*

	PAS
	69.89 ± 0.20a
	25.06 ± 0.16b
	4.46 ± 0.44d
	1.68 ± 0.08ab
	0.02 ± 0.02b

	P†
	<.001*
	.079
	<.001*
	.026*
	.002*

	P ‡
	.253
	 .016*
	.504
	.365
	.426


SD, standard deviation; L, 3Y-TZP of IPS E.max ZirCAD LT; M, 4Y-TZP of IPS E.max ZirCAD MT; T, 5Y-TZP of IPS E.max ZirCAD MT Multi; P, 3Y/5Y-TZP of IPS E.max ZirCAD Prime; E, 4Y/5Y-TZP of IPS E.max ZirCAD Prime esthetic
Significant differences between the values in each column are denoted by different superscript letters, indicating statistical significance (P < .05)
P values were calculated using independent t-test results of samples from the control and first aged groups
P† values were calculated using independent t-test results of the samples from the control and second aged groups 
P‡ values were calculated using the independent t-test results of the samples of the first and second aged groups
*denotes a significant difference at P < .05
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