Supplementary Table 13E. Mean ± standard deviation and statistical elemental analysis of the IPS E.max ZirCAD Prime esthetic groups using EDS.
	Group
	Mean ± SD (wt%)

	
	Zr
	O
	Y
	Hf
	Al

	EC
	68.07± 0.39d
	24.98± 0.15c
	5.20 ± 0.45e
	1.71± 0.07bc
	0.03± 0.02b

	EAF
	67.70 ± 0.33d
	25.27 ± 0.24d
	5.33 ± 0.52e
	1.67 ± 0.07c
	0.04 ± 0.03a

	P
	<.001*
	<.001*
	.319
	.021*
	.175

	EAS
	67.65 ± 0.49d
	24.72 ± 0.22a
	5.94 ± 0.48e
	1.66 ± 0.08ab
	0.03 ± 0.02b

	P†
	 .001*
	<.001*
	<.001*
	.028*
	.650

	P ‡
	.691
	 <.001*
	<.001*
	.957
	.116


SD, standard deviation; L, 3Y-TZP of IPS E.max ZirCAD LT; M, 4Y-TZP of IPS E.max ZirCAD MT; T, 5Y-TZP of IPS E.max ZirCAD MT Multi; P, 3Y/5Y-TZP of IPS E.max ZirCAD Prime; E, 4Y/5Y-TZP of IPS E.max ZirCAD Prime esthetic
Significant differences between the values in each column are denoted by different superscript letters, indicating statistical significance (P < .05)
P values were calculated using independent t-test results of samples from the control and first aged groups
P† values were calculated using independent t-test results of the samples from the control and second aged groups 
P‡ values were calculated using the independent t-test results of the samples of the first and second aged groups
*denotes a significant difference at P < .05
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