Supplementary Information

Figure S1 Equivalent degradation time of native and pre-degraded meshes, after implantation up to 78 weeks (E1, E2, E2’ and E3 represents pre-degraded implants for implantation, black crosses represent equivalent total time in-vivo at termination point)

|  |  | Implanted samples |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  | E1 | E2 | E2’ (collagen disc) | E3 (collagen disc) |
| SRM | SEM picture |  |  |  |  |
|  | Residual gravimetric mass | 100% | 95 ± 1% | 82 ± 1% | 60 ± 2% |
| TIGr® | SEM picture |  |  |  |  |
|  | Residual gravimetric mass | 100% | 98 ± 2% | 76 ± 2% | 57 ± 1% |

Table S1 Characteristics of native and pre-degraded SRM and TIGr® meshes