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Supplementary Information
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Figure S1 Equivalent degradation time of native and pre-degraded meshes, after implantation up to 78 weeks (E1, E2, E2’ and E3 represents pre-degraded implants for implantation, black crosses represent equivalent total time in-vivo at termination point)


	
	Implanted samples

	
	E1
	E2
	E2’ (collagen disc)
	E3 (collagen disc)

	SRM
	SEM 
picture
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	Residual gravimetric mass
	100%
	95 ± 1%
	82 ± 1%
	60 ± 2%

	TIGr®
	SEM 
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	Residual gravimetric mass
	100%
	98 ± 2%
	76 ± 2%
	57 ± 1%



Table S1 Characteristics of native and pre-degraded SRM and TIGr® meshes
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