Supplementary Material

Incorporation of functionalized calcium phosphate nanoparticles in living cells

Manuel Rivas,1 Pau Turon,2 Carlos Alemán,1,* Jordi Puiggalí,1,* and Luis J. del Valle1,*

1 Departament d’Enginyeria Química and Barcelona Research Center for Multiscale Science and Engineering, EEBE, Universitat Politècnica de Catalunya, Av. Eduard Maristany, 16, Barcelona 08019, Spain.

2 B. Braun Surgical, S.A. Carretera de Terrassa 121, 08191 Rubí (Barcelona), Spain

*Correspondence to: carlos.aleman@upc.edu; jordi.puiggali@upc.edu; luis.javier.del.valle@upc.edu

Figure S1. Viability of MCF-7, COS-1 and HUVEC cells treated with extracellular Ca2+ and the two types of loaded NPs (i.e. <200 nm and >200 nm) by non-electroporation (-EP) (a) and electroporation (+EP) (b). Assays were performed in presence and absence of 0.5 mM EGTA as chelating agent. The cellular viability was measured with the Alamar Blue reagent after 48 h of culture.

Figure S2. Viability of MCF-7, COS-1 and HUVEC cells treated with extracellular Ca2+ and the two types of loaded NPs (i.e. <200 nm and >200 nm) by non-electroporation (-EP) (a) and electroporation (+EP) (b). Assays were performed in presence and absence of 0.5 mM EGTA as chelating agent. The cellular viability was measured with the MTT reagent after 24 h of culture.

Figure S3. Viability of MCF-7, COS-1 and HUVEC cells treated with extracellular Ca2+ and the two types of loaded NPs (i.e. <200 nm and >200 nm) by non-electroporation (-EP) (a) and electroporation (+EP) (b). Assays were performed in presence and absence of 0.5 mM EGTA as chelating agent. The cellular viability was measured with the MTT reagent after 48 h of culture.

Figure S4. Viability of MCF-7, COS-1 and HUVEC cells after incorporation of NPs <200 nm coated with biophosphates and biophosphonates (a). The different concentrations of Ca2+ were introduced by non-electroporation (-EP) and electroporation (+EP). b) Effect caused by pre-treatement with alkaline phosphatase and Mg2+ as cofactor. The cellular viability was measured by Alamar Blue assay after 48 h of culture.

Figure S5. Viability of MCF-7, COS-1 and HUVEC cells after incorporation of NPs <200 nm coated with biophosphates and biophosphonates (a). The different concentrations of Ca2+ were introduced by non-electroporation (-EP) and electroporation (+EP). b) Effect caused by pre-treatement with alkaline phosphatase and Mg2+ as cofactor. The cellular viability was measured by MTT assay after 24 h of culture.

Figure S6. Viability of MCF-7, COS-1 and HUVEC cells after incorporation of NPs <200 nm coated with biophosphates and biophosphonates (a). The different concentrations of Ca2+ were introduced by non-electroporation (-EP) and electroporation (+EP). b) Effect caused by pre-treatement with alkaline phosphatase and Mg2+ as cofactor. The cellular viability was measured by MTT assay after 48 h of culture.

Table S1. CC50 of Ca2+ and NPs incorporated into cells by electroporation (+EP) and non-electroporation (-EP). Experiments were performed with and without Ca2+chelation (i.e. +EGTA and –EGTA, respectively). Values were determined from curves displayed in Figure S1.

| Cell line | CC50 (mM) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Ca2+ |  | NPs <200 nm |  | NPs >200 nm |  |
|  | -EGTA | +EGTA | -EGTA | +EGTA | -EGTA | +EGTA |
| -EP |  |  |  |  |  |  |
| MCF-7 | --- | --- | 0.67 | 2.03 | 0.87 | 2.22 |
| COS-1 | --- | --- | 0.53 | 1.33 | 0.71 | 1.47 |
| HUVEC | --- | --- | 0.41 | 0.95 | 0.46 | 0.96 |
| +EP |  |  |  |  |  |  |
| MCF-7 | 0.64 | 1.69 | 1.26 | 2.82 | 1.33 | 3.13 |
| COS-1 | 0.54 | 1.36 | 1.13 | 1.62 | 1.19 | 1.88 |
| HUVEC | 0.39 | 0.92 | 1.00 | 1.32 | 1.08 | 1.37 |

Table S2. CC50 of Ca2+ and NPs incorporated into cells by electroporation (+EP) and non-electroporation (-EP). Experiments were performed with and without Ca2+chelation (i.e. +EGTA and –EGTA, respectively). Values were determined from curves displayed in Figures S2 and S3.

| Cell line | CC50 (mM) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Ca2+ |  | NPs <200 nm |  | NPs >200 nm |  |
|  | -EGTA | +EGTA | -EGTA | +EGTA | -EGTA | +EGTA |
| -EP, 24 h |  |  |  |  |  |  |
| MCF-7 | --- | --- | 0.68 | 2.20 | 0.92 | 2.33 |
| COS-1 | --- | --- | 0.57 | 1.32 | 0.69 | 1.48 |
| HUVEC | --- | --- | 0.45 | 0.97 | 0.48 | 1.00 |
| -EP, 48 h |  |  |  |  |  |  |
| MCF-7 | --- | --- | 0.72 | 2.36 | 1.14 | 2.45 |
| COS-1 | --- | --- | 0.63 | 1.38 | 0.79 | 1.58 |
| HUVEC | --- | --- | 0.49 | 1.06 | 0.59 | 1.09 |
| +EP, 24 h |  |  |  |  |  |  |
| MCF-7 | 0.62 | 1.68 | 1.29 | 2.69 | 1.39 | 2.94 |
| COS-1 | 0.53 | 1.33 | 1.17 | 1.66 | 1.26 | 1.82 |
| HUVEC | 0.42 | 1.01 | 1.01 | 1.30 | 1.12 | 1.38 |
| +EP, 48 h |  |  |  |  |  |  |
| MCF-7 | 0.69 | 2.08 | 1.40 | 2.97 | 1.46 | 3.20 |
| COS-1 | 0.60 | 1.36 | 1.24 | 1.75 | 1.33 | 2.15 |
| HUVEC | 0.46 | 1.11 | 1.13 | 1.36 | 1.27 | 1.48 |

Table S3. CC50 of NPs <200 nm coated with biophosphates and phosphonates .NPs were incorporated into cells by electroporation (+EP) and non-electroporation (-EP). The effect was evaluated with and without treatment of ALP+MgCl2. Values were determined according to curves displayed in Figure S4.

| Nanoparticle | CC50 (mM) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | MCF-7 |  | COS-1 |  | HUVEC |  |
|  | -EP | +EP | -EP | +EP | -EP | +EP |
| No-treatment |  |  |  |  |  |  |
| NP | 0.72 | 1.24 | 0.54 | 1.14 | 0.41 | 1.00 |
| NP/polyP | 1.29 | 1.39 | 1.12 | 1.26 | 1.01 | 1.17 |
| NP/ATMP | 1.17 | 1.34 | 1.02 | 1.22 | 0.80 | 1.10 |
| NP/(P2O7)4- | 0.96 | 1.32 | 0.80 | 1.18 | 0.61 | 1.07 |
| Treatment: ALP+MgCl2 |  |  |  |  |  |  |
| NP | 0.67 | 1.25 | 0.54 | 1.15 | 0.41 | 0.99 |
| NP/polyP | 0.71 | 1.32 | 0.64 | 1.24 | 0.47 | 1.06 |
| NP/ATMP | 1.20 | 1.34 | 1.02 | 1.22 | 0.86 | 1.17 |
| NP/(P2O7)4- | 0.69 | 1.33 | 0.60 | 1.19 | 0.46 | 1.02 |

Table S4. CC50 of NPs <200 nm coated with biophosphates and phosphonates .NPs were incorporated into cells by electroporation (+EP) and non-electroporation (-EP). The effect was evaluated with and without treatment of ALP+MgCl2. Values were determined according to curves displayed in Figures S5 y S6.

| Nanoparticle | CC50 (mM) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | MCF-7 |  | COS-1 |  | HUVEC |  |
|  | -EP | +EP | -EP | +EP | -EP | +EP |
| No-treatment, 24 h |  |  |  |  |  |  |
| NP | 0.67 | 1.29 | 0.58 | 1.17 | 0.44 | 1.02 |
| NP/polyP | 1.23 | 1.40 | 1.13 | 1.28 | 0.97 | 1.16 |
| NP/ATMP | 1.12 | 1.35 | 1.02 | 1.24 | 0.81 | 1.10 |
| NP/(P2O7)4- | 0.86 | 1.34 | 0.84 | 1.21 | 0.62 | 1.07 |
| No-treatment, 48 h |  |  |  |  |  |  |
| NP | 0.72 | 1.39 | 0.63 | 1.25 | 0.29 | 1.14 |
| NP/polyP | 1.29 | 1.47 | 1.19 | 1.34 | 1.01 | 1.28 |
| NP/ATMP | 1.18 | 1.42 | 1.09 | 1.32 | 0.88 | 1.16 |
| NP/(P2O7)4- | 0.97 | 1.38 | 0.94 | 1.27 | 0.70 | 1.14 |
| Treatment: ALP+MgCl2, 24 h |  |  |  |  |  |  |
| NP | 0.66 | 1.29 | 0.57 | 1.17 | 0.44 | 1.02 |
| NP/polyP | 0.72 | 1.34 | 0.63 | 1.20 | 0.48 | 1.06 |
| NP/ATMP | 1.21 | 1.36 | 1.02 | 1.24 | 0.82 | 1.17 |
| NP/(P2O7)4- | 0.69 | 1.33 | 0.60 | 1.18 | 0.46 | 1.04 |
| Treatment: ALP+MgCl2, 48 h |  |  |  |  |  |  |
| NP | 0.72 | 1.40 | 0.64 | 1.24 | 0.48 | 1.02 |
| NP/polyP | 0.76 | 1.38 | 0.68 | 1.28 | 0.54 | 1.06 |
| NP/ATMP | 1.27 | 1.41 | 1.09 | 1.31 | 0.95 | 1.16 |
| NP/(P2O7)4- | 0.74 | 1.38 | 0.64 | 1.26 | 0.51 | 1.03 |