Phytochemical profiling of Phragmites australis leaf extract and its nano-structural antioxidant, antimicrobial, and anticancer activities

Jeremiah O. Unuofin 1, Adewale O. Oladipo 1*, Garland K. More 2, Adeyemi O. Adeeyo 3, Hassan T. Mustapha 4, Titus A.M. Msagati 3, Sogolo L. Lebelo 1

1Department of Life and Consumer Sciences, College of Agriculture and Environmental Sciences, University of South Africa, Private Bag X06 Florida 1710, South Africa

2College of Agriculture and Environmental Sciences Laboratory, University of South Africa, Private Bag X06, Florida 1710, South Africa

3Institute for Nanotechnology and Water Sustainability (iNanoWS), College of Science, Engineering and Technology, University of South Africa, Private Bag X06 Florida 1710, South Africa

4Department of Chemical Sciences, Crescent University, Abeokuta, Ogun state, Nigeria

Author for correspondence: oladiao@unisa.ac.za

Fig. S1 Photographic image of aqueous P. australis extract synthesized AgNPs

Table S1 Zeta-potential and polydispersity index (PDI) of PA-AgNPs (Mean ± SD; n=3)

| Days | Particle size (nm) | PDI |  | Zeta potential (mV) |  |
| --- | --- | --- | --- | --- | --- |
| 0 | 52.4 ± 1.21 | 0.170 | -28.2 ± 2.75 |  |
| 1 | 52.7 ± 0.96 | 0.211 | -28.5 ± 2.16 |  |
| 2 | 52.6 ± 1.08 | 0.201 | -28.4 ± 2.33 |  |
| 3 | 53.1 ± 1.17 | 0.204 | -29.0 ± 3.25 |  |
| 4 | 52.9 ± 2.21 | 0.181 | -28.8 ± 3.41 |  |
| 5 | 53.0 ± 1.98 | 0.192 | -28.9 ± 2.74 |  |

Table S2 The calculated IC50 values (µg/mL) for PAE and PA-AgNPs in MCF-7 and A549 cells incubated for 24 h

| Samples | MCF-7 | A549 |
| --- | --- | --- |
| PAE | 74.68 | >100 |
| PA-AgNPs | 11.47 | ~121.2 |

Fig. S2 The percentage of the cell population in (A) MCF-7 and (B) A549 cells after incubation for 12 h with PAE and PA-AgNPs. Data presented as mean ± SD with the differences * P < 0.05 is considered significant