SUPPLEMENTARY INFORMATION

Green synthesis of Mn-MOFs with tunable optical and structural properties through ligand functionality and framework design

M. J. Robles-Águila1, J. A. Reyes-Avendaño2, R. Silva3, J.M. Bravo-Arredondo1,4*

1 Benemérita Universidad Autónoma de Puebla, Instituto de Ciencias, Centro de Investigación en Dispositivos Semiconductores, Edificio 105 C, Boulevard 14 Sur y Av. San Claudio, Col. San Manuel, C. P. 72570, Puebla, Pue., México.

2 Benemérita Universidad Autónoma de Puebla, Facultad de Ingeniería Química, Ciudad Universitaria, Av. San Claudio y 18 Sur, Col. Jardines de San Manuel, C. P. 72570, Puebla, Pue., México.

3 Benemérita Universidad Autónoma de Puebla, Instituto de Física, Ciudad Universitaria, Av. San Claudio y 18 Sur, Col. Jardines de San Manuel, C. P. 72570, Puebla, Pue., México.

4 Universidad Autónoma de Tlaxcala, Facultad de Ciencias Básicas, Ingeniería y Tecnología, De Apizaquito, 20 de Noviembre, 90401, Apizaco, Tlaxcala, México.

*Corresponding Author: josemanuel.bravo.a@uatx.mx

Table S1: Abbreviations, definitions and units used in this work.

| Abbreviation | Definition |
| --- | --- |
| ATR-FTIR | Attenuated Total Reflectance – Fourier-Transform Infrared Spectroscopy |
| BET | Brunauer–Emmett–Teller (surface area analysis) |
| BJH | Barret-Joyner-Halenda Method |
| DEF | Diethylformamide |
| DMF | Dimethylformamide |
| DoC | Degree of Crystallinity |
| DRS | Diffuse Reflectance Spectroscopy |
| DTA | Differential Thermal Analysis |
| Eg | Band Gap Energy |
| EDS | Energy-dispersive X-ray spectroscopy |
| FA | Fumaric Acid |
| FTIR | Fourier Transform Infrared Spectroscopy |
| LMCT | Ligand-to-Metal Charge Transfer |
| MA | Malic Acid |
| MOF | Metal–Organic Framework |
| Mn-FA | Manganese–Fumarate MOF |
| Mn-MA | Manganese–Malate MOF |
| Mn-MOFs | Manganese-based Metal–Organic Framework |
| Mn-SA | Manganese–Succinate MOF |
| Mn-TA | Manganese–Tartrate MOF |
| PXRD | Powder X-ray Diffraction |
| PL | Photoluminescence |
| SA | Succinic Acid |
| SBET | Specific Surface Area from BET |
| SEM | Scanning Electron Microscopy |
| TA | Tartaric Acid |
| TGA | Thermogravimetric Analysis |
| UV–Vis | Ultraviolet–Visible Spectroscopy |
| eV | Electron Volt |
| nm | Nanometer |
| nm-2 | Per Square Nanometer |
| Ả | Angstrom |
| μm | Micrometer |

Table S2. MOFs synthesized with biogenic C4 dicarboxylic ligands.

| Ligand | Reported MOFs (Metal centers) | Structure Type / Properties | Reference |
| --- | --- | --- | --- |
| FA | Al, Zr, Ce, Ni, Fe | Rigid frameworks, good thermal stability, catalytic uses | [34], [35], [36], [37], [38] |
| SA | Zr, Fe, Co, Cu, Y, La | Flexible, biocompatible, water adsorption, catalysis | [35], [39], [40], [41], [42] |
| MA | Ca, Zr, Zn, Mg | Low symmetry structures, Proton conduction, H-bonded layers, | [35], [43], [44], [45], [46] |
| TA | Zr, La, Nd, Fe, Ce | Chiral frameworks, strong chelation, high functionalization | [43], [47], [48], [49] |

Table S3. Lattice parameters (a, b, c), cell volume (V), average crystallite size from the Scherrer equation (L), dislocation density (δ), and micro-strain (ε) of pure synthetized Mn-MOFs.

| Structural parameter | Mn-FA | Mn-SA | Mn-MA | Mn-TA |
| --- | --- | --- | --- | --- |
| Crystal system | Monoclinic | Monoclinic | Triclinic | Monoclinic |
| a (Å) | 15.776 | 16.394 | 15.867 | 13.752 |
| b (Å) | 12.945 | 8.498 | 12.689 | 11.413 |
| c (Å) | 11.854 | 13.573 | 17.491 | 11.943 |
| α (°) | --- | --- | 65.883 | --- |
| β (°) | 108.788 | 109.393 | 131.005 | 90.861 |
| γ (°) | --- | --- | 145.287 | --- |
| V (Å3) | 2291.930 | 1783.750 | 1441.680 | 1874.250 |
| L (nm) | 28.060 | 26.480 | 19.900 | 24.480 |
| δ (nm-2 × 10-3) | 1.270 | 1.427 | 1.668 | 2.524 |
| ε (× 10-3) | 12.411 | 9.391 | 14.221 | 13.498 |
| DoC (%) | 92.610 | 90.720 | 78.690 | 86.730 |

Table S4. Morphology, particle size and at.% of Mn-MOFs as-synthesized.

| MOF | Morphology | Wide particle size distribution [μm] | Large particle size distribution [μm] | at% of Mn |
| --- | --- | --- | --- | --- |
| Mn-FA | Irregular polyhedra aggregates | 0.49 ± 0.10 | 1.08 ± 0.03 | 9.87 ± 1.08 |
| Mn-SA | Hexagonal rods | 9.78 ± 0.47 | 17.44 ± 0.53 | 10.15 ± 2.93 |
| Mn-MA | Rounded grains | 5.11 ± 0.28 | 7.93 ± 0.08 | 8.79 ± 0.80 |
| Mn-TA | Irregular polyhedra | 2.74 ± 0.07 | 5.52 ± 0.32 | 8.75 ± 0.98 |

Figure S1. EDS element analysis of Mn-MOFs with at% of Mn.

Figure S2. N2 adsorption isotherms of Mn-MOFs.

Table S5. Textural parameters of Mn-MOFs.

| MOF | SBET (m2/g) | Vads (cm3/g) | Vp (cm3/g) | Average Pore Diameter (nm) |
| --- | --- | --- | --- | --- |
| Mn-FA | 2.39 | 0.5499 | 9.93E-03 | 1.659 |
| Mn-SA | 2.66 | 0.6116 | 2.07E-02 | 3.110 |
| Mn-MA | 1.52 | 0.3488 | 1.13E-02 | 2.968 |
| Mn-TA | 2.20 | 0.5047 | 1.88E-02 | 3.417 |

Figure S3. Pore size distribution of Mn-MOFs.

Table S6. Information summarized from TGA and DTA analysis of Mn-MOFs decomposition.

| MOF | Tonset (°C) | Tmax (°C) | % Total water (free, bound) | % Free Ligand | % Ligand decomposed | Residue (%) at 800 °C |
| --- | --- | --- | --- | --- | --- | --- |
| Mn-FA | 350 | 530 | 1.00 | --- | 42.08 | 51.60 |
| Mn-SA | 300 | 515 | 11.78 | 10.09 | 25.01 | 49.66 |
| Mn-MA | 235 | 513 | 15.16 | 8.90 | 27.49 | 39.53 |
| Mn-TA | 215 | 451 | 1.70 | --- | 55.86 | 39.70 |

Table S7. Information summarized from infrared analysis of Mn-MOFs.

| MOF | νas (COO-) | νs (COO-) | Δν = νas - νs | Bonding mode [58] |
| --- | --- | --- | --- | --- |
| Mn-FA | 1550 | 1358 | 192 | Monodentate |
| Mn-SA | 1546 | 1406 | 140 | Quelating Bidentate |
| Mn-MA | 1563 | 1420 | 143 | Quelating Bidentate |
| Mn-TA | 1579 | 1411 | 168 | Bridging Bidentate |

Figure S4. DRS spectra of Mn-FA (black), Mn-SA (red), Mn-MA (blue), and Mn-TA (green).

Figure S5. Normalized PL spectra of Mn-FA (black), Mn-SA (red), Mn-MA (blue), and Mn-TA (green) excited under UV light at 300 nm.