Supplementary material

Effect of electron-beam radiation and other sterilization techniques on structural, mechanical and microbiological properties of thermoplastic starch blend

Authors: Anna Iuliano1,2*, Agata Fabiszewska1, Katarzyna Kozik1, Magdalena Rzepna3, Justyna Ostrowska4, Maciej Dębowski2, Andrzej Plichta2

Affiliations:

1Department of Chemistry, Institute of Food Sciences, Warsaw University of Life Sciences – SGGW, Nowoursynowska 159c, 02-776 Warsaw, Poland

2Faculty of Chemistry, Warsaw University of Technology, Noakowskiego 3, 00-664 Warsaw, Poland, *aiuliano@ch.pw.edu.pl

3Institute of Nuclear Chemistry and Technology, Dorodna 16, Warsaw 03-195, Poland

4Department of Organic Technologies, The Łukasiewicz Research Network – New Chemical Syntheses Institute, al. Tysiąclecia Państwa Polskiego 13A, 24-110 Puławy, Poland

Fig. S1. DSC curves of the TPS/PBS blend before and after sterilization recorded during the 2nd heating carried out at 20 C min−1 rate.

Fig. S2. GPC chromatograms of the PBS fraction in the PBS/TPS blend: non-irradiated and irradiated with a dose of 5 kGy (a), 13 kGy (b) and 26 kGy (c).

Fig. S3. SEM images of the TPS/PBS surface after 7 days of degradation in the presence of commercial -amylase: non-irradiated (a) and irradiated with a dose of 26 kGy (b).

Fig. S4. Influence of incubation time on the activity of amylase derived from B. subtilis.

Table S1. The effect of degradation process on the mass of starch released to the degradation solution.

| Time of degradation | Mass of starch g starch /g specimen (%) |  |  |  |
| --- | --- | --- | --- | --- |
|  | 0 kGy | 5 kGy | 13 kGy | 26 kGy |
| 1 day | 0.24 ± 0.03 | 0.28 ±0.03 | 0.29 ±0.02 | 0.29 ±0.02 |
| 2 day | 0.27 ±0.02 | 0.22 ±0.04 | 0.26 ±0.03 | 0.26 ±0.05 |
| 3 day | 0.14 ± 0.04 | 0.17 ±0.03 | 0.28 ±0.05 | 0.27 ±0.02 |
| 4 day | 0.13 ± 0.01 | 0.27 ± 0.04 | 0.18 ± 0.02 | 0.20 ± 0.02 |
| 7 day | 0.15 ±0.01 | 0.19 ±0.01 | 0.22 ±0.03 | 0.21 ±0.06 |