Table S2. Summary table of phase transition temperatures for each of the tested polyesters after the I, II and III cycles of injection moulding processing, composted for 0, 1, 2, 3 and 6 months.

| 0 months |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Material | Injection cycle no | Tg | ∆Cp | Tm | ∆Hm | Tc/Tcc | ∆Hc/∆Hcc | Xc |
|  |  | ºC | J/g ∙ K | °C | J/g | °C | J/g | % |
| PLA | I | 60.3 | 0.48 | 175.7 | 56.1 | -/100.6 | -/38.1 | 52.9 |
|  | II | 59.3 | 0.21 | 175.4 | 57.9 | 105.3/- | 49.2/- | 54.6 |
|  | III | 59.0 | 0.16 | 175.8 | 58.4 | 104.5/- | 51.2/- | 55.2 |
| PEF | I | 86.4 | 0.42 | - | - | -/- | -/- | - |
|  | II | 84.3 | 0.40 | - | - | -/- | -/- | - |
|  | III | 53.2 | 0.30 | 167.3 | 8.2 | -/140.4 | -/1.8 | 6.0 |
| PET | I | 85.5 | 0.24 | 248.4 | 42.2 | 203.6/- | 38.0/- | 30.1 |
|  | II | 82.4 | 0.22 | 248.6 | 43.0 | 209.3/- | 39.8/- | 30.7 |
|  | III | 83.0 | 0.20 | 244.9 | 43.3 | 209.2/- | 42.3/- | 30.9 |
| PTF | I | 56.1 | 0.39 | - | - | -/- | -/- | - |
|  | II | 56.1 | 0.38 | 172.0 | 4.9 | -/- | -/- | 3.5 |
|  | III | 52.6 | 0.33 | 173.3 | 19.6 | -/132.6 | -/18.5 | 13.9 |
| PTT | I | 61.5 | 0.16 | 228.0 | 49.4 | 198.7/- | 50.9/- | 33.8 |
|  | II | 61.1 | 0.14 | 228.6 | 49.8 | 197.9/- | 50.9/- | 34.1 |
|  | III | 60.9 | 0.16 | 228.2 | 51.1 | 195.5/- | 51.6/- | 35.0 |
| PHF | I | 18.7 | 0.21 | 146.3 | 54.3 | 112.2/- | 52.8/- | 37.9 |
|  | II | 16.1 | 0.18 | 146.7 | 52.8 | 117.7/- | 51.9/- | 36.9 |
|  | III | 15.2 | 0.14 | 145.9 | 52.7 | 112.2/- | 50.8/- | 36.8 |
| PHT | I | 12.8 | 0.19 | 138.8; 147.5 | 51.2 | 121.6/- | 47.4/- | 35.0 |
|  | II | 12.1 | 0.18 | 134.0; 141.0 | 50.7 | 121.5/- | 47.1/- | 34.8 |
|  | III | 11.6 | 0.16 | 134.0; 147.1 | 50.1 | 121.0/- | 47.4/- | 34.3 |

Tg – glass transition temperature, ΔCp - change of heat capacity, Tm – melting temperature, ΔHm – melting enthalpy, Tc/Tcc – crystallization/cold crystallization temperature, ΔHc/ΔHcc – crystallization/cold crystallization enthalpy, Xc – degree of crystallinity

| 1 month |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Material | Injection cycle no | Tg | ∆Cp | Tm | ∆Hm | Tc/Tcc | ∆Hc/∆Hcc | Xc |
|  |  | ºC | J/g ∙ K | °C | J/g | °C | J/g | % |
| PLA | I | 59.2 | 0.46 | 174.9 | 57.1 | -/100.1 | -/39.0 | 53.9 |
|  | II | 58.4 | 0.20 | 175.1 | 56.2 | 105.1/- | 49.8/- | 53.0 |
|  | III | 58.1 | 0.14 | 175.0 | 59.0 | 106.3/- | 50.8/- | 55.7 |
| PEF | I | 86.4 | 0.41 | - | - | -/- | -/- | - |
|  | II | 84.2 | 0.40 | - | - | -/- | -/- | - |
|  | III | 53.0 | 0.31 | 166.8 | 10.1 | -/134.2 | -/3.8 | 7.4 |
| PET | I | 84.5 | 0.21 | 245.5 | 42.6 | 203.2/- | 38.2/- | 30.4 |
|  | II | 81.9 | 0.19 | 246.0 | 43.6 | 209.3/- | 39.4/- | 31.1 |
|  | III | 81.4 | 0.18 | 246.6 | 43.9 | 210.6/- | 40.2/- | 31.3 |
| PTF | I | 55.7 | 0.38 | - | - | -/- | -/- | - |
|  | II | 55.4 | 0.36 | 172.1 | 8.7 | -/- | -/- | 6.2 |
|  | III | 51.8 | 0.31 | 173.3 | 21.2 | -/130.1 | -/20.0 | 13.9 |
| PTT | I | 61.1 | 0.15 | 228.0 | 49.2 | 198.1/- | 50.1/- | 33.7 |
|  | II | 60.9 | 0.14 | 228.1 | 49.3 | 197.6/- | 51.1/- | 33.7 |
|  | III | 60.1 | 0.12 | 228.6 | 50.9 | 195.5/- | 50.5/- | 34.9 |
| PHF | I | 18.1 | 0.20 | 146.2 | 53.2 | 112.2/- | 52.9/- | 37.2 |
|  | II | 15.7 | 0.16 | 146.5 | 52.2 | 117.7/- | 50.9/- | 36.5 |
|  | III | 15.0 | 0.13 | 145.1 | 53.5 | 112.2/- | 51.6/- | 37.4 |
| PHT | I | 11.3 | 0.18 | 137.8; 147.4 | 51.2 | 120.5/- | 48.1/- | 35.0 |
|  | II | 11.1 | 0.17 | 134.9; 143.0 | 50.7 | 121.1/- | 48.0/- | 34.8 |
|  | III | 11.1 | 0.16 | 134.6; 145.6 | 50.1 | 120.9/- | 47.6/- | 34.3 |

Tg – glass transition temperature, ΔCp - change of heat capacity, Tm – melting temperature, ΔHm – melting enthalpy, Tc/Tcc – crystallization/cold crystallization temperature, ΔHc/ΔHcc – crystallization/cold crystallization enthalpy, Xc – degree of crystallinity

| 2 months |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Material | Injection cycle no | Tg | ∆Cp | Tm | ∆Hm | Tc/Tcc | ∆Hc/∆Hcc | Xc |
|  |  | ºC | J/g ∙ K | °C | J/g | °C | J/g | % |
| PLA | I | 59.2 | 0.41 | 174.9 | 59.1 | -/101.2 | -/39.0 | 55.8 |
|  | II | 57.3 | 0.17 | 174.3 | 58.1 | 105.1/- | 49.8/- | 54.8 |
|  | III | 56.9 | 0.11 | 171.2 | 61.8 | 106.3/- | 50.8/- | 58.3 |
| PEF | I | 86.2 | 0.41 | - | - | -/- | -/- | - |
|  | II | 80.0 | 0.39 | 203.1 | 21.2 | -/152.7 | -/13.6 | 15.4 |
|  | III | 38.2 | 0.30 | 166.5 | 22.8 | -/125.4 | -/7.9 | 16.6 |
| PET | I | 84.2 | 0.20 | 246.4 | 43.1 | 203.1/- | 37.9/- | 30.7 |
|  | II | 80.6 | 0.18 | 244.2 | 43.2 | 208.5/- | 39.2/- | 30.8 |
|  | III | 80.1 | 0.17 | 243.6 | 44.2 | 211.4/- | 42.3/- | 31.6 |
| PTF | I | 54.2 | 0.31 | 170.1 | 2.1 | -/- | -/- | 1.5 |
|  | II | 53.7 | 0.30 | 172.1 | 9.1 | -/- | -/- | 6.5 |
|  | III | 51.8 | 0.30 | 173.3 | 25.6 | -/128.6 | -/20.7 | 18.1 |
| PTT | I | 58.9 | 0.14 | 228.3 | 49.7 | 197.6/- | 51.2/- | 34.0 |
|  | II | 57.1 | 0.13 | 227.9 | 49.9 | 197.5/- | 51.1/- | 34.1 |
|  | III | 55.0 | 0.10 | 227.2 | 50.1 | 195.2/- | 50.8/- | 34.3 |
| PHF | I | 17.3 | 0.19 | 146.4 | 52.6 | 111.6/- | 49.1/- | 36.8 |
|  | II | 15.4 | 0.14 | 146.1 | 52.2 | 110.7/- | 50.8/- | 36.5 |
|  | III | 14.6 | 0.13 | 145.3 | 53.4 | 110.4/- | 49.2/- | 37.3 |
| PHT | I | 11.1 | 0.18 | 136.9; 146.2 | 52.8 | 119.1/- | 48.8/- | 36.1 |
|  | II | 10.7 | 0.17 | 135.9; 144.0 | 51.9 | 120.4/- | 48.2/- | 35.5 |
|  | III | 9.2 | 0.15 | 135.8; 144.0 | 52.6 | 119.7/- | 48.5/- | 36.0 |

Tg – glass transition temperature, ΔCp - change of heat capacity, Tm – melting temperature, ΔHm – melting enthalpy, Tc/Tcc – crystallization/cold crystallization temperature, ΔHc/ΔHcc – crystallization/cold crystallization enthalpy, Xc – degree of crystallinity

| 3 months |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Material | Injection cycle no | Tg | ∆Cp | Tm | ∆Hm | Tc/Tcc | ∆Hc/∆Hcc | Xc |
|  |  | ºC | J/g ∙ K | °C | J/g | °C | J/g | % |
| PLA | I | 59.0 | 0.41 | 175.1 | 60.6 | -/100.3 | -/40.2 | 57.1 |
|  | II | 52.8 | 0.16 | 170.2 | 61.1 | 105.3/- | 54.8/- | 57.7 |
|  | III | 52.1 | 0.10 | 169.7 | 63.0 | 106.2/- | 56.1/- | 59.5 |
| PEF | I | 85.0 | 0.41 | - | - | - | -/- | - |
|  | II | 75.2 | 0.40 | 203.8 | 31.5 | -/159.1 | -/12.1 | 23.0 |
|  | III | 37.9 | 0.25 | 161.7 | 32.9 | -/123.1 | -/16.8 | 24.0 |
| PET | I | 82.8 | 0.19 | 245.5 | 41.7 | 203.0/- | 37.2/- | 29.7 |
|  | II | 80.1 | 0.16 | 246.0 | 42.6 | 208.2/- | 39.2/- | 30.4 |
|  | III | 79.8 | 0.15 | 243.4 | 44.1 | 217.4/- | 50.1/- | 31.5 |
| PTF | I | 53.1 | 0.30 | 170.1 | 4.0 | -/- | -/- | 2.8 |
|  | II | 50.1 | 0.27 | 172.1 | 11.6 | -/- | -/- | 8.2 |
|  | III | 43.6 | 0.21 | 172.3 | 27.4 | 143.7/125.7 | 8.9/23.7 | 19.3 |
| PTT | I | 55.6 | 0.13 | 227.3 | 50.2 | 197.3/- | 50.3/- | 34.4 |
|  | II | 52.4 | 0.11 | 227.2 | 51.3 | 196.9/- | 51.9/- | 35.1 |
|  | III | 51.2 | 0.10 | 228.0 | 52.3 | 195.1/- | 52.0/- | 35.8 |
| PHF | I | 16.6 | 0.19 | 145.6 | 55.1 | 110.9/- | 50.2/- | 38.6 |
|  | II | 15.1 | 0.14 | 145.1 | 54.6 | 108.6/- | 49.5/- | 38.2 |
|  | III | 13.2 | 0.11 | 144.1 | 56.2 | 109.9/- | 52.2/- | 39.3 |
| PHT | I | 11.0 | 0.17 | 137.1; 145.9 | 54.4 | 118.8/- | 46.5/- | 37.3 |
|  | II | 9.5 | 0.14 | 136.9; 145.7 | 53.7 | 118.7/- | 46.6/- | 36.8 |
|  | III | 8.7 | 0.13 | 137.3; 146.1 | 56.3 | 113.8/- | 46.4/- | 38.6 |

Tg – glass transition temperature, ΔCp - change of heat capacity, Tm – melting temperature, ΔHm – melting enthalpy, Tc/Tcc – crystallization/cold crystallization temperature, ΔHc/ΔHcc – crystallization/cold crystallization enthalpy, Xc – degree of crystallinity

| 6 months |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Material | Injection cycle no | Tg | ∆Cp | Tm | ∆Hm | Tc/Tcc* | ∆Hc/∆Hcc* | Xc |
|  |  | ºC | J/g ∙ K | °C | J/g | °C | J/g | % |
| PLA | I | 58.5 | 0.38 | 174.7 | 63.1 | -/102.1 | -/45.3 | 59.6 |
|  | II | 51.7 | 0.13 | 172.2 | 66.2 | 106.2/- | 58.2/- | 62.4 |
|  | III | 51.0 | 0.09 | 169.3 | 68.2 | 106.9/- | 60.0/- | 64.3 |
| PEF | I | 84.5 | 0.40 | - | - | -/- | -/- | - |
|  | II | 74.8 | 0.46 | 203.6 | 32.5 | -/169.2 | -/8.5 | 23.7 |
|  | III | 34.4 | 0.21 | 160.6 | 37.4 | -/116.2; -/16.8. | -/20.7 | 27.3 |
| PET | I | 81.6 | 0.18 | 246.6 | 41.8 | 203.2/- | 38.8/- | 29.8 |
|  | II | 80.0 | 0.14 | 244.5 | 42.5 | 207.3/- | 39.0/- | 30.3 |
|  | III | 79.1 | 0.12 | 243.1 | 43.1 | 220.4/- | 56.7/- | 30.8 |
| PTF | I | 52.3 | 0.26 | 170.8 | 8.3 | -/- | -/- | 5.8 |
|  | II | 49.7 | 0.21 | 171.6 | 14.7 | -/141.2 | -/5.2 | 10.4 |
|  | III | 42.7 | 0.20 | 172.0 | 42.7 | 144.8/117.1 | 25.6/31.9 | 30.1 |
| PTT | I | 51.4 | 0.12 | 226.6 | 52.8 | 195.8/- | 52.8/- | 36.2 |
|  | II | 46.2 | 0.11 | 227.5 | 52.4 | 195.5/- | 53.9/- | 35.9 |
|  | III | 43.5 | 0.09 | 225.3 | 53.2 | 194.7/- | 54.9/- | 36.4 |
| PHF | I | 15.7 | 0.18 | 145.5 | 56.7 | 108.6/- | 51.2/- | 39.6 |
|  | II | 14.9 | 0.13 | 145.2 | 56.1 | 107.4/- | 50.8/- | 39.2 |
|  | III | 12.6 | 0.09 | 143.5 | 58.7 | 106.9/- | 52.6/- | 41.0 |
| PHT | I | 10.3 | 0.12 | 136.0; 144.3 | 54.6 | 118.8/- | 47.3/- | 37.4 |
|  | II | 8.5 | 0.11 | 136.6; 146.1 | 56.8 | 114.7/- | 48.5/- | 38.9 |
|  | III | 7.0 | 0.11 | 136.3; 145.1 | 57.9 | 111.4/- | 48.8/- | 39.7 |

Tg – glass transition temperature, ΔCp - change of heat capacity, Tm – melting temperature, ΔHm – melting enthalpy, Tc/Tcc – crystallization/cold crystallization temperature, ΔHc/ΔHcc – crystallization/cold crystallization enthalpy, Xc – degree of crystallinity