SUPPLEMENTARY INFORMATION

Bio-Polyethylene Furanoate Production in Latin America as a Response to the Current Needs for Sustainable Food Packaging.

Lory Ireri Martínez Bello 1, Vimanely Yaneth Vázquez Cuevas 1, Moisés Alberto González-Contreras 2, Diego Gomez-Maldonado 3, Maribel Hernández-Guerrero 4*.

1 Bachelor's Degree in Biological Engineering, Universidad Autónoma Metropolitana, Unidad Cuajimalpa, Vasco de Quiroga 4871, Cuajimalpa, 05348, Mexico City, Mexico.

2 Department of Biotechnological and Environmental Sciences, Universidad Autónoma de Guadalajara; Av. Patria 1201, 45129, Zapopan, Mexico.

3 Fiber and Biopolymer Research Institute, Department of Plant & Soil Science, Texas Tech University, Lubbock, Texas, USA.

4 Department of Processes and Technology, Unidad Cuajimalpa, Vasco de Quiroga 4871, Cuajimalpa, 05348, Mexico City, Mexico.

dgomezma@ttu.edu, mhernandez@cua.uam.mx

TABLE S1.  Yield and selectivity data for the processes.

| ​Process | ​Catalyst | ​Yield (%) | ​Selectivity (%) | ​Reference |
| --- | --- | --- | --- | --- |
| ​Fructose to HMF | ​Concentrated H2SO4 | ​90 | ​90 | ​105 |
| ​Oxidation of HMF to FDCA | ​Pt/TiO2 | ​>90 | ​--------- | ​41 |
|  | ​Au/Ht | ​>90 | ​--------- | ​41 |
|  | ​Ru/C | ​93 | ​--------- | ​41 |
| ​Production of EG | ​Non-catalytic hydrolysis | ​98 | ​98 | ​106 |
|  | ​Hydrolysis H2SO4, Na, K, NH4, acid zeolite | ​95 | ​90 | ​106 |
|  | ​Alkaline Halide or NH4Cl | ​98 | ​95 | ​106 |
|  | ​Palladium Complexes PdCl2+NaNO3 | ​90 | ​95 | ​106 |

TABLE S2. Operating conditions.

| Process | Time (min) | Temperature (°C) | Pressure (atm) |
| --- | --- | --- | --- |
| Obtaining Fructose | 20 | 98 | ---- |
| Obtaining HMF | 10 | 150 | 38.48 |
| Oxidation of HMF to FDCA | 150 | 100 | ---- |
| Oxidation to obtain EG | ---- | 220-275 | 1-2.2 |
| Bio-PEF polymerization | 60-120 | 160-240 | 0.0009868 |