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Results and Discussion 
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Fig. S.1 Particle Size Distribution for the eight experiments using different solvents, ethyl acetate (a) and dichloromethane (DCM)(b) 
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Fig. S.2 TGA curves for ethyl cellulose (EC), (PVA) and unloaded microparticles (formulations E2/A and E4/B)


Table S.1. Results from the regression analysis for quercetin and OP extract quantification in ultrapure water and octanol.
	
	Medium
	λ (nm)
	Regression Equation
	Correlation Coefficient

	Quercetin
	UPW
	315
	Abs = (0.013 ± 0.000)C + (0.028 ± 0.008)
	0.997

	
	Octanol
	215
	Abs = (0.078 ± 0.001)C + (0.07 ± 0.005)
	0.999

	OP extract
	UPW
	290
	Abs = (0.008 ± 0.000)C + (0.031 ± 0.016)
	0.992

	
	Octanol
	300
	Abs = (0.015 ± 0.000)C + (-0.202 ± 0.020)
	0.997


Abs: Absorbance; C: Concentration of bioactive compound (mg∙mL-1); OP: Onion peel; UPW: Ultrapure water.
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