Supplementary Information

Synthesis and Characterization of Eco-Friendly Chitin-Based Superabsorbent Polymers for Fertilizer Slow Release, Water Absorption Kinetics, and Plant Growth Enhancement

a Refilwe Mogale,a, b Janine Blignaut, a Elham Jalali,a Marietjie Schutte-Smith,a Hendrik. G. Visser,a* and Elizabeth Erasmusa

Table S1: The zeta potential (mV) values at different pHs.

|  | Zeta Potential (mV) |  |  |  |
| --- | --- | --- | --- | --- |
| pH | 3 | 5 | 7 | 11 |
| Shellfish-chitin-No Urea (SCNU) | -6.19 | -11.12 | -24.87 | -40.21 |
| Shellfish-chitin-Urea (SCU) | -5.59 | -15.67 | -22.66 | -43.25 |

Figure S1: Urea slow-release behaviour of SCNU in deionised water, as measured by UV/Vis spectroscopy over 24 hours.

Figure S2: The EDS of SCU.

Figure S3: The EDS od SCNU.

Figure S4: Root development of radish seedlings grown in soil mixed with SCU enriched with indole butyric acid, observed on day 7 after planting.