Natural zeolites as host matrices for the development of low-cost and stable thermochemical energy storage materials

Lia Kouchachvilia*, D.A. Bardya, Reda Djebbara, and LuVerne E.W. Hoggb

a Natural Resources Canada, CanmetENERGY-Ottawa, 1 Haanel Drive, K1A 1M1, Ottawa, ON,

b ZMM® Canada Minerals Corp., 6459 Mack Road, Peachland, British Columbia, Canada, V0H 1X8

*corresponding author

Email: lia.kouchachvili@nrcan-rncan.gc.ca

Supplementary Information

Table S1: Results of XRF analysis of selected zeolites

|  | 13XBF | TC-HPC | J-HPC | NS-S |
| --- | --- | --- | --- | --- |
| SiO2 | 37.88 wt% | 48.05 wt% | 51.72 wt% | 48.63 wt% |
| Al2O3 | 26.55 wt% | 18.80 wt% | 16.91 wt% | 11.87 wt% |
| Fe2O3 | 0.09 wt% | 0.43 wt% | 1.01 wt% | 1.08 wt% |
| TiO2 | 0.30 wt% | <0.03 wt% | 0.06 wt% | 0.11 wt% |
| P2O5 | <0.03 wt% | <0.03 wt% | 0.03 wt% | <0.03 wt% |
| CaO | 0.09 wt% | 9.93 wt% | 6.43 wt% | 6.40 wt% |
| MgO | <0.20 wt% | 1.35 wt% | 2.05 wt% | 1.75 wt% |
| SO3 | <0.10 wt% | <0.10 wt% | <0.10 wt% | 5.93 wt% |
| Na2O | 14.08 wt% | 5.34 wt% | 0.37 wt% | 0.75 wt% |
| K2O | <0.02 wt% | 0.37 wt% | 1.71 wt% | 0.56 wt% |
| Barium | <250 ppm | 327 ppm | 3551 ppm | 90626 ppm |
| Strontium | <50 ppm | 1255 ppm | 4647 ppm | 3822 ppm |
| Vanadium | <50 ppm | <50 ppm | <50 ppm | 114 ppm |
| Nickel | <50 ppm | <50 ppm | <50 ppm | <50 ppm |
| Manganese | <50 ppm | 284 ppm | 269 ppm | 485 ppm |
| Chromium | <50 ppm | <50 ppm | <50 ppm | <50 ppm |
| Copper | <30 ppm | <30 ppm | <30 ppm | <30 ppm |
| Zinc | <30 ppm | <30 ppm | <30 ppm | <30 ppm |
| Loss on Fusion | 20.96 wt% | 15.50 wt% | 18.84 wt% | 13.41 wt% |
| Sum | 99.96 wt | 99.95 wt% | 99.95 wt | 99.98 wt% |

Table S2: Results of XRD analysis of the selected zeolites

| Sample | Phase ID | Chemical Formula | PDF-# |
| --- | --- | --- | --- |
| TC-HPC | Analcime | Na(AlSi2O6)*H2O | 98-000-0078 |
|  | Calcite | CaCO3 | 04-012-0489 |
|  | Chabazite-Ca ¦ Chabazite (Ca, Na) | Ca1.57 Na0.49Al 3.39 Si 8.55 O24(H2O)11.53 | 01-079-9984 |
|  | Faujasite-Ca, syn ¦ Zeolite X, (Ca) | (Ca,Na)·Al2Si 2.5 O9·6.4H2O | 00-038-0232 |
|  | Quartz, syn | SiO2 | 01-085-0795 |
|  | Thomsonite-Ca | Na2.2 Ca 2.9 Mg 0.2 Al 8.4 Si 11.6 O 40 (H2O)11.8 | 04-017-0450 |
| J-HPC | Chabazite-Ca | Ca2Al4Si8O24*12H2O | 00-034-0137 |
|  | Heulandite-Ca | Ca(Al2Si7O18)*6H2O | 00-014-0248 |
|  | Phillipsite-Ca I Phillipsite, dipotassium Dicalcium tecto-hexaalumodecasilicate dodecahydrate | K2Ca2(Al6Si10O32)(H2O)12 | 01-076-2791 |
| Stilbite | Baryte, syn | BaSO4 | 04-007-7651 |
|  | Clinoptilolite-Na ¦ Clinoptilolite-(Na) | (Na,K,Ca)6(Si,Al)36O72·20H2O | 00-025-1349 |
|  | Dolomite | CaMg(CO3)2 | 01-075-1759 |
|  | Faujasite-Ca, syn | (Ca,Na)·Al2Si 2.5 O9·6.4H2O | 00-038-0232 |
|  | Fayalite, syn | Fe2(SiO4) | 01-080-0947 |
|  | Quartz | SiO2 | 98-000-0369 |
|  | Stilbite-Ca ¦ Stilbite (Ca) | Na1.35 Ca1.7 Mg 0.1 Al 4.95 Si 13.05 O36(H2O)12.25 | 04-011-6598 |
| 13XBFK | Corundum, syn | Al2O3 | 04-003-5819 |
|  | Faujasite-Na, syn ¦ Species R, Faujasite | Na2Al2Si 2.4 O 8.8 ·6.7H2O | 00-012-0246 |
|  | Sodium Aluminum Silicate | Na 1.84 Al 2 Si 2.88 O 9.68 | 00-048-0731 |