Supplementary information

Use of WetSEM® capsules for convenient multimodal scanning electron microscopy, energy dispersive X-ray analysis, and micro Raman spectroscopy characterisation of technetium oxides.

D. J. Bailey,1* M. C. Stennett,1 J. Heo,2,3 N. C. Hyatt1*

*Corresponding author: d.j.bailey@sheffield.ac.uk, n.c.hyatt@sheffield.ac.uk

1Department of Materials Science and Engineering, University of Sheffield, Mappin Street, Sheffield, S1 3JD, United Kingdom

2Department of Materials Science and Engineering, Pohang University of Science and Technology (POSTECH), Pohang, Gyeongbuk 790-784, South Korea

3Division of Advanced Nuclear Engineering, Pohang University of Science and Technology (POSTECH), Pohang, Gyeongbuk 790-784, South Korea

Fig. S1: X-ray diffraction pattern of synthesised Ti0.9Tc0.1O2.  Tick marks show allowed reflections for TiO2 (rutile).

Fig. S2: X-ray diffraction pattern of synthesised TlTcO4.  Tick marks show allowed reflections for TlTcO4, minimum 1 % of maximum intensity.

Table S1: Raman shifts and tentative mode/symmetry assignments for TlTcO4, assignments based on TlReO4. Rot. = rotation, Sci. = scissoring, Wagg. = wagging, Rock. = rocking, Twist. = twisting, Asym. Str. = Asymmetric stretching and Sym. Str = symmetric stretching [1].

| Raman shift (cm-1) | Symmetry | Assignment |
| --- | --- | --- |
| 67.34 | Eg | Rot. of TcO4 |
| 95.04 | Bg | Rot. of TcO4 |
| 316.76 | Ag | Sci. in TcO4 |
| 334.27 | Eg | Wagg., Rock. in TcO4 |
| 344.82 | Bg | Sci., Twist. in TcO4 |
| 864.88 | Eg | Asym. Str. of Tc-O bonds |
| 886.28 | Bg | Asym. Str. of Tc-O bonds |
| 900.05 | Ag | Sym. Str of all bonds in TcO4 |

References

- Mondal S, Vaitheeswaran G, Kennedy BJ, et al (2020) Crystal structure and phase transition of TlReO4: a combined experimental and theoretical study. J Phys Condens Matter 33:. https://doi.org/10.1088/1361-648X/abb651