Supplementary Information

Hybrid Inorganic-Organic Fluorescent Silica Nanoparticles – Influence of Dye Binding Modes on Dye Leaching

Nadja Klippel1, Gregor Jung2, Guido Kickelbick1,*

1 Saarland University, Inorganic Solid-State Chemistry, Campus C4 1, 66123 Saarbrücken, Germany

2 Saarland University, BioPhysical Chemistry, Campus B2 2, 66123 Saarbrücken, Germany

*Corresponding author: E-mail: guido.kickelbick@uni-saarland.de

Contents

Experimental Section	2

Fluorescence anisotropy	2

CP/MAS spectra	3

References	5

# Experimental Section

Phosphate-buffered saline (PBS buffer). The buffer was prepared by dissolving 8.00 g NaCl, 0.20 g KCl, 1.44 g Na2HPO4 and 0.24 KH2PO4 in 1 L distilled water. The pH was adjusted to pH 7.4 by adding small amounts of a HCl solution.

# Fluorescence anisotropy

Table S1: Overview anisotropy values of the free dyes and particles

| Dye | free dye | Core NPs | Core-shell NPs |
| --- | --- | --- | --- |
| Uranine | 0.023 ± 0.002 | 0.037 ± 0.003 | 0.028 ± 0.002 |
| FITC | 0.027 ± 0.002 | 0.316 ± 0.004 | 0.227 ± 0.004 |
| Rhodamine B | 0.026 ± 0.002 | 0.034 ± 0.001 | 0.045 ± 0.004 |
| RBITC | 0.044 ± 0.003 | 0.410 ± 0.005 | 0.352 ± 0.009 |

# CP/MAS spectra

Table S2: Assignment of CP/MAS signals

| Functional group |  | Signals [ppm] | Literature |
| --- | --- | --- | --- |
| Ethoxy- | 13C: 16.68, 58.57 29Si: - | [1] |
| Trimethylsilyl- | 13C: -1.29 29Si: 12.99 (M1) | [1] |
| Dodecylsilyl-Octadecylsilyl- | 13C: 12.19, 22.06, 29.09, 31.62, 58.57 29Si: -66.31 (T3), -56.91 (T2) | [2, 3] |
| 2-[Methoxy(poly-ethyleneoxy)6-9-propyl]silyl- | 13C: not measured. 29Si: -110.74, -101.87, -93.26, -58.92 | [4] |

Figure S1: 13C-CP/MAS NMR of fluorescent silica particles with alkyl surface functional-izations with different chain lengths. Signals at 16.6 ppm and 58.5 ppm are from surface bound ethoxy groups, * are signals from toluene which was used as solvent for alkylation.

Figure S2: 29Si-CP/MAS NMR of alkylated particles. M1 results of Si(Me)3-groups, T3 indicates connection via three covalent bonds (alkyl-Si-O≡silica), T2 means two covalent bonds to the silica network (alkyl-Si(OHsilica)).

# References

1. 	Yokogawa H, Yokoyama M (1995) Hydrophobic silica aerogels. J Non Cryst Solids 186:23–29. https://doi.org/10.1016/0022-3093(95)00086-0

2. 	Zhou WJ, Fang L, Fan Z, et al (2014) Tunable catalysts for solvent-free biphasic systems: Pickering interfacial catalysts over amphiphilic silica nanoparticles. J Am Chem Soc 136:4869–4872. https://doi.org/10.1021/ja501019n

3. 	Oc HH, Yoon KB, Soon YJ (2008) Carbon-13 CP MAS NMR study on structures of octadecyl chains influenced by co-presence of 3-aminopropyl chains on SBA-15. Bull Korean Chem Soc 29:405–407. https://doi.org/10.5012/bkcs.2008.29.2.405

4. 	Ma K, Werner-Zwanziger U, Zwanziger J, Wiesner U (2013) Controlling growth of ultrasmall sub-10 nm fluorescent mesoporous silica nanoparticles. Chem Mater 25:677–691. https://doi.org/10.1021/cm303242h