Figure S1: Distribution of REEs (represented as Ce3+) species at pH 1 to 12. According to the Hydra and Medusa software, 1000 mg/L Ce3+.

Figure S2: Graphical determination of point of zero care (pHzpc) for the magnesium fluoride surface.

Figure S3: Nonlinear pseudo-first-order model (PFOM) (red curve) and pseudo-second-order model (PFSOM) (blue curve) for REEs adsorption onto magnesium fluoride.

Figure S4: Nonlinear Langmuir model (blue curve) and Freundlich model (red curve) for REEs adsorption onto magnesium fluoride.

Table S1: Chemical compositions of total rare earth elements sourced from NMA.

| REEs Elements | Concentration mg/L |
| --- | --- |
| La | 182625 |
| Ce | 222109.6 |
| Pr | 67414.4 |
| Nd | 55430.6 |
| Sm | 7285.2 |
| Eu | 327.8 |
| Gd | 2267.4 |
| Tb | 497.6 |
| Dy | 1119 |
| Ho | 26 |
| Er | 172.8 |
| Tm | -- |
| Yb | 48.6 |
| Lu | 3.6 |
| Sc | 11.2 |
| Y | 2783.4 |

Table S2: Mediterranean Sea sample analysis (major constituents).

| Element | Concentration mg/l |
| --- | --- |
| Mg | 1500 |
| Ca | 492 |
| K | 920 |
| Na | 1022 |

Table S3: Interference findings of REEs separation over MgF2 at pH 1 (ion exchange mechanism) and at pH 4 (adsorption mechanisms).

| Interfering ion | pH 1 (Exchange) |  |  | pH 4 (Exchange) |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | REEs uptake |  | REEs % | REEs uptake |  | REEs % |
|  | Uptake decline | Uptake decline % |  | Uptake decline | Uptake decline % |  |
| Na | 301 | 0. 46 | 75.25 | 301 | 0.46 | 75.25 |
| K | 300.5 | 0.79 | 75.15 | 302 | 0.13 | 75.5 |
| Ba | 299.5 | 0.96 | 74.8 | 300 | 0.8 | 75 |
| Al | 300.9 | 0.49 | 75.2 | 261 | 13.7 | 65.2 |
| Fe | 300.4 | 0.78 | 75.1 | 254 | 14.7 | 63.5 |
| Zn | 301.2 | 0.39 | 75.3 | 295 | 2.45 | 73.7 |
| Cu | 302 | 0.13 | 75.5 | 301 | 0.48 | 75.25 |
| Sn | 301.6 | 0.26 | 75.4 | 298 | 1.45 | 75.4 |

All finding were calculated relative to optimum REEs saturation capacity of 302.4 mgg-1 and optimum REEs % is 75.6%.

Table S4: Nonlinear constants and parameters for PFOM and PSOM of REEs adsorption onto magnesium fluoride.

| Kinetic model | qmax mg.g-1 | R2 | Order constant |
| --- | --- | --- | --- |
| Pseudo First order | 387.7 | 0.96 | K1 =0.0009 |
| Pseudo second order | 314.9 | 0.979 | K2 =0.0667 |

Table S5: Nonlinear constants and parameters for the Langmuir and Freundlich model of REEs adsorption onto magnesium fluoride.

| Isotherm model | qmax | R2 | Model constant |
| --- | --- | --- | --- |
| Langmuir model | 397 | 0.73 | KL =0.0114 |
| Freundlich model |  | 0.888 | KF =41.8, n-1=0.35 |

Table S6. Several second-group fluoride saturation capacities for REEs at pH 4.

| qe | REE% | Second group |
| --- | --- | --- |
| 302.4 | 75.6 | MgF2 |
| 285.5 | 71.4 | CaF2 |
| 229.1 | 57.5 | BaF2 |
| 190.8 | 47.7 | SrF2 |

Table S7: Comparison of MgF2 with different materials for REEs separation.

| Materials | REEs uptake mgg-1 |
| --- | --- |
| intercalated cellulose nanocomposite | 300 |
| barite-gypsum composite | 168.05 |
| activated talc | 68 |
| Phosphogypsum | 357 |
| composite hybrid nanomaterials | 139.09 |
| two-dimensional titanium carbide nanosheets | 229.85 and 175.83 |
| Poly(acrylic acid–co-acrylamide/16, 16-dimethylheptadecan-1-amine) Composite | 182.1 |