ONLINE RESOURCES

Synthesis of MgAl2O4 by Sol-Gel Method and Investigation of Catalytic Performances in CO2 Methanation

Duygu Yeşiltepe-Özçelik1,2*, Utku Burgun3,4, Faruk Kaya1, Emircan Uysal1, Bora Derin1, Andreas Schaefer5,6, Per-Anders Carlsson5,6, Gamze Gümüşlü-Gür3,4, Alper Sarıoğlan3,4, Sebahattin Gürmen1

1 Department of Metallurgical and Materials Engineering, Istanbul Technical University, 34469, Istanbul, Turkey

2 Department of Mechanical Engineering, Osmaniye Korkut Ata University, 80000, Osmaniye, Turkey

3 Department of Chemical Engineering, Istanbul Technical University, 34469, Istanbul, Turkey

4 ITU Synthetic Fuels and Chemicals Technology Center, ITU-SENTEK, Istanbul Technical University, 34469, Istanbul, Turkey

5 Department of Chemistry and Chemical Engineering, Chalmers University of Technology, Kemigården 4, 41296, Gothenburg, Sweden

6 Competence Centre for Catalysis, Chalmers University of Technology, Kemigården 4, 41296, Gothenburg, Sweden

*Corresponding author: yesiltepe15@itu.edu.tr

Fig. S1 TGA-DTG curves of the uncalcined MA support under air atmosphere.

Fig. S2 XRD analysis results between 2theta=30-90º of the spent NiCo-MA catalysts plus SiO2 mixture. NiCo700spent (black curve), NiCo800spent (red curve), and NiCo900spent (blue curve).

(c)

Fig. S3 EDS analysis results and X-ray mapping (a) MA calcined at 800 °C, (b) NiCo-MA-800 fresh catalyst, (c) NiCo-MA-800 spent catalyst.

Fig. S4 TEM-EDS mapping results of the NiCo-MA-800 fresh catalyst. The red circles indicate a region where Co and Ni signals exhibit locally increased intensity, suggesting potential metal segregation or particle aggregation in that specific area.

Fig. S5 TEM-EDS mapping results of the NiCo-MA-800 spent catalyst.