Plant mediated synthesis of zirconium oxide nanoparticles using Jasminum officinale and screening its antimicrobial activity - An efficient Photocatalyst for decomposition of various dyes

Nazeer Abbas(a), Tanzeela Batool (a), Daoud Ali(b), Tehmina Anjum (c), Shamaila Shahzadi(d), Anjum N Sabri(e), M Akram Raza (a), Shahzad Naseem (a), Saira Riaz(a)*

a) Centre of Excellence in Solid State Physics, University of the Punjab, QAC, Lahore-54590, Pakistan

b) Department of Zoology, College of Science, King Saud university, PO Box 2455, Riyadh-11451, Saudia Arabia

(c) Department of Plant Pathology, University of the Punjab, Lahore, Pakistan

d) Waterloo institute for nanotechnology, university of waterloo, Ontario, Canada.

e) Department of Microbiology and Molecular Genetics, University of the Punjab, QAC, Lahore-54590, Pakistan

Supplementary data:

Dielectric Properties:

Dielectric properties of ceramics play a significant role in many electronic and biological applications [1-3]. The dielectric constant of zirconia samples, synthesized via a green approach, was calculated using frequency dependent responses of resistance and capacitance. Equations (1-2) were used to estimate dielectric constant (ε) and loss tangent (tanδ) [4]:

ɛ= CdɛoA										(1)

tanδ= 12πɛɛofρ									(2)

where, C, d, ɛo, A and ρ are capacitance, thickness of specimen, free space permittivity, area and resistivity, respectively.

Differences in ɛ and tanδ as a function of frequency are shown in Fig. S1. The usual dispersion behaviour was evident for all samples in the low frequency region. Space charges required sufficient time, at low frequency values, for their alignment with the applied frequency producing a normal dispersion trend. However, these space charges don’t have adequate time to become aligned in the direction of the applied field when the frequency is increased, thus producing small values of dielectric constant.

When dipoles align themselves to create maximum polarisation in the direction of the applied field, this is known as the relaxation time for dielectric substances. Dipoles quickly flip between low frequency values in response to an applied field that causes the dielectric constant to be high at low frequencies. Conversely, dipole flipping typically does not follow the direction of high frequency applied fields, resulting in a lower dielectric constant at high frequencies [3].

Change in dielectric constant agrees with the Debye model; if the applied frequency is less than 1/τ of the Debye relaxation time, then charge carriers contribute to the observed polarization. However, if the applied frequency is beyond 1/τ, then charge carriers cannot participate in polarization, thus leading to smaller values of dielectric constant [5, 6]. Variations in dielectric and loss tangent (at log f = 4.5) are shown in the inset of Fig. S1. Relatively higher dielectric constant values were observed for zirconia synthesized using extract of JO. Relatively smaller dielectric constant values were observed for zirconia samples prepared using extract of VV and AB.

Figure S1: (i) Dielectric constant and (ii) loss tangent of zirconia NPs prepared using extract of (a-c) VV, (d-f) AB and (g-i) JO for 0.1-0.3 M

Table S1: Comparison of the photocatalytic performance of green synthesized ZrO2 NPs with previously published literature

| Sr# | Sample | Method | Dye | Time (min) | Degradation (%) | References |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | ZrO2 | Green synthesis | Methylene blue | 240 | 91% | [7] |
| 2 | N-ZrO2 | Thermal decomposition | Methylene blue | 240 | 59% | [8] |
| 3 | ZrO2 | Precipitation | Methylene blue | 70 | 89% | [9] |
| 4 | ZrO2 | Microwave assisted | Methyl red, methyl orange, methylene blue | 120 | 74%, 62%, 57% | [10] |
| 4 | ZrO2 | Green synthesis | Methylene blue | 35 | 88% | Present Work |

Figure S2: Physiological weight loss of tomatoes with time

References:

[1] Youness, R. A., Al-Ashkar, E., & Taha, M. A. (2023). Role of porosity in the strength, dielectric properties, and bioactivity of hardystonite ceramic material for use in bone tissue engineering applications. Ceramics International, 49(24), 40520-40531.

[2] SanaUllah, I., Khan, S., Ali, D., Sajjad, A., Shamaila, S., Kanwal, Z., ... & Riaz, S. (2024). Investigation and optimization of In-Vitro behaviour of Perovskite barium titanate as a scaffold and protective coatings. Journal of the Mechanical Behavior of Biomedical Materials, 149, 106215.

[3] Tavangar, M., Heidari, F., Hayati, R., Tabatabaei, F., Vashaee, D., & Tayebi, L. (2020). Manufacturing and characterization of mechanical, biological and dielectric properties of hydroxyapatite-barium titanate nanocomposite scaffolds. Ceramics International, 46(7), 9086-9095.

[4] Macdonald, J. R., & Johnson, W. B. (2018). Fundamentals of impedance spectroscopy. Impedance spectroscopy: theory, experiment, and applications, 1-20.

[5] R. Hill, L. Dissado, Debye and non-Debye relaxation, J. Phy. C: Solid. State. Phy., 18 (1985), 3829-3836.

[6] Waqas, M., Niaz, S., Batoo, K. M., Xu, Y. B., Noor, H., Ahmad, N., Riaz, S. (2024). Exploring the microwave assisted sol-gel synthesized multivalent doped thin films of iron oxide for detailed impedance and magnetodielectric response. Solid State Sciences, 149, 107441.

[7] Shinde, H. M., Bhosale, T. T., Gavade, N. L., Babar, S. B., Kamble, R. J., Shirke, B. S., & Garadkar, K. M. (2018). Biosynthesis of ZrO2 nanoparticles from Ficus benghalensis leaf extract for photocatalytic activity. Journal of Materials Science: Materials in Electronics, 29(16), 14055-14064.

[8] H. Sudrajat, S. Babel, H. Sakai, S. Takizawa, Rapid enhanced photocatalytic degradation of dyes using novel N-doped ZrO2, J. Environ. Manage 165 (2016) 224–234.

[9] Rajesh, G., Akilandeswari, S., Govindarajan, D., & Thirumalai, K. (2020). Enhancement of photocatalytic activity of ZrO2 nanoparticles by doping with Mg for UV light photocatalytic degradation of methyl violet and methyl blue dyes. Journal of Materials Science: Materials in Electronics, 31(5), 4058-4072.

[10] Yuan, Y., Wu, Y., Suganthy, N., Shanmugam, S., Brindhadevi, K., Sabour, A., Alshiekheid, M., Chi, N.T.L., Pugazhendhi, A., & Shanmuganathan, R. (2022). Biosynthesis of zirconium nanoparticles (ZrO2 NPs) by Phyllanthus niruri extract: Characterization and its photocatalytic dye degradation activity. Food and Chemical Toxicology, 168, 113340.