Supporting Information

Sol-gel engineered diffusion-type nickel cobaltite hollow fibrous electrode for high-capacity hybrid supercapacitors

Mohammed Kukua,c, and Mohammad Arishib,c*

aDepartment of Mechanical Engineering, College of Engineering and Computer Sciences, Jazan University, Jazan 45142, Saudi Arabia

b Department of Chemical Engineering, College of Engineering and Computer Sciences, Jazan University, Jazan 45142, Saudi Arabia

cEngineering and Technology Research Center, Jazan University, P.O.Box 114, Jazan 82817, Saudi Arabia

Corresponding author: maarishi@jazanu.edu.sa

Physical Characterization: Scanning electron microscopy (SEM, ZEISS Sigma 500, field emission scanning electron microscope) equipped with Energy -dispersive X-ray spectroscopy (EDX) mapping was used to examine the morphology and elemental composition of the microstructure. X-ray diffraction (XRD, Malvern Panalytical Aeris X-ray diffractometer) analysis was performed to assess the crystalline properties of the prepared material. The surface area analysis of H-NiCo2O4 was investigated by Brunauer-Emmett-Teller (BET) analyzer (Micromeritics Instrument corporation, ASAP 2020)

Electrochemical measurements:

The electrochemical properties of the as-prepared hybrid electrodes were studied on a Biologic electrochemical analyzer using a beaker-based three-electrode cell system with an electrolyte solution of 1M KOH. The Ni foam coated with H-NiCo2O4 electrode was used as the working electrode, a platinum mesh and an Ag/AgCl electrode were used as the counter and reference electrode, orderly. The cyclic voltammetry tests were conducted in the voltage window of 0 to 0.6 V at different scan rates. The galvanostatic charge-discharge tests were carried out at different current densities within a potential range of 0 to 0.5 V. Electrochemical impedance spectroscopy was recorded at open-circuit voltage with 20 mV amplitude in a frequency range from 0.01 Hz to 100 kHz in a 1 M KOH. The specific capacitance of the electrode in three-electrode mode was calculated from the GCD curves according to the following equation.

C = I×Δtm×ΔV

where C is the specific capacitance (F/g or F/cm2), I is the discharge current (A), ∆t is the discharge time (s), ΔV is the potential window (V), and m is the mass of the active material (g). The specific energy (E) and specific power (P) of the electrodes were calculated from the following equations:

E = 1×CV22×3.6;

P = EΔt,

where E is the specific energy (Wh/kg), C is the specific capacitance (F/g), ΔV is the potential range (V), P is the specific power (W/kg) and Δt is the discharge time (s).

Coin-cell type asymmetric supercapacitor (ASC)

The device was assembled in a coin-cell using H-NiCo2O4 and commercial activated carbon composite was used as negative electrode. The negative electrode was prepared by casting a slurry of the electroactive material: activated carbon, carbon black and PVdF binder with a weight ratio of 8:1:1 in N-methyl-2-pyrrolidine (NMP) onto a nickel foam current collector and then the electrode was pressed and dried at 60 °C overnight. To assemble the cell, the negative electrode and positive electrode were placed face to face with a filter paper that was coated with PVA-KOH gel electrolyte.

Figure S1. Preparation process of H-NiCo2O4 and AC electrodes using PVdF binder and carbon black as conductive additive. The mixture of these blends was made into slurry using few drops of N-methyl pyrrolidone and casted on Ni foam current collector.

Figure S2. CV curves of HySC device at different scan rates of 5-50 mV s-1.

Table S1. Specific energy storage performance and cycling stability of various mixed metal oxides (CuCo2O4, NiCo2O4 and ZnCo2O4) redox type electrodes with our hybrid nanoarchitecture.

| Synthesis process | Nanostructured shape | Specific capacitance or capacity | Cycling stability | SI Ref. |
| --- | --- | --- | --- | --- |
| Co-precipitation | Nanosheets | 291 F/g (40.4 mAh/g) | No decay | [1] |
| Hydrothermal | Microsphere | 284 F/g (37 mAh/g) | 75.6% (1000 cycles) | [2] |
| Dry synthesis | Nanoparticles with rhombohedral | 306.1 F/g | 96.1% (10000 cycles) | [3] |
| Hydrothermal | Nanoplates | 132 F/g | 86% (2000 cycles) | [4] |
| Room-temperature (RT) and heating process | Nanoflowers | 225 F/g (31.2 mAh/g) | 88% (1000 cycles) | [5] |
| Sol-gel process | Nanoparticles | 243 F/g | 100% (5000 cycles) | [6] |
| Wet-chemical and annealing process | Hexagonal nanoplates | 105.8 mAh/g | No fading | [7] |
| Electrochemical deposition | Nanosheets | 290 and 250 F/g | 95% (1000 cycles) | [8] |
| Combustion method | Cauliflower-shaped nanostructures | 338 F/g (46.9 mAh/g) | 77% (1000 cycles) | [9] |
| Solvothermal | Nanorods | 188 F/g | 93% (1000 cycles) | [10] |
| Sol-gel process | Porous crystals | 217 F/g | 96.3% (600 cycles) | [11] |
| Wet-chemical process | Hybrid nanostructures | 313.3 F/g (34.8 mAh/g) | 93.6% (8000 cycles) | [12] |
| Sol-gel process | Hollow fibers | 648.5 F g-1 (383.9 C g-1) | 85.6% after 7000 cycles | This work |

SI Reference

[1] P. Liang, F. Wang, Z.-A. Hu, Controlled synthesis of ordered sandwich CuCo2O4/reduced graphene oxide composites via layer-by-layer heteroassembly for high-performance supercapacitors, Chemical Engineering Journal 350 (2018) 627-636.

[2] S.K. Hussain, J.S. Yu, HMTA-assisted uniform cobalt ions activated copper oxide microspheres with enhanced electrochemical performance for pseudocapacitors, Electrochimica Acta 258 (2017) 388-395.

[3] M. Al-Aqeel, Liquid-free simple synthesis of nickel cobaltite nanostructures for high-performance supercapacitors and electrocatalyst applications, Journal of Solid State Electrochemistry  (2025).

[4] T. Kim, A. Ramadoss, B. Saravanakumar, G.K. Veerasubramani, S.J. Kim, Synthesis and characterization of NiCo2O4 nanoplates as efficient electrode materials for electrochemical supercapacitors, Applied Surface Science 370 (2016) 452-458.

[5] A. Fathi, M. Eskandari, P.T. Antelo, E. Saievar-Iranizad, ZIF-derived Cu doped Co3O4/RGO composites for asymmetric supercapacitors, Solid State Sciences 132 (2022) 106967.

[6] M. Zhang, S. Guo, L. Zheng, G. Zhang, Z. Hao, L. Kang, Z.-H. Liu, Preparation of NiMn2O4 with large specific surface area from an epoxide-driven sol−gel process and its capacitance, Electrochimica Acta 87 (2013) 546-553.

[7] F. Semerci, H. Eşgin, Step-wise synthesis of mesoporous CuCo2O4@reduced graphene oxide composites for supercapacitor applications, Journal of Electroanalytical Chemistry 970 (2024) 118550.

[8] S. Sahoo, K.K. Naik, C.S. Rout, Electrodeposition of spinel MnCo2O4 nanosheets for supercapacitor applications, Nanotechnology 26(45) (2015) 455401.

[9] A. Pendashteh, M.S. Rahmanifar, R.B. Kaner, M.F. Mousavi, Facile synthesis of nanostructured CuCo2O4 as a novel electrode material for high-rate supercapacitors, Chemical Communications 50(16) (2014) 1972-1975.

[10] L. Ren, J. Chen, X. Wang, M. Zhi, J. Wu, X. Zhang, Facile synthesis of flower-like CoMn2O4 microspheres for electrochemical supercapacitors, RSC Advances 5(39) (2015) 30963-30969.

[11] Y.Q. Wu, X.Y. Chen, P.T. Ji, Q.Q. Zhou, Sol–gel approach for controllable synthesis and electrochemical properties of NiCo2O4 crystals as electrode materials for application in supercapacitors, Electrochimica Acta 56(22) (2011) 7517-7522.

[12] Al-Aqeel, M. Formation of hybrid nanoarchitectured CuCo2O4 as a binder-free redox-type electrode for high-rate performance supercapacitors. J Porous Mater 32, (2025), 2151–2162